Q=A2gh,	(1)

where Q: volumetric flow rate (m3/s);
A: area of the orifice (m2);

h: water height above the pipe (m);

g: gravitational acceleration (9.8 m/s2).

However, the flow rate in a uniformly sized porous medium can be expressed by the Blake–Kozeny equation, as shown in Equation 2. MacDonald et al. (1991) noted that Equation 2 was well matched with the experimental results.

QA=d2(1-ε)2150μφε3△p	(2)

where Q: volumetric flow rate in a porous medium (m3/s);

A: pond area (m2);

ε: porosity in the layer (-);

μφ: coefficient of kinematic viscosity of water (Pa·s);

d: particle diameter (m);

|△p|: differential pressure (Pa).

Rl=334πWsnoρD,	(4)

where Ws: dry weight of the iron deposit recovered at the orifice (g);

ρD: distribution density of the iron deposit in the glass bead layer (g/m3);

no: number of orifices (-).

Because the water flowing into the pipes and orifices is directly related to their respective cross-sectional area, the number of orifices, no, is expressed in terms of the diameter of the pipe, DL, and the diameter of the orifice, DC, as per Equation 3.

no=DLDo2.	(3)