Electronic supplementary material

Achieving porous carbon fibers pretreated with a swarm of CO2 micro-nanobubbles

S1. Properties of pitch by various softening points. With a fairly high reaction temperature, pitch resulted in a formation of large condensed and planar molecules. This allows an increase in viscosity and softening point. Herein, a softening point of 300 °C successfully shaped mesophase texture from domain-like to fiber-like.

| Sample | C (wt %) | H (wt %) | N (wt %) | O (wt %) | Total (wt %) |
| --- | --- | --- | --- | --- | --- |
| Raw pitch | 92.6 | 3.1 | 0.2 | 4.1 | 100 |
| Softening point (°C) | TSa (wt %) | TI-PSb (wt %) | PIc (wt %) | Mesophase content (φ %) | Mesophase texture |
| 280 | 4.4 | 9.9 | 85.7 | 100 | Domain-like |
| 290 | 3.6 | 7.3 | 89.1 | 100 | Domain-like |
| 300 | 2.5 | 5.8 | 91.6 | 100 | Fiber-like |

aToluene soluable.

bToluene insoluble but pyridine soluble.

cPyridine insoluble.

S2. Textural properties of samples treated with various activation temperature ranges. With increasing activation temperature from 850 to 880 °C, the porous structure has gradually consolidated as can be seen in BET growth. Regardless of the activation temperature, all samples show the dominance of micropores over macropores. However, the trinity of surface characteristics has an apparent improvement with the increase of activation temperature. The surface characteristics have experienced decrease from 890 °C by the collapse of pore structures.

S3. Comparison of physical properties of samples prepared by various CO2 treatments.

| Sample | SBETa (m2 g-1) | SMb (m2 g-1) | SEc (m2 g-1) | %SMd | %Yield |
| --- | --- | --- | --- | --- | --- |
| ACF-3 | 735 | 488 | 247 | 66.4 | 73.12 |
| ACF-6 | 1209 | 875 | 334 | 72.4 | 62.01 |
| BACF-3 | 792 | 584 | 208 | 73.7 | 64.96 |
| BACF-6 | 1395 | 1159 | 236 | 83.1 | 53.89 |

aSpecific surface area determined via Brunauer-Emmett-Teller (BET) method.

bTotal micropore volume.

cTotal pore volume excluding micropore volume.

dProportion of micropores over specific surface area.

S4. Comparison of chemical properties of samples prepared by various CO2 treatments.

| Sample | X-ray photoelectron spectroscopy (%at) |  |  | Energy-dispersive X-ray spectrometer (%at) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | C | O | N | C | O | N |
| ACF-6 | 92.01 | 7.04 | 0.95 | 91.11 | 6.54 | 2.35 |
| BACF-6 | 89.70 | 9.40 | 0.90 | 87.60 | 10.04 | 2.36 |