Supplementary Information for

Bridging synthesis and controllable doping of monolayer 4-inch transition-metal dichalcogenides single crystals with record-breaking electron mobility

Hui Li1,#, Junbo Yang1,#, Xiaohui Li1,#, Quankun Luo2, Mo Cheng1, Wang Feng1, Ruofan Du1, Yuzhu Wang1, Luying Song1, Xia Wen1, Yao Wen3, Mengmeng Xiao4, Lei Liao5, Yanfeng Zhang6, Jianping Shi1*, Jun He3*

1The Institute for Advanced Studies, Wuhan University, Wuhan 430072, China

2Hunan Institute of Advanced Sensing and Information Technology, Xiangtan University, Xiangtan 411105, China

3Key Laboratory of Artificial Micro- and Nano-structures of Ministry of Education, School of Physics and Technology, Wuhan University, Wuhan 430072, China

4Key Laboratory for the Physics and Chemistry of Nanodevices and Center for Carbon-based Electronics, School of Electronics, Peking University, Beijing 100871, China

5College of Semiconductors, School of Physics and Electronics, Hunan University, Changsha 410082, China

6School of Materials Science and Engineering, Peking University, Beijing 100871, China

*Address correspondences: jianpingshi@whu.edu.cn, He-jun@whu.edu.cn

#These authors contributed equally to this work.

Supplementary Fig. 1 | CVD synthesis of 4-inch Fe-MoS2 single crystals on c-plane sapphire, with MoO3 and sulphur powders as the precursors. The temperatures of sulphur and MoO3 powders are set to be ~150 and ~900 °C, respectively.

Supplementary Fig. 2 | OM images of as-grown monolayer Fe-MoS2 captured from the different areas of 4-inch c-plane sapphire, showing the unidirectionally aligned feature of Fe-MoS2.

Supplementary Fig. 3 | XPS characterizations of as-grown Fe-MoS2 on c-plane sapphire. a,b, The Mo 3d and S 2p spectra of as-grown Fe-MoS2 on c-plane sapphire. The characteristic peaks at ~233.2 and ~230.1 eV are attributed to Mo 3d3/2 and 3d5/2, and the characteristic peaks at ~164.1 and ~162.9 eV are in line with S 2p1/2 and S 2p3/2, respectively. c, The Fe 2p spectrum of as-grown Fe-MoS2 on c-plane sapphire. The characteristic peak at ~712.9 eV is corresponded to Fe-S.

Supplementary Fig. 4 | Raman and PL characterizations of as-grown monolayer Fe-MoS2 and pristine monolayer MoS2 on c-plane sapphire. The red-shift of A1g mode and the reduced PL intensity indicate the n-type doping effect of Fe on monolayer MoS2.

Supplementary Fig. 5 | OM images of as-grown monolayer Fe-MoS2 on c-plane sapphire, synthesized at different growth time. After increasing the growth time to ~60 minutes, the single-crystal Fe-MoS2 monolayer films are synthesized on c-plane sapphire.

Supplementary Fig. 6 | The determination of single-crystal feature of 4-inch monolayer Fe-MoS2 film. a, SAED patterns captured from nine different areas of monolayer Fe-MoS2 film, revealing the nearly identical lattice orientations and confirming the single-crystal feature. b, Corresponding SAED intensities along the white boxes in (a).

Supplementary Fig. 7 | The determination of chemical constitutions and their distributions. a–c, EDS mapping images of Mo, S, and Fe, respectively. The uniform color contrast within the domain reveals the high crystalline quality of monolayer Fe-MoS2. d, Quantified elemental analysis of Fe-MoS2. The Fe doping concentration is determined to be ~4%.

Supplementary Fig. 8 | OM image of two merged unidirectional alignment Fe-MoS2 domains on c-plane sapphire.

Supplementary Fig. 9 | The morphologies of c-plane sapphire surfaces annealing at different conditions. a–c, AFM images of c-plane sapphire annealing at ~900 ℃ for 5 minutes without the presence of FeCl2, showing the distorted steps on surfaces. d–f, AFM images of c-plane sapphire annealing at ~900 ℃ for 5 minutes with the presence of FeCl2, showing the perfect parallel steps on surfaces.

Supplementary Fig. 10 | Schematic diagram of monolayer Fe-MoS2 back-gated FET across the merged area of two unidirectionally aligned domains.

Supplementary Fig. 11 | The device performances of large-channel monolayer Fe-MoS2 back-gated FET. a, Output characteristic curve of a large-channel monolayer Fe-MoS2 back-gated FET. b, Transfer characteristic curves of monolayer Fe-MoS2 back-gated FETs with different channel lengths. Inset: OM image of monolayer Fe-MoS2 back-gated FETs with different channel lengths.

Supplementary Fig. 12 | Temperature-dependent electrical measurements of a monolayer Fe-MoS2 back-gated FET. a, Temperature-dependent transfer characteristic curves of a monolayer Fe-MoS2 back-gated FET. b, The electron mobility evolution for a monolayer Fe-MoS2 back-gated FET as a function of temperature. c, Arrhenius plots of a monolayer Fe-MoS2 back-gated FET. The deviation from the thermionic emission model and almost saturated slopes at low temperatures are obviously observed, indicating the disappearance of energy barrier.

Supplementary Fig. 13 | OM images of as-grown monolayer Fe-WS2 captured from the different areas of 4-inch c-plane sapphire, showing the unidirectionally aligned feature of Fe-WS2.

Supplementary Fig. 14 | The determination of single-crystal feature of 4-inch monolayer Fe-WS2 film. a, SAED patterns captured from twelve different area of monolayer Fe-WS2 film, revealing the nearly identical lattice orientations and confirming the single-crystal feature. b, Corresponding SAED intensities along the white boxes in (a).

Supplementary Fig. 15 | XPS characterization of as-grown Fe-WS2 on c-plane sapphire. a,b, The W 4f and S 2p spectra of as-grown Fe-WS2 on c-plane sapphire, respectively. The characteristic peaks at ~36.0 and ~33.8 eV are attributed to W 4f5/2 and 4f7/2, and the characteristic peaks at ~164.1 and ~162.9 eV are in line with S 2p1/2 and S 2p3/2, respectively. c, The Fe 2p spectrum of as-grown Fe-WS2 on c-plane sapphire. The characteristic peak at ~712.9 eV is corresponded to Fe-S.

Supplementary Fig. 16 | The determination of chemical constitutions and their distributions. a–c, EDS mapping images of W, S, and Fe, respectively. The uniform color contrast within the domain reveals the high crystalline quality of monolayer Fe-WS2. d, Quantified elemental analysis of Fe-WS2. The Fe doping concentration is determined to be ~5%.

Supplementary Fig. 17 | Raman and PL characterizations of as-grown monolayer Fe-WS2 and pristine monolayer WS2 on c-plane sapphire. The red-shift of A1g mode and the reduced PL intensity indicate the n-type doping effect of Fe on monolayer WS2.

Supplementary Table 1. Comparison of the device performances of monolayer Fe-MoS2 with the other MoS2

| Synthesis method | Layer number | Channel length (μm) | Gate oxide | Mobility (cm2 V–1 s–1) | Ref. |
| --- | --- | --- | --- | --- | --- |
| CVD | 1 | 1 | 300 nm SiO2 | 15 | 1 |
| CVD | 1 | 10 | 300 nm SiO2 | 7.33 | 2 |
| CVD | 1 | 20 | 20 nm ZrO2 | 17 | 3 |
| CVD | 2 | 8 | 25 nm Al2O3 | 122.6 | 4 |
| CVD | 1 | 1 | 20 nm Al2O3 | 54 | 5 |
| CVD | 2 | 0.04 | 11 nm HfO2 | 36 | 6 |
| CVD | 2 | 2 | 22 nm Al2O3 | 3 | 7 |
| CVD | 1 | 1 | 285 nm SiO2 | 35 | 8 |
| CVD | 1 | 20 | 20 nm HfO2 | 65.7 | 9 |
| CVD | 1 | 10 | 20 nm Al2O3 | 102.6 | 10 |
| CVD | 1 | 2 | 16 nm SrTiO3 | 39.7 | 11 |
| CVD | 1 | 10 | 90 nm SiO2 | 49 | 12 |
| MOCVD | 1 | 1 | 100 nm SiNx | 55 | 13 |
| MOCVD | 1 | 5 | 50 nm Al2O3 | 30 | 14 |
| Exfoliated | 3 | 2 | 285 nm SiO2 | 60 | 15 |
| Exfoliated | 1 | 1.2 | 100 nm SiO2 | 50 | 16 |
| Exfoliated | 1 | 2 | 30 nm Al2O3 | 41 | 17 |
| Exfoliated | 2 | 0.001 | 5.8 nm ZrO2 | 65 | 18 |
| Solution synthesis | 4 | 50 | 90 nm SiO2 | 7~11 | 19 |
| CVD | 1 | 10 | 285 nm SiO2 | 231 | This work |

Supplementary Table 2. Comparison of the contact resistances of monolayer Fe-MoS2 with the other MoS2

| Type of MoS2 | Electrode | Contact resistance (KΩ μm) | Ref. |
| --- | --- | --- | --- |
| Exfoliated remote modulation doped trilayer MoS2 | Cr/Au | 6~15 | 15 |
| CVD synthesized O-doped monolayer MoS2 | Ni/Au | 1 | 1 |
| CVD synthesized monolayer MoS2 | In/Au | 3 | 20 |
| CVD synthesized monolayer MoS2 | Bi | 0.123 | 13 |
| CVD synthesized monolayer MoS2 | Au/Ti/Au | 2.9 | 21 |
| CVD synthesized monolayer MoS2 | WTe2 | 57~67 | 2 |
| CVD synthesized monolayer MoS2 | Graphene | 10 | 3 |
| CVD synthesized monolayer MoS2 | Ni/Au | 9.2 | 14 |
| Exfoliated few-layer MoS2 | Ag | 2 | 22 |
| Exfoliated monolayer MoS2 | Au | 200 | 23 |
| Exfoliated multilayer MoS2 | Pd | 430 | 24 |
| CVD synthesized monolayer Fe-MoS2 | Cr/Au | 0.489 | This work |

- Shen, P.-C. et al. Healing of donor defect states in monolayer molybdenum disulfide using oxygen-incorporated chemical vapour deposition. Nat. Electron. 5, 28–36 (2022).

- Song, S. et al. Wafer-scale production of patterned transition metal ditelluride layers for two-dimensional metal-semiconductor contacts at the Schottky-Mott limit. Nat. Electron. 3, 207–215 (2020).

- Zhao, M. et al. Large-scale chemical assembly of atomically thin transistors and circuits. Nat. Nanotechnol. 11, 954–959 (2016).

- Liu, L. et al. Uniform nucleation and epitaxy of bilayer molybdenum disulfide on sapphire. Nature 605, 69–75 (2022)

- Meng, W. Q. et al. Three-dimensional monolithic micro-LED display driven by atomically thin transistor matrix. Nat. Nanotechnol. 16, 1231–1236 (2021).

- Gao, Q. G. et al. Scalable high performance radio frequency electronics based on large domain bilayer MoS2. Nat. Commun. 9, 4778 (2018).

- Wachter, S., Polyushkin, D. K., Bethge, O. & Mueller, T. A microprocessor based on a two-dimensional semiconductor. Nat. Commun. 8, 14948 (2017).

- Li, S. S. et al. Vapour-liquid-solid growth of monolayer MoS2 nanoribbons. Nat. Mater. 17, 535–542 (2018).

- Ma, S. L. et al. A 619-pixel machine vision enhancement chip based on two-dimensional semiconductors. Sci. Adv. 8, eabn9328 (2022).

- Li, T. T. et al. Epitaxial growth of wafer-scale molybdenum disulfide semiconductor single crystals on sapphire. Nat. Nanotechnol. 16, 1201–1207 (2021).

- Huang, J.-K. et al. High-κ perovskite membranes as insulators for two-dimensional transistors. Nature 605, 262–267 (2022).

- Chang, M.-C. et al. Fast growth of large-grain and continuous MoS2 films through a self-capping vapor-liquid-solid method. Nat. Commun. 11, 3682 (2020).

- Shen, P.-C. et al. Ultralow contact resistance between semimetal and monolayer semiconductors. Nature 593, 211–217 (2021).

- Sebastian, A., Pendurthi, R., Choudhury, T. H., Redwing, J. M. & Das, S. Benchmarking monolayer MoS2 and WS2 field-effect transistors. Nat. Commun. 12, 693 (2021).

- Lee, D. et al. Remote modulation doping in van der Waals heterostructure transistors. Nat. Electron. 4, 664–670 (2021).

- Kappera, R. et al. Phase-engineered low-resistance contacts for ultrathin MoS2 transistors. Nat. Mater. 13, 1128–1134 (2014).

- Yu, Z. H. et al. Atomristors: memory effect in atomically-thin sheets and record RF switches. In 2018 IEEE International Electron Devices Meeting (IEDM) 22.6.1–22.6.4 (IEEE, 2018).

- Desai, S. B. et al. MoS2 transistors with 1-nanometer gate lengths. Science 354, 99–102 (2016).

- Lin, Z. Y. et al. Solution-processable 2D semiconductors for high-performance large-area electronics. Nature 562, 254–258 (2018).

- Wang, Y. et al. Van der Waals contacts between three-dimensional metals and two-dimensional semiconductors. Nature 568, 70–74 (2019).

- Li, N. et al. Large-scale flexible and transparent electronics based on monolayer molybdenum disulfide field-effect transistors. Nat. Electron. 3, 711–717 (2020).

- Wang, J. L. et al. Transferred metal gate to 2D semiconductors for sub-1 V operation and near ideal subthreshold slope. Sci. Adv. 7, eabf8744 (2021).

- Liu, G. Y. et al. Graphene-assisted metal transfer printing for wafer-scale integration of metal electrodes and two-dimensional materials. Nat. Electron. 5, 275–280 (2022).

- Wang, Y. et al. P-type electrical contacts for two-dimensional transition metal dichalcogenides. Nature 610, 61–66 (2022).