Supplementary Information

The performance of Cu2+ as dissolved cathodic electron-shuttle mediator for Cr6+ reduction in the microbial fuel cell

Praveena Gangadharan1* and Indumathi M Nambi2

1 Department of Civil Engineering, Indian Institute of Technology Palakkad

Kerala – 678557, India.

2 Environmental and Water Resources Engineering Division, Department of Civil Engineering,

Indian Institute of Technology, Madras-600036, India.

*Corresponding Author. Tel.: - +91 - 49 - 23226473. Fax: - +91-49-23226301

E-mail Address: praveenag@iitpkd.ac.in

1. Pourbaix diagram for chromium and copper

Pourbaix diagram was constructed based on the potentials (E in V) for cathodic reduction is a function of chromium ion concentration/activity ([Cr6+] in mM) and the pH of the system. In the present study, the chromium species considered for constructing the Pourbaix diagram are [Cr6+], [Cr3+] and Cr2O3. The initial total chromium [CrT] concentration and [Cr6+] concentrations are considered as equal, and 100 mg/L of [CrT] or [Cr6+] was used throughout the experiment. Therefore, the adopted concentration/activity of [Cr6+] was 1.92 mM for constructing the Pourbaix diagram. In addition, the activity/concentration of [Cr3+] was considered as 2.88 mM as the removal efficiency of 99.85% (reduction of [Cr6+] to [Cr3+]) achieved in the experimental study.

Similarly, the copper species considered for constructing the Pourbaix diagram are [Cu2+], [Cu0], [CuO], and [Cu2O]. According to the experimental condition, the total [Cu2+] concentration adopted was 1.57 mM (100 mg/L). Table S1 shows the free energy of formation (∆G0) of elements at the standard condition and expressed in kilojoules per mole.

Table 1.  Free energy of formation of elements in a Cr-Cu-H2O system at standard condition.

| Sl. No | Formula | ∆G0 KJ/mol |
| --- | --- | --- |
| 1 | HCrO4- | -761.4 |
| 2 | H+ | 0 |
| 3 | OH- | -37,595 | -37,595 |
| 4 | Cr3+ | -198.3 |
| 5 | H2O | -237.14 |
| 6 | Cr2O3 | -1059.3 |
| 7 | Cu+ | +12,000 |
| 8 | Cu2+ | +15,530 |
| 9 | Cu2O | -34,980 |
| 10 | CuO | -30,400 |

1.1 Thermodynamic calculation

The half-cell reaction of an electrochemical reaction is represented as follows.

| aA + mH+ + ne ↔ bB + cH2O | 1 |
| --- | --- |

Where a, m, b, and c are the stoichiometric coefficients for species A, H+, B, and H2O in the electrochemical reaction, respectively; and n is the electron transfer number of the electrode reaction. The activity of water [H2O] is considered to be 1 for a dilute solution, and the corresponding equilibrium potential was represented by Nernst isothermal equation (Eq. (1)).

| E = | E0 – 2.303 m R Tn F pH-2.303 R Tn Flog10aBbaAa | Eq. 1 |
| --- | --- | --- |

Where,

E = Electrochemical potential for a reaction at temperature, T.

E0= Standard electrochemical potential for a reaction at standard temperature, (298.15 K).

F = Faraday’s constant (96.485 KJ/volt or 23061 cal/volt).

R = Universal gas constant (8.314 J/mol. K or 1.98 cal/K).

aA and aB are the overall activity of species A and B, respectively.

The relationship between the potential, pH, and ∆G0 is represented in Eq. (2):

| ∆G0= | -RT lnK= -nFE0 | Eq. 2 |
| --- | --- | --- |

Where, ∆G0 = Standard Gibb’s free energy of reaction at temperature, T.

K = Equilibrium constant.

Table 2 listed the thermodynamic data of the elements considered in the Cr-H2O system. To avoid the complexity in the Pourbaix diagram, the species considered in the aqueous state are [Cr6+] and [Cr3+], and the solid-state is Cr2O3. The acidic pH varied from 0 to 6 was adopted for the construction Pourbaix diagram.

Table 2.  Thermodynamic data of the elements in the Cr-Cu-H2O system.

| No | Reaction | E0 or log K | E-pH system* |
| --- | --- | --- | --- |
| 1 | O2(g)+ 4H+ + 4e- ↔ H2O(l) | 1.228 V | E = E0- (2.303 RT/F) pH +(2.303 RT/4F) log PO2 |
| 2 | 2H+ + 2e- ↔ H2(g) | 0 V | E = - (2.303 RT/F) pH +(2.303 RT/2F) log PH2 |
| 3 | HCrO4-(l) + 7 H+ +3e- ↔ Cr3+(l) + 4H2O(l) | 1.33V | E= 1.33V – 0.020 log [Cr3+] +0.020 log [HCrO4-]-0.14 pH |
| 4 | 2 Cr3+(l) + 3H2O(l) ↔ Cr2O3 (s) + 6 H+ | Log K = -8.3426 | pH = 8.346 – 2 log [Cr3+] 6 |
| 5 | Cu2+(l) + 2e- ↔ Cu0(c) | 0.337 V | E= 0.337 V + 0.0605 log [Cu2+] |
| 6 | Cu2+(l) + H2O(l) ↔ CuO (s) + 2 H+ | Log K = -8. 062 | pH = 8.062 – 2 log [Cu2+] 2 |
| 7 | 2Cu2+(l) + H2O(l) + 2e-↔ Cu2O(c) + 2 H+ | 0.2027 V | E= 0.2027 V + 0.0605 pH + 0.0605 log [Cu2+] |
| 8 | 2 CuO (s) + 2e-+ 2 H+ ↔ Cu2O(c) + H2O(l) | 0.669 V | E= 0.669 V - 0.0605 pH |
| 9 | Cu2O(c) + 2 H++ 2e- ↔ 2Cu0(c) + H2O(l) | 0.470 | E= 0.470 V – 0.0605 pH |

*Note that E0 and K values are adjusted according to the experimental temperature 305 K (320C).

Reference

- McCafferty, E. (2010). Thermodynamics of corrosion: pourbaix diagrams. In Introduction to Corrosion Science (pp. 95-117). Springer New York.

- Kotaś, J., & Stasicka, Z. (2000). Chromium occurrence in the environment and methods of its speciation. Environmental pollution, 107(3), 263-283.

- Beverskog, B., & Puigdomenech, I. (1997). Revised Pourbaix diagrams for chromium at 25–300 C. Corrosion Science, 39(1), 43-57.

- Zhang, L. J., Tao, H. C., Wei, X. Y., Lei, T., Li, J. B., Wang, A. J., & Wu, W. M. (2012). Bioelectrochemical recovery of ammonia–copper (II) complexes from wastewater using a dual-chamber microbial fuel cell. Chemosphere, 89(10), 1177-1182.