Supporting Information

Easily separated and sustainable cellulose-based adsorbent using a facile two-steps modification for highly efficient methylene blue removal

Keming Zhou,a Lianpeng Yan,a Rui Zhang,*a,b and Xuedong Zhua

a. Engineering Research Centre of Large Scale Reactor Engineering and Technology, Ministry of Education, School of Chemical Engineering, East China University of Science and Technology, 130 Meilong Road, Shanghai 200237, China.

b. Shanghai Key Laboratory of Green Chemistry and Chemical Processes, East China

Normal University, School of Chemistry and Molecular Engineering, Shanghai

200062, China.

* Corresponding authors.

E-mail address: r.zhang@ecust.edu.cn (R. Zhang).

Fig. S1 UV-Vis absorption spectrum a) and the equilibrium adsorption capacity b) using different adsorbents, pH=11, initial dye concentration of 100 mg/L, 303 K and 10 mg of absorbents.

Fig. S2 The nitrogen adsorption-desorption isotherm of M-CA/JEPP.

The measurement of nitrogen adsorption-desorption isotherms and the Brunauer–Emmett–Teller (BET) surface area towards M-CA/JEPP was carried out. As seen from Figure S2, the isotherm could be classified as type IV with an apparent hysteresis loop, revealing the presence of mesopores. The BET specific surface area of M-CA/JEPP was 34.15 m2/g.

Fig. S3 TEM images of a-c) M-CA/JEPP; d) Size distribution histogram of the synthesized Fe3O4 nanoparticles.

Fig. S4 Thermodynamic fitting of MB adsorption at different concentrations.

Adsorption kinetic models:

Pseudo-first-order model:

qt=qe1-e-k1t		(S1)

Pseudo-second-order model:

qt=qe2k2t1+qek2t		(S2)

Intraparticle diffusion model:

qt=1βlnαβ+1βlnt		(S3)

Elovich model:

qt=kp,it12+Ci		(S4)

where qt (mg/g) and qe (mg/g) are the adsorption capacity of dye adsorbed at time t (min) and at equilibrium, respectively. k1 (min-1) and k2 (g mg-1 min-1) are rate constants for pseudo-first-order and pseudo-second-order models, respectively. α (mg g-1 min) and β (g/mg) are the initial adsorption rate and the desorption coefficient for Elovich model, respectively. kp,i (mg g-1 min−0.5) and Ci (mg/g) are the rate constant of the intraparticle diffusion model and the constant related to the thickness of the boundary layer, respectively.

Adsorption isotherm models:

Langmuir model:

qe=qmaxklCe1+klCe		(S5)

Freundlich model:

qe=kfCe1/n		(S6)

Temkin model:

qe=RTbTlnAT+RTbTlnCe, RTbT=B		(S7)

where qmax (mg/g) and qe (mg/g) are the maximum adsorption capacity and equilibrium adsorption capacity, respectively. Ce (mg/L) is the equilibrium concentration of dye solution; kl (L/mg) and kf [(mg/g)/(mg/L)1/n] are empirical constants for Langmuir and Freundlich isotherms; bT, AT (L/g) and B (J/mol) are empirical constants for Temkin isotherm. R is gas constant (8.314 J mol-1 K-1) and T is temperature (K).

Separation factor:

RL=11+klC0		(S8)

where RL is a dimensionless separation factor; C0 (mg/L) is the initial dye concentration; kl (L /mg) is empirical constants for Langmuir isotherm. The value of RL predicts whether an adsorption system is irreversible (RL=0), favorable (0<RL<1), linear (RL=1), or unfavorable (RL>1).

Adsorption thermodynamic parameters were calculated as follows

lnKd=∆SR-∆HRT	(S9)

Kd=qeCe	(S10)

∆G=∆H-T∆S	(S11)

where Kd is the distribution coefficient; Ce (mg/L) and qe (mg/g) are the equilibrium concentration and adsorption capacity of dye solution, respectively. ∆G (kJ/mol), ∆S (kJ mol-1 K-1) and ∆H (kJ/mol) are Gibbs free energy change, entropy change and enthalpy change, respectively. R is gas constant (8.314 J mol-1 K-1) and T is temperature (K).

Table S1 M-CA/JEPP Adsorbent Samples Made under Various Conditions

| Samples | JEPP (g) | FeCl3·6H2O (g) | FeSO4·7H2O(g) |
| --- | --- | --- | --- |
| JEPP | 0.926 | 0 | 0 |
| M:CA/JEPP-1 | 0.926 | 1.081 | 0.695 |
| M:CA/JEPP-2 | 0.926 | 2.162 | 1.390 |
| M:CA/JEPP-3 | 0.926 | 4.324 | 2.780 |

Table S2 Thermodynamic Parameters for Different Initial Concentrations of MB on M-CA/JEPP

| Initial concentration (mg/L) | Temperature (K) | Thermodynamic parameters |  |  |
| --- | --- | --- | --- | --- |
|  |  | ΔH (kJ/mol) | ΔS [kJ/(mol K)] | ΔG (kJ/mol) |
| 50 | 303 | -5.755 | 0.026 | -13.558 |
| 50 | 313 |  |  | -13.816 |
| 50 | 323 |  |  | -14.073 |
| 50 | 333 |  |  | -14.331 |
| 100 | 303 | -9.752 | 0.009 | -12.463 |
| 100 | 313 |  |  | -12.553 |
| 100 | 323 |  |  | -12.642 |
| 100 | 333 |  |  | -12.731 |
| 150 | 303 | -4.039 | 0.014 | -8.268 |
| 150 | 313 |  |  | -8.407 |
| 150 | 323 |  |  | -8.547 |
| 150 | 333 |  |  | -8.686 |