Table 1. Optimization of the reaction conditionsa

| Entry | Catalyst | Solvent | Time/min | Yield/%b |
| --- | --- | --- | --- | --- |
| 1 | K-CN | CH2Cl2 | 30 | 31 |
| 2 | K-CN | CH3CN | 30 | 35 |
| 3 | K-CN | EL | 30 | 44 |
| 4 | K-CN | MeOH | 30 | 80 |
| 5 | K-CN | H2O | 30 | 88 |
| 6 | K-CN | EtOH | 30 | 95 |
| 7 | K-CN | EtOH/H2O (1:1) | 30 | 99 |
| 8c | K-CN | EtOH/H2O (1:1) | 25 | 93 |
| 9d | K-CN | EtOH/H2O (1:1) | 30 | 63 |
| 10e | K-CN | EtOH/H2O (1:1) | 30 | 99 |
| 11 | K-CN | EtOH/H2O (1:1) | 20 | 95 |
| 12 | K-CN | EtOH/H2O (1:1) | 10 | 47 |
| 13 | g-CN | EtOH/H2O (1:1) | 60 | 25 |
| 14 | no | EtOH/H2O (1:1) | 60 | trace |
| 15f | K-CN | EtOH/H2O(1:1) | 30 | 97 |
| a Reaction conditions: benzaldehyde (1 mmol), malononitrile (1 mmol), catalyst (10 mg) in solvent (2 ml), room temperature otherwise specified in the table. b Isolated yields. c The reaction was performed at 50 °C. d Catalyst (5 mg). e Catalyst (15 mg). f The reaction was carried out on 20 mmol scale. |  |  |  |  |

Table 2 Scope of the Knoevenagel condensation reaction catalyzed by K-CN a

Table 3 Comparison of this system with the reported Knoevenagel condensation of benzaldehyde and malononitrile

| Entry | Catalyst | Conditions | Yield (%) | Ref. |
| --- | --- | --- | --- | --- |
| 1 | MOF (JUC-199) (100 mg) | 1,4-dioxane, 90 °C, 4 h | 99 | He et al. 2016 |
| 2 | RhPt/TC@GO NPs (2 mg) | H2O/MeOH (1:2), r. t., 10 min | 99 | Şen et al. 2018 |
| 3 | KOH/SnO2 (50 mg) | DMF, r. t., 15 min | 97 | Xie et al.2015 |
| 4 | SO3H-AA@MNP (10 mg) | Toluene/H2O, 90 °C, 2 h | 94 | Wang et al.2018 |
| 5 | UiO-66-Ru (58 mg) | Toluene, 100 °C, 5 h | 89.3 | Yang et al.2018 |
| 6 | TABTA-COF (3 mol%) | Toluene/H2O, 60 °C, 1 h | 94 | Li et al. 2019 |
| 7 | N-HPC-800 (0.02 g) | EtOH, 60 °C, 6 h | 97.8 | Kong et al. 2020 |
| 8 | Ga4B2O9 (30 mg) | DMSO, 40 °C, 30 min | 90 | Yang et al. 2020 |
| 9 | Zn(II) β-oxodithioester complexes (5 mol%) | MeOH, 60 °C, 1 h | 98 | Yadav et al. 2020 |
| 10 | K-CN | EtOH/H2O, r. t., 30 min | 99 | This work |