Supporting Information

for “Feasibility of nanoscale zero-valent iron loaded sediment-based biochar (nZVI-SBC) for simultaneous removal of nitrate and phosphate: high selectivity towards dinitrogen and synergistic mechanism”

Xiaohui Liu, Jia Wei *, Liangang Hou, Yuhan Zhu, Yaodong Wu, Luyi Xing, Yifei Zhang, Jun Li

College of Architecture Engineering, Beijing University of Technology, 100 Pingleyuan, Chaoyang district, Beijing 100124, China.

Corresponding author: weij@bjut.edu.cn (Jia Wei)

Details of materials and methods

1. Materials

The sediment was sampled from the esturary of the Tonghui River (39°54′20″N; 116°33′11″E), which is a polluted river connecting the Gaobeidian sewage treatment plant (Beijing, China). A core sampler (Ø80 mm × L500 mm) was used and the sediment was transported into a laboratory with airtight polyethylene self-sealing bags within 4 h. Sediment was prepared as the precursor of SBC, and was dried, smashed and passed through a 0.15 mm sieve.

Sodium borohydride (NaBH4, ≥97.0%), potassium dihydrogen phosphate (KH2PO4, ≥99.0%), potassium nitrate (KNO3, ≥99.0%), sodium nitrite (NaNO2, ≥99.0%) and ammonium chloride (NH4Cl, ≥99.8%) were purchased from Tianjin Guangfu Development Company Limited, China. Ferrous sulfate heptahydrate (FeSO4·7H2O, 99.0-101.0%) was purchased from Sheng Ao Chemical Reagent (Tianjin, China). Anhydrous ethanol (CH3CH2OH, ≥99.7%) was purchased from Fuyu Chemical Co., Ltd (Tianjin, China). All chemicals were used as purchased without further purification, and all solutions were prepared with high purity deionized water (EC =2.0 μs·cm -1).

2. Preparation of nZVI-SBC

SBC was produced through pyrolysis of 20 g dry sediment at 400 °C for 4 h in an anaerobic muffle furnace (KABML-602A, Coal, China). The product was then smashed and passed through a 0.15 mm sieve and kept under oxygen-limited condition.

In order to prepare nZVI-SBC, a certain concentration of FeSO4·7H2O and SBC were mixed in the ultrasonic cleaning machine (Model B12, Yamato, Japan) for 1h to disperse it evenly. N2 was purged into the solution for 30 min to exclude the dissolved O2. Then excessive NaBH4 was dissolved in 20 mL of deionized water and added drop-wise to the above solution. The mixture was stirred at 120 rpm for another 30 min to complete the reaction. After settled and washed 3 times with deionized water and anhydrous ethanol respectively, the solution was finally dried by purging N2 and vacuum pump alternately.

3. Characteration

The morphology of samples was examined by scanning electron microscopy (SEM) (Vega-3XMU, Tescan, Czech). Transmission electron microscopy (TEM) images were taken by Tecnai G2 F20 S-TWIN (FEI, USA) at 200 kV to characterize the size and dispersion of nZVI on the surface of nZVI-SBC. Brunauer-Emmett-Teller (BET) specific surface areas and the pore size distribution were measured by Micromeritics ASAP 2460 (Micromeritics, USA) at 77 K. X-ray diffraction (XRD) was carried out scanning from 10° to 90° 2θ (BRUKER, Germany) and counting time of 2 s·step -1 to determine the composition. Fourier transformation infrared spectroscopy (FTIR) (Thermo, USA) was used to evaluate the functional groups over the spectra range of 400-4000 cm−1. Zeta potentials were measured by Zetasizer Nano zeta potential analyzer (Malvern Instruments, UK) at varying solution pH from 3.0 to 11.0 and the isoelectric point were determined. X-ray photoelectron spectrometer (XPS) (ESCLAB 250Xi, Thermo Fischer, USA) was used to characterize the surface composition and combination state of element with a monochromatic Al-Ka source.

4. Analytical methods

All nitrogen-containing compounds (NO3−, 220 nm and 275 nm; NO2−, 540 nm; NH4+, 420 nm) and phosphate (700 nm) were measured by a 765 UV–vis spectrophotometer (Shanghai, China). Values of DO and pH were monitored by a portable DO meter (HQ30d, Hach, USA) and a pH meter (MP220, Mettler Toledo, Switzerland) respectively. The nitrate removal efficiency and byproducts were calculated using the following equations:

RNO3-%=[NO3-]i-[NO3-]f[NO3-]i×100                   (1)               BNH4+%=[NH4+]f[NO3-]i-[NO3-]f×100            (2)                             BNO2-%=[NO2-]f[NO3-]i-[NO3-]f×100 (3)                                 BN2%=[NO3-]i-NO3-f-NH4+f-[NO2-]f[NO3-]i-[NO3-]f×100									 (4)

where [NO3−], [NH4+] and [NO2−] represent the concentration (mg·L-1) of nitrate, ammonium and nitrite, respectively. The subscripts i and f are the initial and final sampls, respectively.

Supplementary Figures

Fig. S1. Effect of dosage on removal capacity (20 NO3–-N mg·L-1, 5 PO43-P mg·L-1, pH = 7, DO = 3 mg·L-1).

Fig. S2. Effects of initial solution pH on nitrate and ammonium production (20 NO3–-N mg·L-1, 5 PO43-P mg·L-1, dosage = 2g·L-1, DO = 3 mg·L-1).

Fig. S3. Effect of DO on nitrate and ammonium production (20 NO3–-N mg·L-1, 5 PO43-P mg·L-1, dosage = 2 g·L-1, pH = 7).

Fig. S4. X-ray diffraction patterns of nVZI-SBC after reaction.

Fig. S1. Effect of dosage on removal capacity (20 NO3–-N mg·L-1, 5 PO43-P mg·L-1, pH = 7, DO = 3 mg·L-1).

Fig. S2. Effects of initial solution pH on nitrate and ammonium production (20 NO3–-N mg·L-1, 5 PO43-P mg·L-1, dosage = 2g·L-1, DO = 3 mg·L-1).

Fig. S3. Effect of Do on nitrate and ammonium production (20 NO3–-N mg·L-1, 5 PO43-P mg·L-1, dosage = 2 g·L-1, pH = 7).

Fig. S4. X-ray diffraction patterns of nVZI-SBC after reaction.