Supporting Information

Internal Electric Fields in Asymmetric Single-layer Lattices for Enhancing Photocatalytic Solar-to-Hydrogen Efficiency

Yu-Liang Liua, Yongfeng Wana, Bo Lia, Xingshuai Lvb, Chuan-Lu Yangc,*, Ying Shia,*

a Institute of Atomic and Molecular Physics, Jilin University, 130012 Changchun, China

b Beijing Computational Science Research Center (CSRC), 100193 Beijing, China

c School of Physics and Optoelectronic Engineering, Ludong University, 26425 Yantai, China

*Corresponding author. Email: shi_ying@jlu.edu.cn (Y. Shi); ycl@ldu.edu.cn (C.L. Yang)

Fig. S1| The flow diagram of stability evaluation.

Fig. S2| The enthalpies of formation Ef (eV/atom) of 22 selected MSi2N2XY monolayers.

Fig. S3| The phonon spectrum of 18 unstable MSi2N2XY monolayers.

Fig. S4| Polar diagrams of (a) Young’s modulus Y(θ) and (b) Poisson’s ratio υ(θ) for MoSi2N3P, MoSi2N3As, WSi2N3P and WSi2N3As monolayers.

Fig. S5| Band-decomposed charge density of the CBM and VBM for MSi2N4, MSi2N3P and MSi2N3As monolayers, respectively.

Fig. S6| The calculated absorption coefficients of MSi2N3Y monolayers and MSi2N4 monolayers by HSE06 functional.

Table S1. The calculated structural properties, including lattice constant (a), bond length (dSi-X/Yout and dM-X/Yin), and inner-layer height (dSi-X/Yin) for MSi2N2XY monolayers.

| Monolayers | M | a (Å) | dSi-Xout (Å) | dSi-Yout (Å) | dM-Xin (Å) | dM-Yin (Å) | hX-Yin (Å) | Distortion (Y/N) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MSi2N3P | Mo | 2.967 | 1.745 | 2.227 | 2.107 | 2.358 | 2.846 | N |
|  | W | 2.974 | 1.746 | 2.222 | 2.117 | 2.367 | 2.868 | N |
| MSi2N3As | Mo | 2.982 | 1.746 | 2.337 | 2.106 | 2.463 | 2.973 | N |
|  | W | 2.988 | 1.747 | 2.331 | 2.116 | 2.472 | 2.996 | N |
| MSi2N3S | Mo | 2.938 | 1.748 | 2.239 | 2.094 | 2.429 | 2.966 | N |
|  | W | 2.937 | 1.748 | 2.269 | 2.102 | 2.432 | 2.986 | N |
| MSi2N3Se | Mo | 2.959 | 1.749 | 2.446 | 2.095 | 2.542 | 3.094 | N |
|  | W | 2.959 | 1.747 | 2.516 | 2.103 | 2.540 | 3.106 | N |
| MSi2N3Te | Mo | 3.000 | 1.749 | 2.695 | 2.104 | 2.726 | 3.298 | N |
|  | W | 3.003 | 1.749 | 2.735 | 2.114 | 2.737 | 3.327 | N |  |
| MSi2N2PAs | Mo | 3.051 | 2.230 | 2.353 | 2.363 | 2.488 | 3.333 | N |  |
|  | W | 3.053 | 2.229 | 2.353 | 2.375 | 2.499 | 3.363 | N |  |
| MSi2N2PS | Mo | 3.007 | 2.248 | 2.200 | 2..363 | 2.448 | 3.329 | N |  |
|  | W | 3.011 | 2.252 | 2.216 | 2.376 | 2.449 | 3.344 | N |  |
| MSi2N2PSe | Mo | 3.034 | 2.241 | 2.396 | 2.345 | 2.579 | 3.452 | N |  |
|  | W | 3.040 | 2.245 | 2.424 | 2.361 | 2.584 | 3.475 | N |  |
| MSi2N2PTe | Mo | 3.072 | 2.237 | 3.854 | 2.351 | 2.751 | 3.646 | Y |  |
|  | W | 3.091 | 2.236 | 3.881 | 2.366 | 2.736 | 3.628 | Y |  |
| MSi2N2AsS | Mo | 3.025 | 2.371 | 2.198 | 2.493 | 2.405 | 3.432 | N |  |
|  | W | 3.032 | 2.375 | 2.218 | 2.501 | 2.418 | 3.453 | N |  |
| MSi2N2AsSe | Mo | 3.055 | 2.367 | 2.398 | 2.463 | 2.543 | 3.551 | N |  |
|  | W | 3.059 | 2.370 | 2.432 | 2.476 | 2.552 | 3.578 | N |  |
| MSi2N2AsTe | Mo | 3.092 | 2.363 | 3.871 | 2.460 | 2.723 | 3.749 | Y |  |
|  | W | 3.028 | 2.379 | 2.760 | 2.452 | 3.150 | 4.339 | Y |  |
| MSi2N2SSe | Mo | 3.023 | 2.217 | 2.440 | 2.327 | 2.637 | 3.515 | N |  |
|  | W | 3.021 | 2.237 | 2.485 | 2.355 | 2.619 | 3.536 | N |  |
| MSi2N2STe | Mo | 3.072 | 2.199 | 3.743 | 2.348 | 2.776 | 3.675 | Y |  |
|  | W | 3.075 | 2.218 | 3.735 | 2.372 | 2.768 | 3.697 | Y |  |
| MSi2N2SeTe | Mo | 3.098 | 2.387 | 3.619 | 2.490 | 2.719 | 3.780 | Y |  |
|  | W | 3.100 | 2.412 | 3.799 | 2.515 | 2.729 | 3.826 | Y |  |

For a mechanically stable material, the elastic constants should fulfill the Born-Huang stability criteria1: C11>C12, C11C22-C122>0, C66>0. Considering that Janus MoSi2N3P belongs to C3v point group, thus C11=C22 and C66=0.5(C11-C12), the criterion turns out to be only C11>C12. As shown in Table S3, the calculated C11 is larger than C12 suggesting that four MoSi2N3Y monolayers are mechanically stable. To evaluate the in-plane stiffness, we calculated Young’s modulus Y(θ) and Poisson’s ratio υ(θ) along the in-plane θ, which is given as follow:

Yθ=C11C22-C122C11 sin4θ+A sin2θ cos2θ+C22 cos4θ                               (1)

υθ=C12 sin4θ-B sin2θ cos2θ+C12 cos4θC11 sin4θ+A sin2θ cos2θ+C22 cos4θ                               (2)

where A=C11C22-C122C66-2C12 and B=C11+C22-C11C22-C122C66.

Table S2. The obtained in-plane elastic constants C11, C22, C12 and C66 of four monolayers.

| Monolayers | C11 (N/m) | C22 (N/m) | C12 (N/m) | C66 (N/m) |
| --- | --- | --- | --- | --- |
| MoSi2N3P | 331.0 | 331.0 | 77.6 | 126.7 |
| MoSi2N3As | 276.4 | 276.4 | 95.6 | 90.4 |
| WSi2N3P | 341.8 | 341.8 | 76.7 | 132.5 |
| WSi2N3As | 274.1 | 274.1 | 100.6 | 86.8 |

Table S3. The calculated band gap at HSE06 level (Eg), the potentials of photo-generated electrons/holes (Ue/Uh), dipole moments (μ) and electrostatic potential difference (ΔΦ) for four stable monolayers.

| Monolayers | Eg (eV) | Ue (eV) | Uh (eV) | μ (Debye) | ΔΦ (eV) |
| --- | --- | --- | --- | --- | --- |
| MoSi2N3P | 0.96 | 1.37 | 1.71 | 0.43 | 2.12 |
| MoSi2N3As | 0.46 | 1.36 | 1.65 | 0.53 | 2.55 |
| WSi2N3P | 0.79 | 1.37 | 1.42 | 0.40 | 2.00 |
| WSi2N3As | 0.45 | 1.37 | 1.54 | 0.48 | 2.46 |

The Gibbs free energy

The change of Gibbs free energy (∆G) in water splitting reaction is calculated using the method proposed by Nørskovet et al2. The formula can be expressed as:

∆G=∆E+∆EZPE-T∆S                                       (3)

where ∆E is the adsorption energy, ∆EZPE and ∆S are the differences in the zero-point energy and entropy difference between the adsorbed state and corresponding free-standing state, respectively.

EZPE could be derived after the frequency calculation by

EZPE=12hν                                                   (4)

where ν represents the vibrational frequency.

Meanwhile, TS is given by

TS=kbTKln11-e-hνkbT+KhνkbT1e-hνkbT-1+1            (5)

where e represents the electron charge, h represents Planck’s constant and kb is Boltzmann’s constant. Here, T is set to be 298.15K.

The effect of external potential and pH have been taken into account to evaluate the HER and OER activities. The ∆G for HER process include two steps, which was expressed as:

(1)  * + H++ e-→ H*                                                                                            (6)

∆G1=GH*-12GH2-G*+∆GU+∆GpH

=∆EH+∆EZPEH-T∆SH+∆GU+∆GpH

=∆GH                                                                                                                         (7)

(2) H*+ H++ e- → *+ H2g                                                                              (8)

∆G2=G*+12GH2-GH*+∆GU+∆GpH

=-(∆EH+∆EZPEH-T∆SH)+∆GU+∆GpH

=-∆GH+ 2∆GU+2∆GpH                                                                                        (9)

Meanwhile, the OER can be decomposed into four elementary steps. The ∆G for each step was calculated as follows:

(3) H2Ol+ * →OH*+ H++ e-                                                                           (10)

∆G3=GOH*+12GH2-G*-GH2O+∆GU-∆GpH

=∆EOH+∆EZPEOH-T∆SOH+∆GU-∆GpH

=∆GOH                                                                                                                       (11)

(4) OH* →O*+ H++ e-                                                                                         (12)

∆G4=GO*+12GH2-GOH*+∆GU-∆GpH

=(∆EO+∆EZPEO-T∆SO+2∆GU-2∆GpH)-(∆EOH+∆EZPEOH-T∆SOH+     ∆GU-∆GpH)

=∆GO-∆GOH                                                                                                            (13)

(5) H2Ol+ O*→OOH*+ H++ e-                                                                     (14)

∆G5=GOOH*+12GH2-GO*-GH2O+∆GU-∆GpH

=(∆EOOH+∆EZPEOOH-T∆SOOH+3∆GU-3∆GpH)-(∆EO+∆EZPEO-     T∆SO+2∆GU-2∆GpH)

=∆GOOH-∆GO                                                                                                         (15)

(6) OOH* →*+ O2g+ H++ e-                                                                          (16)

∆G6=G*+12GH2+GO2-GOOH*+∆GU-∆GpH

=(4.92+4∆GU-4∆GpH)-(∆EOOH+∆EZPEOOH-T∆SOOH+3∆GU-3∆GpH)

=(4.92+4∆GU-4∆GpH)-∆GOOH                                                                        (17)

where ∆GU (∆GU=-eU) denotes extra potential bias provided by an electron in the electrode, where U represents the potential difference from the standard hydrogen electrode potential. ∆GpH represents the effect of pH on ∆G, which is calculated by ∆GpH=kbT×ln10× pH.

Table S4. The adsorption energies ΔE (eV) of all adsorbed species on four structures.

| Species | MoSi2N3P | MoSi2N3As | WSi2N3P | WSi2N3As |
| --- | --- | --- | --- | --- |
| H* | -0.15 | -0.84 | -0.16 | -0.80 |
| OH* | 0.86 | 0.71 | 0.80 | 0.63 |
| O* | 3.40 | 3.17 | 3.30 | 2.75 |
| OOH* | 4.30 | 4.14 | 4.23 | 4.06 |

Table S5. The zero-point energy EZPE (eV) and entropy TS (eV) of molecules and adsorbates on four structures.

| Species | MoSi2N3P | MoSi2N3As | WSi2N3P | WSi2N3As |
| --- | --- | --- | --- | --- |
| H2O(l) | 0.56/0.67 | 0.56/0.67 | 0.56/0.67 | 0.56/0.67 |
| H2(g) | 0.27/0.41 | 0.27/0.41 | 0.27/0.41 | 0.27/0.41 |
| H* | 0.24/0.01 | 0.23/0.01 | 0.24/0.01 | 0.23/0.01 |
| OH* | 0.37/0.09 | 0.37/0.09 | 0.38/0.09 | 0.37/0.09 |
| O* | 0.07/0.06 | 0.07/0.06 | 0.07/0.06 | 0.08/0.06 |
| OOH* | 0.46/0.17 | 0.46/0.17 | 0.45/0.18 | 0.46/0.16 |

Solar-to-hydrogen (STH) efficiency

STH efficiency is estimated by the product of the efficiency of light absorption ηabs and carrier utilization ηcu using the following expression3:

ηSTH=ηabs×ηcu                                              (18)

The efficiency of light absorption is defined as:

ηabs=Eg∞Pℏωdℏω0∞Pℏωdℏω                                      (19)

where Eg is the band gap of photocatalyst and Pℏω is the AM1.5 solar energy flux at the photon energy ℏω.

The efficiency of carrier utilization (ηcu) is estimated by

ηcu=∆GH2OE∞PℏωℏωdℏωEg∞Pℏωdℏω                                      (20)

where ∆GH2O is the potential difference for water splitting (1.23 eV) and E is the energy of photons that can be used for water splitting, which can be defined as

E=Eg, (χ(H2)≥0.2, χ(O2)≥0.6)Eg+0.2-χ(H2), (χ(H2)<0.2, χ(O2)≥0.6)Eg+0.6-χ(O2), (χ(H2)≥0.2, χ(O2)<0.6)Eg+0.8-χ(H2)-χ(O2), (χ(H2)<0.2, χ(O2)<0.6)         (21)

where χ(H2) and χ(O2) are the over potentials for HER and OER, respectively. Considering the energy loss during carrier migration between different materials, the required over potentials for HER and OER are assumed to be 0.2 and 0.6 eV, respectively.

The intrinsic electric filed does positive work for the electron-hole separation during the process of photocatalytic water splitting. Therefore, this part of work should be added into the total energy, and then the corrected STH efficiency of photocatalytic water splitting for 2D material with vertical intrinsic EF is calculated as

η'STH=ηSTH×0∞Pℏωdℏω∆ΦEg∞Pℏωℏωdℏω+0∞Pℏωdℏω                  (22)

where ∆Φ is the vacuum level difference on the two respective surfaces.

Table S6. The calculated Over-Potential for HER χ(H2), Over-Potential for OER χ(O2), the photons energy (E), energy conversion efficiency of light absorption (ηabs), carrier utilization (ηcu), and corrected STH (η'STH) of four monolayers pH=7.

| Monolayers | χ(H2) (eV) | χ(O2) (eV) | E (eV) | ηabs (%) | ηcu (%) | η'STH (%) |
| --- | --- | --- | --- | --- | --- | --- |
| MoSi2N3P | 0.96 | 0.89 | 0.96 | 91.13 | 70.89 | 30.57 |
| MoSi2N3As | 0.95 | 0.82 | 0.46 | 99.82 | 78.41 | 29.84 |
| WSi2N3P | 0.96 | 0.60 | 0.79 | 95.52 | 74.20 | 32.93 |
| WSi2N3As | 0.97 | 0.72 | 0.45 | 99.82 | 78.41 | 30.51 |

References

1.	Andrew, R. C., Mapasha, R. E., Ukpong, A. M. & Chetty, N. Mechanical properties of graphene and boronitrene. Phys. Rev. B  85, 125428 (2012).

2.	Nørskov, J. K. et al. Origin of the Overpotential for Oxygen Reduction at a Fuel-Cell Cathode. J. Phys. Chem. B  108, 17886-17892 (2004).

3.	Fu, C. F. et al. Intrinsic Electric Fields in Two-dimensional Materials Boost the Solar-to-Hydrogen Efficiency for Photocatalytic Water Splitting. Nano Letters 18, 6312-6317 (2018).