Rheological and anti-microbial study of silica and silver nanoparticles-reinforced k-carrageenan/hydroxyethyl cellulose composites for food packaging applications

Balasubramanian Rukmanikrishnana, Srinivasan Ramalingamb, Sam Soo kim a* and Jaewoong Leea*

aDepartment of Fiber System Engineering, Yeungnam University.

bDepartment of food science and technology, Yeungnam University.

*Corresponding author

Email: jaewlee@yu.ac.kr

Address:  Jaewoong Lee. Department of Fiber System Engineering, Yeungnam University, 280 Daehak-Ro, Gyeongsan, Gyeongbuk 38541, South Korea. Tel: +82-53-810-2786; Fax: +82-53.810.4685; Email: jaewlee@yu.ac.kr.

Co-corresponding author: Prof. Sam Soo Kim, Department of Fiber System Engineering, Yeungnam University, 280 Daehak-Ro, Gyeongsan, Gyeongbuk 38541, South Korea. Email: sskim@yu.ac.kr,

Characterization methods

Fourier transform infrared (FT-IR) spectra of the prepared nanocomposites were obtained using a PerkinElmer (Spectrum 100, USA) spectrometer. X-ray diffraction patterns of the prepared nanocomposite films were obtained using an X-ray diffractometer (D/Max, Rigaku, Japan). XRD spectra were recorded using Cu Kα radiation as the incident X-ray source (40 kV, 200 mA) and a scanning speed of 2°/min from 2θ = 10 ° to 80° at room temperature. Differential scanning calorimetry (DSC) analysis of the prepared nanocomposite films was performed using a DSC instrument (TA Instruments, USA) at a heating rate of 10 °C/min (25–300 °C) under an N2 atmosphere. Thermogravimetric analysis (TGA) was carried out at 10 °C/min, up to 600 °C, under an N2 atmosphere, using an SDT Q600 (TA Instruments, USA). The optical properties of the prepared nanocomposite films were characterized using a Shimadzu spectrophotometer (UV-1601, Japan) at 200–800 nm. To measure the moisture contents of the GP and GPZ composite films, they were equilibrated at 25 °C and then dried at 100 °C. The weight difference was calculated as follows:

Moisture content (%) (W1–W2)/W1×100 		(1)

W1 and W2 are the initial and dried weights of the specimen, respectively. The contact angle (CA) of water on the film surfaces was analyzed using a CA analyzer (OCA 20, GmbH, Germany), on a movable sample stage. A ~10 μL drop of water was placed on the surface with a micro-syringe. The water vapor permeability (WVP) of the prepared films was determined using the ASTM E-96-95 standard method. The water vapor mass flux (WVTR) in g/m2·s was determined using the slope of the steady-state (linear) portion of the weight change versus time curve. The WVP (g·m/m2·s Pa) of the film was calculated as follows:

WVP = (WVTR×L/Δp)×100		(2)

L is the mean film thickness (m), and Δp is the partial water vapor pressure difference across the film. The morphology of the material, after being coated with platinum was observed using a scanning electron microscope (SEM, Hitachi S-4100), operated at an accelerating voltage of 15 kV. The rheological properties of the composites were evaluated using a rheometer (Physica MCR301; Anton Paar, Austria) with parallel-plate geometry (PP25, 1 mm gap) at 25 °C with a dynamic frequency sweep range of 0.1–100 1/s and a fixed strain amplitude (λ = 1.0%) within the linear viscoelastic region. The mechanical properties of the film were measured using a universal testing machine (Model 3345, Instron, USA) at a crosshead speed of 300 mm/min using strips. The gauge length was 200 mm. The film thickness of the prepared composite was determined using a digital micrometer (Mituto, Japan). All reported values are the averages of five different locations on each specimen. The antimicrobial activity of the prepared CH-SiO2-10 wt% /Ag nanocomposite films was tested against Staphylococcus aureus, Bacillus cereus, Listeria monocytogenes, Bacillus subtilis, Salmonella typhi, and Cronobacter sakazakii using an agar diffusion method. Wells that were 6 mm in diameter were punched and transformed with the respective polymer solution (100 and 500 µg per well). Ciproflaxacin (500 µg per well) served as the positive control for the bacteria assays, and sterile distilled water was used as the negative control. The plates were incubated for 24 h at 37 °C, and bacterial growth was monitored.