Supporting Information
Ultrafast rechargeable room-temperature solid-state sodium ion battery based on graphene-based liquid alloy
Qianqian Zhao, Haoqing Tian, Shan Liu*, Ling, Wang*, Lei Dai
School of Chemical Engineering, North China University of Science and Technology, Tangshan 063009, China.
*Corresponding authors: Email: sliu@ncst.edu.cn and tswling@126.com

[image: image14.png]



Supplementary Figure 1. Phase diagram of the Na-K alloy.
[image: image2.jpg]1150
=

L> Mo 2 4 - —
SRS ot e
g NEr





Supplementary Figure 2. Wettability test of Na-K alloy on different matrixs. a carbon felt, b nickel foam, c copper foil, d carbon paper.

[image: image3]
Supplementary Figure 3. The digital image of the surface of carbon paper after wetting.
[image: image4.jpg]Intensity (a.u.)

20

40 60
2 theta (degree)

80





Supplementary Figure 4. The X-ray diffraction patterns of Na3Hf2Si2PO12.
[image: image5.jpg]Hf

Si





Supplementary Figure 5. The crystal Structure of Na3Hf2Si2PO12.
[image: image6.jpg]log (sT (S cm'1K))

1.2
10_ Na3Hf28i2PO12

0.8
0.6
0.4]
0.2
0.0
0.2
0.4
16 1.8 20 22 24 26 2.8 3.0 32 3.4
1000 / T (K™)





Supplementary Figure 6. Arrhenius plot of Na3Hf2Si2PO12.
[image: image7.jpg]Surface tension / dny cm!

200 -

150 -

100 -

2

o

97.8°C

Na

Melting point
30°C
64 °C
K Na-K56%

Liquid metal




Supplementary Figure 7. The surface tension and melting point of the Na-K alloy.
[image: image8.jpg]e .




Supplementary Figure 8. Cross-section SEM images of Na/Na3Hf2Si2PO12 interface.
[image: image9.jpg]g -10 _
| Na-K/Na3Hf28|2PO12/Na-K
-84
£ -6
9 i
N
2]
o VY
20 25 30 35 40

Z" (Ohm)

b -60

.50
40-
_30;
204

-2’ (Ohm)

-104

10

1 Na/Na3Hf28i2PO12/Na

’.“

Z" (Ohm)

160 180 200 220 240 260 280





Supplementary Figure 9. Impedance of symmetric cells. a Na-K/Na3Hf2Si2PO12/Na-K, b Na/Na3Hf2Si2PO12/Na (tin oxide modified).
[image: image10.jpg]Voltage (v)

0-

"

)

3

- 0.1 mA cm™

5-U Na/NaszHf>SioPO4,/Na
0 2 3 4

Time (h)




Supplementary Figure 10. Galvanostatic cycling performance of the Na/Na3Hf2Si2PO12/Na symmetric cell under 0.1 mA cm-2.
[image: image11.jpg](,.wo yw) Aysusp juaun)d

(1) ebeyon




Supplementary Figure 11. Voltage-time profile of Na/Na3Hf2Si2PO12/Na symmetric cell (tin oxide modified) on galvanostatic cycling with stepped current density.
[image: image12.jpg](%) Aousiolyle o1qwoNoD

3 o o o o
T O © < N o
|w i 1 | s )
@)
5 L=
L)
. I
o o o o o o
i N o © ™
(.6 uyw) Ayoede oypads

40 60 80 100

20

Cycle number




Supplementary Figure 12. The cycling performance of the Na-K/Na3Hf2Si2PO12/Na3V2(PO4)3 full cells at a current rate of 5 C. 
[image: image13.jpg]Q

Voltage (v)

4.2 Na-K/NazHf,Si,PO12/NasVa(POs)s
3.9-

3.6- JJ
33

3.0-

57 20C10C5C
24. ——————— '

0 30 60 9 120

Specific capacity (mAh g”)

150

Voltage (v)

4.2 —Na/Na3Hf28i2PO12/Na3V2(PO4)3
3.9 1 —Na-K/NangZSi2P012/Na3V2(PO4)3
3.6 /J
3.3
3.04
271 10cC
2-4 T L T T T T
0 30 60 90 120

Specific capacity (mAh g”)

150




Supplementary Figure 13. Electrochemical performance of full cells. a Charge/discharge curves of the Na-K/Na3Hf2Si2PO12/Na3V2(PO4)3 full cell tested at different currents. b Charge/discharge curves comparison of the Na-K/Na3Hf2Si2PO12/Na3V2(PO4)3 and Na/Na3Hf2Si2PO12/Na3V2(PO4)3 full cells tested at 10 C.
Supplementary Table 1 Comparison wetting condition of Na-K alloy in various matrixs.
	Host
	Wetting condition

(temperature/time)
	Ref.

	carbon paper 
	RT/2.5 h 
	[1]

	carbon paper 
	420 oC
	[2]

	CFC 
	420 oC 
	[
 ADDIN EN.CITE 
3
]

	CC (carbon cloth)
	acid treatment and

heated (400 oC) 
	[4]

	rGO (layered graphene)
	RT/1 min
	This work


Supplementary Table 2 Comparison recent advances of NASICON-base solid state sodium ion batteries.
	cell type
	Critical current density(mA cm-2)
	Stability
(mA cm-2
/cycles)
	Test

temperature
	Ref.

	Na/TiO2@NASICON
	N 
	0.2/750 
	RT
	[5]

	Na/NASICON (surface heat treatment)
	N
	0.3/250
	RT
	[6]

	SiO2@Na/NASICON
	0.5 
	0.1-0.2/135 
	RT
	[7]

	Na/NASICON (Ca2+ doped) 
	N
	0.1-0.3/400 
	RT
	[8]

	Na/graphene-like 

@NASICON 
	N
	1/500 
	RT
	[9]

	Na/AlF3@NASICON
	1.2
	0.15-0.25/300 
	60 °C
	[10]

	Na/PVDF-HFP+ipn-PEA
@NASICON
	N
	0.2/200
	60 °C
	[11]

	molten Na 

/Sn@NASICON 
	50
	N
	110 °C
	[12]

	Na-K/NASICON
	65
	25/440 
40/60 
	RT
	This work


References

1.
Zhang, L. et al. Graphite intercalation compound associated with liquid Na-K towards ultra-stable and high-capacity alkali metal anodes. Energy Environ. Sci. 12, 1989-1998 (2019).

2.
Xue, L. et al. Liquid K-Na alloy anode enables dendrite-free potassium batteries. Adv. Mater. 28, 9608-9612 (2016).

3.
Zhang, L. et al. Exploring self-healing liquid Na-K alloy for dendrite-free electrochemical energy storage. Adv. Mater. 30, 1804011 (2018).

4.
Xie, Y., Hu, J. & Zhang, Z. A stable carbon host engineering surface defects for room-temperature liquid Na-K anode. J. Electroanalytical. Chem. 856, 113676 (2020).

5.
Yang, J. et al. Guided-formation of a favorable interface for stabilizing Na metal solid-state batteries. J. Mater. Chem. A. 8, 7828-7835 (2020).

6.
Gao, Z., Yang, J., Yuan, H., Fu, H. & Huang, Y. Stabilizing Na3Zr2Si2PO12/Na interfacial performance by introducing a clean and Na-deficient surface. Chem. Mater. 32, 3970-3979 (2020).
7.
Fu, H. et al. Reducing interfacial resistance by Na-SiO2 composite anode for NASICON-based solid-state sodium battery. ACS Materials. Lett. 2, 127-132 (2019).

8.
Lu, Y. et al. A high‐performance monolithic solid‐state sodium battery with Ca2+ doped Na3Zr2Si2PO12 electrolyte. Adv. Energy Mater. 9, 1901205 (2019).

9.
Matios, E. et al. Graphene regulated ceramic electrolyte for solid-state sodium metal battery with superior electrochemical stability. ACS Appl. Mater. Interfaces. 11, 5064-5072 (2019).

10.
Miao, X. et al. AlF3-modified anode-electrolyte interface for effective Na dendrites restriction in NASICON-based solid-state electrolyte. Energy Storage Mater. 30, 170-178 (2020).

11.
Ling, W. et al. A flexible solid electrolyte with multilayer structure for sodium metal batteries. Adv. Energy Mater. 10, 1903966 (2020).

12.
Gross, M. M. et al. Tin-based ionic chaperone phases to improve low temperature molten sodium-NaSICON interfaces. J. Mater. Chem. A. 8, 17012-17018 (2020).
[image: image1.jpg]Temperature / °C

100

80+
60
404 (Na)+L
20-
| 9°C
0_
(Na)+(NayK)
-80 (K)+(NayK)
0 20 40 60 80

w(K) / %



