Supporting Information

Synthesis of CaWO4 as a photocatalyst for degradation of methylene blue and carmine under ultraviolet light irradiation

Cunyang Yuan1,2, Fuwei Sun1,2, Haibo Liu1,2, Tianhu Chen1,2, Ziyang Chu1,2, Hanlin Wang1,2, Xuehua Zou1,2, Peixun Zhai1,2, Dong Chen1,2

1 Key Laboratory of Nano-Minerals and Pollution Control of Anhui Higher Education Institutes, Hefei University of Technology, Hefei 230009, China

2 Institute of Environmental Minerals and Materials, School of Resources and Environmental Engineering, Hefei University of Technology, Hefei 230009, China

Fig. S1 the temperature of the solution during the reaction process

| 元素 | 重量百分比 | 原子百分比 |
| --- | --- | --- |
| O | 21.94 | 65.37 |
| Ca | 15.48 | 18.41 |
| W | 62.58 | 16.22 |

Fig. S2 calculation of element proportion

Fig. S3a nitrogen adsorption-desorption isotherms of CaWO4

Fig. S3b pore size distribution of CaWO4

Fig. S4 photocatalytic degradation of MB by comparation experiments.

[CaWO4]=1.0 g/L; light intensity=80 W; [MB]=100 mg/L; pH=8.2

Fig. S5 TOC removal efficiency in photocatalytic degradation of MB

[CaWO4]=1.0 g/L; light intensity=80 W; [MB]=100 mg/L; pH=8.2

Fig. S6 UV–vis spectra in the course of photocatalytic degradation MB

[CaWO4]=1.0 g/L; light intensity=80 W; [MB]=100 mg/L; pH=8.2

Fig. S7 photocatalytic degradation of CR by comparation experiments.

[CaWO4]=1.0 g/L; light intensity=80 W; [CR]=100 mg/L; pH=6

Fig. S8 TOC removal efficiency in photocatalytic degradation of CR

[CaWO4]=1.0 g/L; light intensity=80 W; [CR]=100 mg/L; pH=6

Fig. S9 potential of CaWO4 solution at different pH values

Fig. S10 UV–vis spectra in the course of photocatalytic degradation CR

[CaWO4]=1.0 g/L; light intensity=80 W; [CR]=100 mg/L; pH=6

Corresponding author: Dong Chen, cdxman@hfut.edu.cn