Table S1. Compositions of working solutions used to construct different substrates.

| Samples | Component contents (g) in the exchange solutions of ddH2O (200 mL) |
| --- | --- |
|  | MgCl2·6H2O |
| AT | 0 |
| AT-Mg 1 | 0.008 |
| AT-Mg 2 | 0.080 |
| AT-Mg 3 | 0.800 |

Table S2 Compositions of modified SBF used to generate CaP coating.

| Samples | Component contents (mg) in the mixture solution of ddH2O (5000 mL) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | NaCl | NaHCO3 | Na2SO4 | Tris | CaCl2 | MgCl2·6H2O | KCl | K2HPO4·3H2O |
| AT-CaP | 40175 | 1675 | 360 | 30590 | 1752 | 1555 | 1125 | 1386 |
| AT-Mg1-CaP | 40175 | 1675 | 360 | 30590 | 1752 | 1555 | 1125 | 1386 |
| AT-Mg2-CaP | 40175 | 1675 | 360 | 30590 | 1752 | 1555 | 1125 | 1386 |
| AT-Mg3-CaP | 40175 | 1675 | 360 | 30590 | 1752 | 1555 | 1125 | 1386 |

Table S3 Primer sequences performed for quantitative real-time PCR analysis.

| Primer name | Primer sequence (5′to3′) |
| --- | --- |
| Runx2(F) | TCCTGTAGATCCGAGCACCA |
| Runx2 (R) | CTGCTGCTGTTGTTGCTGTT |
| ALP(F) | CCAGAAAGACACCTTGACTGTGG |
| ALP(R) | TCTTGTCCGTGTCGCTCACCAT |
| OPN(F) | GCTTGGCTTATGGACTGAGGTC |
| OPN(R) | CCTTAGACTCACCGCTCTTCATG |
| Col1(F) | GCTTGGTCCACTTGCTTGAAGA |
| Col1(R) | GAGCATTGCCTTTGA TTGCTG |
| DMP1(F) | AGTGAGGAGGACAGCCTGAA |
| DMP1(R) | TCCCTGTGGAGTTGCTCTCT |
| SOST(F) | CCACAGAGGTCATCCCA |
| SOST(R) | GACACATCTTTGGCGTCATAG |
| GAPDH(F) | GCACCGTCAAGGCTGAGAAC |
| GAPDH(R) | TGGTGAAGACGCCAGTGGA |

Fig. S1. SEM morphology of the AT-CaP and various AT-Mg(x)-CaP (x=1,2,3) coatings when generated without PAsp

Fig. S2. The EDS spectral line scanning images with Ti, P, and O elements of AT-Mg2-CaP before and after acid elution.

Fig. S3. The EDX mappings (Ti, Mg, Ca, P, O, V, Cl, and Al) images of AT-Mg2-CaP substrates after acid-elution.

Fig. S4. (A) The elemental composition of the AT-Mg2-CaP implant taken from rat femurs by EDS. (B-D) The EDX mappings (Merge, V, and C) images of AT-Mg2-CaP implant taken from rat femurs.