Electronic Supplementary Information

Highly Efficient Regulation Strategy of Fluorescence Emission Wavelength via Designing the Structure of Carbon Dots

Haiyan Baia,b, Xilang Jina,b,c ∗, Zhao Chengd, Hongwei Zhoua,b, Haozhe Wanga, Jiajia Yua, Jialing Zuoa, Weixing Chena,b ∗

CONTENTS

Fig S1 Effect of (a) reaction temperature; (b) reaction time on the fluorescence intensity of CDs; (c) pH stability (d) salt resistance (e) UV absorption of CDs

Fig S2 High-resolution XPS spectra of d-CDs: (a) N (b) O (c) S

Fig S3 High-resolution XPS spectra of e-CDs: (a) N (b) O (c) S

Fig S4 High-resolution XPS spectra of m-CDs: (a) N (b) O (c) S

Tab S1 The peaks of the four constituent elements of C1s, N1s, O1s and S2p

Fig S5 Raman spectrum of d-CDs and a-CDs

Materials and measurements

All reagents were obtained from commercial sources and used without further purification throughout the experiments.

Fluorescence spectra were performed on a Quanta Master 8000 spectrofluorometer with a slit width of 5 nm for both excitation and emission. UV-Vis spectra were measured on a Shimadzu UV-2550 spectrophotometer. FT-IR analyses were performed on a Bruker VERTEX 70 spectrometer. Raman spectrum was obtained using a Lab RAM HR Evolution. The X-ray photoelectron spectrum (XPS) was acquired on Thermo Scientific K-Alpha. The XRD spectrum was measured on a D2 PHASER Gen2 x-ray diffractometer. The TEM spectrum was measured on a JEM-2010 transmission electron microscope.

Fig S1 Effect of (a) reaction temperature; (b) reaction time on the fluorescence intensity of CDs; (c) pH stability (d) salt resistance (e) UV absorption of CDs

Fig S2 High-resolution XPS spectra of d-CDs: (a) N (b) O (c) S

Fig S3 High-resolution XPS spectra of e-CDs: (a) N (b) O (c) S

Fig S4 High-resolution XPS spectra of m-CDs: (a) N (b) O (c) S

Tab S1 High-resolution XPS spectra of CDs

|  | d-CDs |  | e-CDs |  | m-CDs |  |
| --- | --- | --- | --- | --- | --- | --- |
| Peak of C | 284eV | C=C/C-C | 283.7 eV | C=N | 283.7 eV | C=N |
|  | 284.4eV | C-O | 284.4eV | C-O | 284.4eV | C-O |
|  | 285.3eV | C-N | 285.3eV | C-N | 285.3eV | C-N |
|  | 287.4 eV | -CONH- |  |  |  |  |
| Peak of N | 397.5 Ev | Pyridine N | 397.5 Ev | Pyridine N | 397.5 Ev | Pyridine N |
|  | 398.8 eV | Graphitic N | 398.8 eV | Graphitic N | 398.8 eV | Graphitic N |
|  | 400 eV | Pyrrolic N | 400 eV | Pyrrolic N | 400 eV | Pyrrolic N |
| Peak of O | 531.4 eV | C-OH/C-O-C | 531.4 eV | C-OH/C-O-C | 531.4 eV | C-OH/C-O-C |
|  | 532 eV | C=O | 532 eV | C=O | 532 eV | C=O |
| Peak of S | 162.5 eV | C-S | 162.5 eV | C-S | 162.5 eV | C-S |
|  | 163.5 eV | C=S | 163.5 eV | C=S | 163.5 eV | C=S |
|  |  |  | 164.9 eV | S-N | 164.9 eV | S-N |

Fig S5 Raman spectrum of d-CDs and a-CDs