## Slide 1
RPR: rind penetrometer resistance; N, sample number; SCM, scatter correction methods; SD, standard deviation of reference value; RMSEC, root mean square error of calibration; R2, determination coeffcient of calibration; R2cv, determination coeffcient of cross-validation; RMSECV, root mean square error of cross-validation; RMSECV, root mean square error of cross-validation; RMSEP, root mean square error of external validation; R2ev, determination coeffcient of external validation; RPD, ratio of prediction to deviation; SNV, standard normal variate; FD+SNV, a combination of FD and SNV.
Table 2. Calibration and external validation statistics for RPR and breaking force in sugarcane stalks
 | Calibration |  |  |  |  |  |  |  |  |  | Cross-validation |  |  |  | External validation |  |  | 
 | Rank | N | SCM | Spectrum range | Mean | SD | RMSEC | R2 | RPD |  | RMSECV | R2cv | RPD |  | N | RMSEP | R2ev | RPD
RPR (N·mm-2) | 23 | 458 | SNV | 5669.7-9626.9, 10406-11200.6 | 42.0 | 7.62 | 0.40 | 1.00 | 19.60 |  | 0.74 | 0.99 | 10.30 |  | 68 | 0.76 | 0.99 | 10.20
Breaking force (N) | 12 | 350 | FD+SNV | 4882.9-6464.2, 8037.9-9626.9 | 20.3 | 6.08 | 2.15 | 0.88 | 2.88 |  | 2.51 | 0.83 | 2.42 |  | 90 | 2.08 | 0.85 | 2.58