Supporting information

Crosslinked Reprocessable Phosphor/Polyurethane Hybrid Networks with Thermal Induced Self-Healing Capacity and Ultraviolet Conducted Fluorescence Effect

Xiyang Zeng2#, Li Wang1#*, Xiaohu Chen2, Ting Zhang1, Tao Chen1, Junfeng Li2

1 School of Big Health and Intelligent Engineering, Chengdu Medical College, Chengdu 610500, P. R. China

2 College of Materials, Chemistry & Chemical Engineering, Chengdu University of Technology, Chengdu 610059, Sichuan, P. R. China

# Authors contributed equally

⁎Corresponding author: E-mail addresses: liwang@cmc.edu.cn (Li Wang)

Supplemental table: Table S1

Supplemental Figures: Fig. S1-Fig. S12

Fig. S1 Cooling curves for PTMGBP films.

Table S1. Enthalpies of PTMGBP films.

| Samples | Onset Temperature (°C) | Offset Temperature (°C) | Tc (°C) | ΔH (J·g−1)b | Onset Temperature (°C) | Offset Temperature (°C) | Tm (°C) | ΔH (J·g−1)b |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PTMGBP0 | -13.92 | 3.62 | -3.71 | 51.18 | 4.61 | 28.91 | 21.72 | -57.48 |
| PTMGBP1 | -16.62 | 3.20 | -4.59 | 63.05 | 3.47 | 29.15 | 21.93 | -56.28 |
| PTMGBP3 | -18.42 | 0.26 | -7.80 | 37.23 | 0.57 | 28.51 | 20.13 | -45.93 |
| PTMGBP5 | -14.31 | 5.21 | -3.61 | 59.27 | 3.26 | 29.10 | 21.61 | -59.25 |
| PTMGBP7 | -13.96 | 3.26 | -4.25 | 46.77 | 1.56 | 29.80 | 21.92 | -66.61 |

Fig. S2 DTG curves for PTMGBP films.

Fig. S3 Degree of swelling of PTMGBP films after 24 hours of immersion in ethyl acetate.

Fig. S4 Stress-strain curves for PTMGBP films.

Fig. S5 Stress-strain curves of PTMGBP3 films initially and after 1 hour of healing at 60 °C.

Fig. S6 Stress-strain curves of PTMGBP5 films initially and after 1 hour of healing at 60 °C.

Fig. S7 Stress-strain curves of PTMGBP7 films initially and after 1 hour of healing at 60 °C.

Fig. S8 Stress-strain curves of PTMGBP films after 1 hour of healing at different temperatures.

Fig. S9 Healing efficiency of PTMGBP films after 1 hour of healing at different temperatures

.

Fig. S10 Photograph of the colour change of strontium aluminate powder under a UV lamp.

Fig. S11 Excitation spectrum of strontium aluminate powder.

Fig. S12 Emission spectrum of strontium aluminate powder.