Supporting Information for

C3N Nanodots Impede Aβ Peptides Aggregation Pathogenic Path in Alzheimer's Disease

Xiuhua Yin1,2#, Hong Zhou1#, Mengling Zhang 2,5#, Juan Su3, Xiao Wang 2, Sijie Li3, Zaixing Yang1,3*, Zhenhui Kang2,5*, Ruhong Zhou1,4*

- Institute of Quantitative Biology, Shanghai Institute for Advanced Study, College of Life Sciences, Zhejiang University, Hangzhou 310027, China

- Jiangsu Key Laboratory for Carbon-based Functional Materials and Devices, Institute of Functional Nano and Soft Materials (FUNSOM), Soochow University, Suzhou 215123, China

- State Key Laboratory of Radiation Medicine and Protection, School for Radiological and Interdisciplinary Sciences (RAD-X), Soochow University, Suzhou 215123, China

- Department of Chemistry, Columbia University, New York, New York 10027, United States;

- Macao Institute of Materials Science and Engineering (MIMSE), MUST−SUDA Joint Research Center for Advanced Functional Materials, Macau University of Science and Technology, Taipa 999078, Macao, China.

#These authors contribute equally.

*Corresponding authors: rhzhou@zju.edu.cn (R. Zhou); zhkang@suda.edu.cn (Z. Kang); zxyang@suda.edu.cn (Z. Yang)

Figure S1. Characterization of C3N nanodots. (a) UV-vis spectrum, (b) Fourier transform infrared spectrum, and (c) X-ray photoelectron spectroscopy of C3N nanodots.

Figure S2. TEM images of Aβ42 peptides treated with/without C3N nanodots at different concentrations for 24 hours.

Figure S3. (a) C3N model and (b) the initial Aβ42 structure (PDB ID: 1Z0Q) used in the molecular dynamics simulations.

Figure S4. Time evolutions of the secondary structure of Aβ42 peptides (a) in the presence or (b) in the absence of C3N nanodots. Three panels from top to bottom in each figure represent three independent runs of each system. Here, the secondary structures of each residue were assigned according to the DSSP definition52.

Figure S5. Cytotoxicity of C3N nanodots on various cell lines for 24 hours by CCK-8 kit. n=5, data are shown as the mean ± SD.

Figure S6. Hemolysis activity of C3N nanodots. (a) The hemolysis activity of C3N nanodots via direct observation of color changes of the RBC centrifuge supernatant after incubation with C3N nanodots at different concentrations (50–500 µg/mL) under 37°C for 3 h. (+) and (−) symbols represented the positive and negative control, respectively. (b) Hemolysis ratio was calculated by spectrophotometric analysis of RBC centrifuge supernatant. Data are shown as the mean ± SD of three independent experiments.

Figure S7. Monitoring changes in body weight of mice in each group during the entire C3N nanodots administration period. Data are shown as the mean ± SD (n=6).

Figure S8. Histopathological (H&E) analyses of important organs of mice in each group.