Supporting Information

Synthesis of MoS2 with Tubular Hierarchical Structures.

MoS2 with tubular structures (MS-T) were synthesized by hydrothermal method with ammonium molybdate tetrahydrate ((NH4)6Mo7O24∙4H2O) and thioacetamide (TAA) as raw materials, and tetramethylammonium bromide (TMAB) as additive. In a typical synthesis, (NH4)6Mo7O24∙4H2O (0.024 mol/L), TAA (0.42 mol/L) and TMAB (0.42 mol/L) were dissolved in deionized water. After stirring for 30 min, the obtained suspension as hydrothermally treated in a 100 mL Teflon-lined autoclave at 200 °C for 6 h. The precipitate was filtered and dried at 50 °C for 12 h in a vacuum oven.

Theoretical Calculation

The densitiy functional theory (DFT) calculations were performed with CASTEP (J. Quantum Chem. 2000, 77, 895) using ultrasoft pseudopotential, plane-wave basis and periodic boundary conditions. The Perdew-Burke-Ernzerh generalized gradient approximation (GGA-PBE) (Phys. Rev. B, 1992, 45, 13244) function for the exchange-correlation term, and a 340 eV cut-off energy for the plane-wave basis set were used in all relaxation process. The self-consistent field (SCF) tolerance was 2.0  10-6 eV. The k-point was set to 331 for the Brillouin zone integration. MoS2 and MoP was modeled by a 22 supercell slab, which is periodic in the x and y direction, whereas separated by a 15 Å vacuum region in the z direction to avoid the interactions with the adjacent atomic slabs.

The adsorption free energies of H (ΔGH*) is usually considered as an effective descriptor for HER activity and a catalyst with ΔGH* = 0 can be an excellent candidate for HER. The Gibbs free-energy of H* (ΔGH*) was calculated by the equation ΔGH* = ΔEH* + 0.24 eV instead of ΔGH*= ΔEH* + ΔEZPE – TΔS.

Table S1 Relative molar percentage of measured elements evaluated with EDX elemental mapping

| Sample | relative molar percentage of measured elements (%) |  |  |
| --- | --- | --- | --- |
|  | Mo | S | P |
| MoP/MoS2-0 | 34.40 | 65.60 | \ |
| MoP/MoS2-1/3 | 34.47 | 62.11 | 3.42 |
| MoP/MoS2-1 | 35.03 | 59.88 | 5.09 |
| MoP/MoS2-5 | 35.63 | 57.47 | 6.90 |
| MoP/MoS2-40 | 50.91 | \ | 49.19 |

Fig. S1 SEM image (a) and elemental mapping images of Mo and S for MoS2

Fig. S2 SEM image (a) and elemental mapping images of Mo (b), S (c) and P (d) for MoP/MoS2-1/3

Fig. S3 SEM image (a) and elemental mapping images of Mo (b), S (c) and P (d) for MoP/MoS2-5

Fig. S4 SEM image (a) and elemental mapping images of Mo (b) and P (c) for MoP/MoS2-40

Fig. S5 Nitrogen sorption isotherms (a) and pore size distribution curves (b) of MoP/MoS2-0, MoP/MoS2-1/3, MoP/MoS2-1, MoP/MoS2-5 and MoP/MoS2-40

Fig. S6 CV of MoP/MoS2-0 (a), MoP/MoS2-1/3 (b), MoP/MoS2-5 (c) and MoP/MoS2-40 (d) with rates from 10 to 60 mV/s

Fig. S7 Polarization curves (a,c) and Tafel plots (b,d) for MoP/MoS2-1 in 1 M KOH (a,b) and 1 M PBS (c,d)