8. Extended Data

Extended Data Table 1. Collection of C1 reactions in the chemical network of dry reforming of methane

| Chemical equation | ΔHO at 298 K (kJ mol-1) | Name | Number |
| --- | --- | --- | --- |
| CO2 + CH4 2H2 + 2CO | 247 | Dry reforming | S1 |
| H2O + CH4 CO + 3H2 | 206 | Steam reforming | S2 |
| ½ O2 + CH4 CO + 2H2 | -44 | Partial oxidation | S3 |
| 2H2O + CH4 CO2 + 4H2 | 169 | Steam reforming | S4 |
| 2CO CO2 + C | -172 | Boudouard | S5 |
| CH4 C + 2H2 | 75 | Cracking | S6 |
| CO2 + H2 CO + H2O | 41 | RWGS | S7 |
| CO2 + 2H2 C + 2H2O | -90 | Water formation | S8 |
| CO + H2 C + H2O | -131 | Water formation | S9 |
| 2O2 + CH4 CO2 + 2H2O | -891 | Combustion | S10 |

Extended Data Figure 1. The catalyst state depends on the gas environment investigated. a, NAP-XP spectra of Ni 2p, O 1s, C 1s and Si 2p core levels at kinetic energies (KE) of 130 eV (surface-sensitive, 0.4 nm probing depth), 300 eV (sub-surface-sensitive, 0.8 nm probing depth) and 600 eV (sub-surface-sensitive, 1.1 nm probing depth) detection modes. surface-sensitive Conditions of acquisition: Gas mixture composed of 0.3 mlNmin-1 Ar, 0.6 mlNmin-1 H2. Reaction temperature: 810 °C. Reaction pressure: 16 Pa. b, NAP-XP spectra of Ni 2p, O 1s, C 1s at kinetic energies (KE) of 130 eV (surface-sensitive) after switching H2 with CO2 in the feed. Conditions of acquisition: Gas mixture initially composed of 0.3 mlNmin-1 Ar, 0.6 mlNmin-1 H2, then switched to 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2. Reaction temperature: 810 °C. Reaction pressure: 16 Pa. Spectra from bottom to top are equally separated by 60 minutes. c, NAP-XP spectra of Ni 2p, O 1s, C 1s at kinetic energies (KE) of 130 eV (surface-sensitive) after switching H2 with CH4 in the feed. Conditions of acquisition: Gas mixture initially composed of 0.3 mlNmin-1 Ar, 0.6 mlNmin-1 H2, then switched to 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2. Reaction temperature: 810 Celsius. Reaction pressure: 16 Pa. Spectra from bottom to top are equally separated by 60 minutes.

Extended Data Figure 2. Dominant oxygen species depend on gas feed and catalyst history. a, line deconvolution of XP spectra of O 1s core levels at kinetic energies of 130 eV  shows and ioncrease of NiO over time on stream. Conditions of acquisition: Gas mixture composed of 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2. Reaction temperature: 810 °C. Reaction pressure: 16 Pa. b, line deconvolution of O 1s core levels at kinetic energies of 130 eV show consumption of NiOx species. Conditions of acquisition: Gas mixture composed of 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2, 0.4 mlNmin-1 CH4. Reaction temperature: 810 Celsius. Reaction pressure: 16 Pa. Spectra from bottom to top are equally separated by 60 minutes. c, Parameters used for O 1s XPS fits in CasaXPS software package. Shirley + linear background were used as baselines.

Extended Data Figure 3. A correlative analysis between OSEM and NAP-XPS campaigns is possible thanks to their similar activity trends. Time series of catalytic activation during the reaction-induced phase transition determined in a, the OSEM and b, NAP XPS reactors. Note, OSEM and NAP-XPS campaigns gives similar activity trends. c, Line decomposition of the O 1s core level measured by NAP XPS, featuring the contributions of NiO, NiOd, SiO and SiOH. d, The time evolution of NiO and NiOd contributions reveals their differential reactivities during the phase transition. Note, NiOx signals were normalized  to SiOx as these species seem to be unchanged with the changing gaseous environments (Extended Data Figure 2). NiO (BE= 529.4 eV) depletes faster than NiOd (BE= 531.3 eV) during the DRM-induced phase transition, suggesting a higher durability of NiOd under reaction conditions due to its location in subsurface and bulk regions of the material. Conditions of acquisition: Gas mixture composed of 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2, 0.4 mlNmin-1 CH4. Reaction pressure: 16 Pa.

Extended Data Figure 4. OSEM close-up ROIs of catalyst surface during the oscillations. The metallic surface reconstructed before Instant 1. Instant 2 featured maximum oxides growth. Instant 3 closed the oscillation, with oxide shrinkage and surface smoothening. Scale bar= 2µm. Conditions of acquisition: Gas mixture composed of 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2, 0.4 mlNmin-1 CH4. Reaction temperature: 818-830 °C.

Extended Data Figure 5. Spatially-resolved investigation of the ongoing redox transition. a, an overview TEM image of the cross-section reveals the bulk character of the in situ formed oxide. b, c: the close-up image of the ongoing phase transition reveals the formation of a layered interphase between NiO and Ni. d, the HRTEM image of the cross section and Fast Fourier Transform images with pattern indexing for the highlighted ROIs reveal the coexistence of multiple phases and overlapping lattices at the interphase, and mechanical strain at the metallic substrate.

Extended Data Figure 6. A representation of the complex redox network of DRM governing catalytic selectivities over a 4-atom cluster of surface sites with varying oxidation state. Numbers represent the oxidation state of the cluster. a, Catalytic redox cycles representative of purely DRM selectivity. CO2 is initially activated on reduced sites (Eq. 1). Stepwise catalyst reduction of the type (+8  +6  +4  +2  0) by methane (Eq. 2). Combination of surface oxidation and stepwise reduction gives a product characteristic of DRM. b, a representation of the reaction path involving catalyst reductions of the type (+8  +4  0), ( +6  +2), leading to CO + H2 + H2O per reduction step (Eq. 3). c, a representation of the reaction path involving reductions of the type (+8  +2), ( +6  0), leading to CO + 2H2O per reduction step (Eq. 4). d, a representation of the reaction path involving transitions of the type (+8  0) leading to CO2 + 2H2O per reduction step (Eq. 5). Note, b-d lead to increasingly oxidized products compared to a.

Extended Data Video 1. Oscillations of the Ni catalyst during DRM as detected by OSEM. Conditions of acquisition: Gas mixture composed of 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2, 0.4 mlNmin-1 CH4. Reaction temperature: 817-832 °C.

Extended Data Video 2. Magnified ROIs of the oscillating catalyst surface. The video shows the out-of-phase cycles of surface roughening and smoothening during the oscillations. Scale bar= 2µm. Conditions of acquisition: Gas mixture composed of 0.3 mlNmin-1 Ar, 0.3 mlNmin-1 CO2, 0.4 mlNmin-1 CH4. Reaction temperature: 817-832 °C.

10. Supplementary Information

Numeric approach to the oscillations

We approximated the reaction-induced catalyst strain by the following expression:

Frestoring=-kHooke∆X =IΔXd2ΔXdt2		6

Frestoring is the restoring force exerted by the metallic substrate when the average size of NiO has increased and pushed the metallic sublayers by ΔX length units away from equilibrium position of the pristine lattice. The third part of Eq. 6 contains the motion conditions of Newton’s second law in which IX represents the inertia of NiO to grow or to recede. At some point of oxide accumulation, the generated restoring force becomes large enough to impede further growth into the bulk. Consequently, the rate of CO2 activation (Eq. 1) is diminished and the reaction deactivates (instant 1  instant 2, Figures 3h and 4b). In terms, the chemical potential of oxygen is too low as to enable oxygen diffusion into the strained Ni bulk, and oxide growth stops.

Due to the formation of discrete oxide islands during the oscillations, oxide contents and islands sizes represented by ΔX are directly correlated. The modulation in the rate of Eq. 1 can be represented as a decreasing function of oxide content:1

r1=k1inte(-kf1*ΘNiO)ΘNin[CO2]			7

In which r1 is the rate of Eq. 1, k1int is its rate constant without mechanical modulation, and kf1 is a parametric feedback constant combining intrinsic kHooke, IX, and the geometric dimensions of the volume occupied by NiO. Eq. 7 denotes a decrease in the magnitude of CO2 activation as the oxide contents ΘNiO increase.

The rate of Eq. 1 continues to decrease until CH4 activation (Eq. 2-5) becomes comparably faster. At this point, the mechanical strain accumulated around the NiO pushes the phase outwards, which favors rapid depletion of oxides by dominant Eq. 2-5, leading to H2 and H2O production enhancements and increasing H2/CO ratios. The accelerated transit (instant 2  instant 3, Figures 3h and 4b) is thus caused by the strain-generated restoring mechanical force. This influence is mathematically represented by Eq. 8, in analogy to Eq. 7:

r2-5=k2-5inte(+kf2*ΘNiO)ΘNiOm[CH4]			Eq. 8

It follows that one of the reaction cycles (for n =1) can be represented by:

CO2 + Ni  k1k-1  CO + NiO			Dissociative adsorption of CO2

CH4 + NiO k2k-2  CO + 2H2 + Ni		Partial oxidation of CH4 1

CH4 + 2NiO k3k-3 CO + H2 + H2O + 2Ni	Partial oxidation of CH4 2

CH4 + 3NiO k4k-4 CO + 2H2O + 3Ni		Partial oxidation of CH4 3

CH4 + 4NiO k5k-5 CO2 + 2H2O + 4Ni	Total oxidation of CH4

In addition, two types of NiOx species were produced, which we assume that reached an equilibrated state during the oscillations according to the following reaction:

Nirelaxed + NiO k6k-6  NiOd + Nistrained

Here, slowly reacting subsurface NiOd accounts for long term accumulation of mechanical strain. We calculated the numerical solutions of the evolving dynamics using the kinetic constants compiled in Table S1.

Table S1. A compilation of kinetic parameters leading to oscillations according to the assumptions of the model

| kiint | Absolute value (abundancep * simulation time-1) | Reaction step |
| --- | --- | --- |
| k1 | 1.1 * 10+1 | CO2 + Ni k1k-1 CO + NiO |
| k-1 | 8.0 * 10-3 |  |
| k2 | 4.6 * 10-2 | CH4 + NiO k2k-2 CO + 2H2 + Ni |
| k-2 | 2.1 * 10-4 |  |
| k3 | 1.0 * 10-3 | CH4 + 2NiO k3k-3 CO + H2 + H2O + 2Ni |
| k-3 | 7.2 * 10-7 |  |
| k4 | 1.5 * 10-4 | CH4 + 3NiO k4k-4 CO + 2H2O + 3Ni |
| k-4 | 1.7 * 10-8 |  |
| k5 | 1.7 * 10-5 | CH4 + 4NiO k5k-5 CO2 + 2H2O + 4Ni |
| k-5 | 9.6 * 10-9 |  |
| k6 | 7.5 * 10-5 | Nirelaxed + NiO k6k-6 NiOd + Nistrained |
| k-6 | 1.1 * 10-4 |  |
| kf1 | 4.5 * 101 | Modulation |
| kf2 | 2.1 * 100 |  |

p: molecularity of the step

References to Supplementary Information

1.	Bassett, M. R. & Imbihl, R. Mathematical modeling of kinetic oscillations in the catalytic CO oxidation on Pd(110): The subsurface oxygen model. The Journal of Chemical Physics 93, 811-821, doi:10.1063/1.459451 (1990).