Novel nanocellulose - microcrystalline cellulose complex with hierarchical structure reinforcing polylactic acid as 3D printing materials

Haibo Long a, Jianbin Mo a, Feiwen Yang a, Jialin Xiao a, Shuting Zhang a, Dingshu Xao b, Litao Guan a,*, Wenxu Zheng a, Jin Gu a, Wuyi Zhou a,*, Yen Wei c, Xianming Dong a,b,*

a Key Laboratory for Biobased Materials and Energy of Ministry of Education, College of Materials and Energy, Research Center of Biomass 3D Printing Materials, South China Agricultural University, Guangzhou 510642, P. R. China

b Daya Bay Chemical Engineering Research Institute of Huizhou University，Huizhou University，516200, Huizhou, P. R. China

c Department of Chemistry and the Tsinghua Center for Frotier Polymer Research , Tsinghua University, Beijing, 10084, P.R. China

Table S1. The printing parameters of the specimens were printed by FDM printer.

| Parameter | Value |
| --- | --- |
| Nozzle diameter | 0.4 mm |
| Layer height | 0.2 mm |
| Layer width | 0.4 mm |
| Top/Bottom thickness | 0.8 mm |
| Top/Bottom pattern | Lines |
| Infill density | 100% |
| Infill pattern | Grid |
| Extruder temperature | 200 C |
| Standby temperature | 185 C |
| Bed temperature | 45 C |
| Retraction distance | 3.0 mm |
| Retraction speed | 70 mm/s |
| Printing speed | 55 mm/s |
| Travel speed | 60 mm/s |
| Initial Layer speed | 30 mm/s |
| Fan speed | 100% |
| Generate support | None |
| Build Plate adhesion | Brim |

* Corresponding author.  E-mail address: dongxming@263.net (X. Dong), ltguan@scau.edu.cn (L. Guan), zhouwuyi@scau.edu.cn (W. Zhou) ,  .