Supporting Information

Fe-N/C nanozyme with specifically boosted peroxidase-like activity for ultrasensitive colorimetric bioanalysis

Shumin Xia, Mengrui Caoa, Ding Wangb, Renyong zhaoa

aProv Key Lab Cereal Resource Transformat & Utilize, Henan University of Technology, Zhengzhou 450001, China.

bNational Engineering Research Center for WheatCorn Further Processing, Henan University of Technology, Zhengzhou 450001, China

Contents

Fig. S1 Long-term durability of Fe-N/C nanozyme stored at 4 °C.	2

Table S1 Analyzing the kinetic parameters	3

Table S2 Performance compared with other reported AA investigative techniques	4

Fig. S2 Fe-N/C system's capability to recognize AA.	5

Fig. S3 The consistency of real samples after seven days of storage.	6

References	7

# Fig. S1 Long-term durability of Fe-N/C nanozyme stored at 4 °C.

# Table S1 Analyzing the kinetic parameters

| nanozyme | Km(mM) |  | Vmax (10-7 M·s-1) |  | Ref |
| --- | --- | --- | --- | --- | --- |
|  | TMB | H2O2 | TMB | H2O2 |  |
| HRP | 0.434 | 3.7 | 1 | 0.871 | (Gao, et al. 2007) |
| Co3O4/CeO2 | 0.36 | 132.21 | 1.666 | 0.434 | (Alizadeh, et al. 2019) |
| FeNi MOF | 1.97 | 0.01 | 0.131 | 0.529 | (Wang, et al. 2020) |
| Fe3O4@Apt | 0.088 | 30.24 | 0.0406 | 0.0342 | (Li, et al. 2019) |
| Fe3O4 | 0.485 | 1175.3 | 0.563 | 0.24 | (Ma, et al. 2013) |
| NiONPs | 0.0067 | 208 | 0.0267 | 0.132 | ( Liu, et al. 2015) |
| Hemin@MOF | 0.068 | 10.9 | 0.898 | 0.607 | (Qin, et al. 2013) |
| 2D Ni/Fe MOF | 0.411 | 0.037 | 1.25 | 0.33 | ( Li, et al. 2021) |
| Fe-N/C | 0.2580 | 1.9164 | 0.4586 | 0.3373 | This work |

# Table S2 Performance compared with other reported AA investigative techniques

| Biosensing materials | Analytical method | Limit of detection (µM) | Linear range (µM) | Ref |
| --- | --- | --- | --- | --- |
| CODs | Fluorescence | 0.32 | 1.11-300 | ( Liu, et al. 2017) |
| CQDs-MnO2 | Fluorescence | 0.042 | 0.18-90 | ( Liu, et al. 2016) |
| CuNPs@C | Colorimetric | 1.41 | 10-100 | (Tan, et al. 2014) |
| CeO2/rGO | Colorimetric | 0.15 | 0.5-40 | (Wang, et al. 2017) |
| Fe3O4/CoFe-LDH | Colorimetric | 0.2 | 0.5-10 | (Yang, et al. 2020) |
| Cu-BDC-NH2 NPs | Colorimetric | 0.15 | 0.5-60 | (Yao, et al. 2019) |
| CDs/Fe3O4 | Colorimetric | 0.285 | 0-50 | (Chen, et al. 2017) |
| Co3O4@β-CD NPs | Colorimetric | 1.09 | 10-60 | (Lu, et al. 2020) |
| IrO2/GO | Colorimetric | 0.324 | 5-70 | (Sun, et al. 2020) |
| CoOOH-ABTS | Colorimetric | 0.16 | 0.5-15 | (Fang, et al. 2019) |
| Fe3O4/N–C | Colorimetric | 0.04 | 0-50 | (Jiang, et al. 2017) |
| CNFs/MnCo2O4.5 | Colorimetric | 0.05 | 0-40 | (Gao, et al. 2017) |
| Fe-N/C | Colorimetric | 0.03 | 0.1-160 | This work |

# Fig. S2 Fe-N/C system's capability to recognize AA.

# Fig. S3 The consistency of real samples after seven days of storage.

# References

Gao L, Zhuang J, Nie L, Zhang J, Zhang Y, Gu N, Wang T, Feng J, Yang D, Perrett S, Yan X (2007) Intrinsic peroxidase-like activity of ferromagnetic nanoparticles. Nat Nanotechnol 2(9):577-583

Alizadeh N, Salimi A, Hallaj R (2019) Mimicking peroxidase-like activity of Co3O4-CeO2 nanosheets integrated paper-based analytical devices for detection of glucose with smartphone. Sens Actuators B 288:44-52

Wang J, Bao M, Wei T, Wang Z, Dai Z (2020) Bimetallic metal-organic framework for enzyme immobilization by biomimetic mineralization: Constructing a mimic enzyme and simultaneously immobilizing natural enzymes. Anal chim acta 1098:148-154

Li S, Zhao X, Yu X, Wan Y, Yin M, Zhang W, Cao B, Wang H (2019) Fe3O4 Nanozymes with Aptamer-Tuned Catalysis for Selective Colorimetric Analysis of ATP in Blood. Anal chem 91(22):14737-14742

Ma M, Xie J, Zhang Y, Chen Z, Gu N (2013) Fe3O4@Pt nanoparticles with enhanced peroxidase-like catalytic activity. Mater Lett 105:36-39

Liu Q, Yang Y, Li H, Zhu R, Shao Q, Yang S, Xu J (2015) NiO nanoparticles modified with 5,10,15,20-tetrakis(4-carboxyl pheyl)-porphyrin: Promising peroxidase mimetics for H2O2 and glucose detection. Biosens Bioelectron 64:147-153

Qin F-X, Jia S-Y, Wang F-F, Wu S-H, Song J, Liu Y (2013) Hemin@metal-organic framework with peroxidase-like activity and its application to glucose detection. Catal Sci Technol 3(10):2761-2768

Li Q, Wang Q, Li Y, Zhang X, Huang Y (2021) 2D bimetallic Ni/Fe MOF nanosheet composites as a peroxidase-like nanozyme for colorimetric assay of multiple targets. Anal Methods 13(17):2066-2074

Liu H, Na W, Liu Z, Chen X, Su X (2017) A novel turn-on fluorescent strategy for sensing ascorbic acid using graphene quantum dots as fluorescent probe. Biosens Bioelectron 92:229-233

Liu J, Chen Y, Wang W, Feng J, Liang M, Ma S, Chen X (2016) "Switch-On" Fluorescent Sensing of Ascorbic Acid in Food Samples Based on Carbon Quantum Dots-MnO2 Probe. J Agric Food Chem 64(1):371-380

Tan H, Ma C, Gao L, Li Q, Song Y, Xu F, Wang T, Wang L (2014) Metal-Organic Framework-Derived Copper Nanoparticle@Carbon Nanocomposites as Peroxidase Mimics for Colorimetric Sensing of Ascorbic Acid. Chem Eur J 20(49):16377-16383

Wang J, Su P, Li D, Wang T, Yang Y (2017) Fabrication of CeO2/rGO Nanocomposites with Oxidase-like Activity and Their Application in Colorimetric Sensing of Ascorbic Acid. Chem Res Chin Univ 33(4):540-545

Yang W, Li J, Wang M, Sun X, Liu Y, Yang J, Ng DHL (2020) A colorimetric strategy for ascorbic acid sensing based on the peroxidase-like activity of core-shell Fe3O4/CoFe-LDH hybrid. Colloids Surf B 188:110742

Yao Z, Li Z, Liu H, Liu Y, Sun Y, Li Z (2019) A novel colorimetric assay based on the peroxidase-like properties of amino functionalized copper metal-organic framework nanoparticles for ascorbic acid sensing. Anal Methods 11(12):1697-1706

Chen S, Chi M, Yang Z, Gao M, Wang C, Lu X (2017) Carbon dots/Fe3O4 hybrid nanofibers as efficient peroxidase mimics for sensitive detection of H2O2 and ascorbic acid. Inorg Chem Front 4(10):1621-1627

Lu W, Zhang J, Li N, You Z, Feng Z, Natarajan V, Chen J, Zhan J (2020) Co3O4@beta-cyclodextrin with synergistic peroxidase-mimicking performance as a signal magnification approach for colorimetric determination of ascorbic acid. Sens Actuators B 303:127106

Sun H, Liu X, Wang X, Han Q, Qi C, Li Y, Wang C, Chen Y, Yang R (2020) Colorimetric determination of ascorbic acid using a polyallylamine-stabilized IrO2/graphene oxide nanozyme as a peroxidase mimic. Microchim Acta 187(2)

Fang X, Wang J, Cui X, Zhang Y, Zhu R, Zhao H, Li Z (2019) Sensitive and facile colorimetric sensing strategy for ascorbic acid determination based on CoOOH nanoflakes-ABTs oxidative system. Colloids Surf A 575:66-74

Jiang Y, Song N, Wang C, Pinna N, Lu X (2017) A facile synthesis of Fe3O4/nitrogen-doped carbon hybrid nanofibers as a robust peroxidase-like catalyst for the sensitive colorimetric detection of ascorbic acid. J Mater Chem B 5(27):5499-5505

Gao M, Lu X, Nie G, Chi M, Wang C (2017) Hierarchical CNFs/MnCo2O4.5 nanofibers as a highly active oxidase mimetic and its application in biosensing. Nanotechnology 28(48):485708

Corresponding authors at: College of Food Science and Engineering, Henan University of Technology, Zhengzhou 450001, China.

E-mail addresses: dingwang0816@163.com, (D. Wang), zry8600@haut.edu.cn (R.Y. Zhao)