Coping with abrasion and structural failure – diverging inorganic coatings of radular teeth in two Porifera-consuming nudibranch species (Mollusca, Gastropoda) and their mechanical properties

Wencke Krings1,2,3*, Heike Wägele4, Charlotte Neumann1,2, Stanislav N. Gorb3

1 Department of Behavioral Biology, Institute of Cell and Systems Biology of Animals, Universität Hamburg, Martin-Luther-King-Platz 3, 20146 Hamburg, Germany

2 Department of Mammalogy and Palaeoanthropology, Leibniz Institute for the Analysis of Biodiversity Change, Hamburg, Germany

3 Department of Functional Morphology and Biomechanics, Zoological Institute, Christian-Albrechts-Universität zu Kiel, Kiel, Germany

4 Department of Phylogenetics and Evolutionary Biology, Leibniz Institute for the Analysis of Biodiversity Change, Bonn, Germany

*corresponding author: wencke.krings@uni-hamburg.de

Supplementary materials

Supplementary Table 1. Results from the EDX analysis and nanoindentation (mean and standard deviation). For each species, atomic % of analyzed elements, hardness, and Young’s modulus from all teeth and tooth layers pooled together are given. E, Young’s modulus (GPa); h, hardness (GPa).

| Species | Element | Quantity of measurements | Mean | Standard deviation |
| --- | --- | --- | --- | --- |
| Doris pseudoargus | Ae | 545 | 5.51 | 5.56 |
| Felimare picta | Ae | 410 | 6.11 | 8.13 |
| Doris pseudoargus | Ca | 545 | 2.48 | 3.99 |
| Felimare picta | Ca | 410 | 0.93 | 1.92 |
| Doris pseudoargus | Cl | 545 | 0.25 | 0.67 |
| Felimare picta | Cl | 410 | 0.64 | 0.66 |
| Doris pseudoargus | Cu | 545 | 0.00 | 0.00 |
| Felimare picta | Cu | 410 | 0.06 | 0.11 |
| Doris pseudoargus | F | 545 | 0.44 | 1.14 |
| Felimare picta | F | 410 | 0.00 | 0.00 |
| Doris pseudoargus | Fe | 545 | 0.08 | 0.74 |
| Felimare picta | Fe | 410 | 0.04 | 0.05 |
| Doris pseudoargus | K | 545 | 0.24 | 0.56 |
| Felimare picta | K | 410 | 0.16 | 0.27 |
| Doris pseudoargus | Mg | 545 | 0.59 | 0.50 |
| Felimare picta | Mg | 410 | 0.20 | 0.66 |
| Doris pseudoargus | Na | 545 | 0.62 | 0.67 |
| Felimare picta | Na | 410 | 0.66 | 0.43 |
| Doris pseudoargus | P | 545 | 0.32 | 0.64 |
| Felimare picta | P | 410 | 0.16 | 0.38 |
| Doris pseudoargus | S | 545 | 0.27 | 0.46 |
| Felimare picta | S | 410 | 0.41 | 0.45 |
| Doris pseudoargus | Si | 545 | 0.14 | 0.50 |
| Felimare picta | Si | 410 | 2.81 | 5.35 |
| Doris pseudoargus | Zn | 545 | 0.10 | 0.26 |
| Felimare picta | Zn | 410 | 0.03 | 0.11 |
| Species | Mechanical property | Quantity of measurements | Mean | Standard deviation |
| Doris pseudoargus | H | 1197 | 0.35 | 0.08 |
| Felimare picta | H | 810 | 0.35 | 0.19 |
| Doris pseudoargus | E | 1197 | 8.11 | 2.73 |
| Felimare picta | E | 810 | 7.39 | 2.89 |

Supplementary Table 2. Results from Kruskal-Wallis test and pairwise comparison by Wilcoxon method between the species for the atomic % and mechanical properties. Orange p-values = highly significant differences, red p-values = significant differences, black = no significant differences. E, Young’s modulus; h, hardness.

| Element | Species 1 | Species 2 | Wilcoxon method, p-value |
| --- | --- | --- | --- |
| Ae | Felimare picta | Doris pseudoargus | <.0001* |
| Ca | Felimare picta | Doris pseudoargus | <.0001* |
| Cl | Felimare picta | Doris pseudoargus | <.0001* |
| Cu | Felimare picta | Doris pseudoargus | <.0001* |
| F | Felimare picta | Doris pseudoargus | <.0001* |
| Fe | Felimare picta | Doris pseudoargus | <.0001* |
| K | Felimare picta | Doris pseudoargus | 0.0913 |
| Mg | Felimare picta | Doris pseudoargus | <.0001* |
| Na | Felimare picta | Doris pseudoargus | <.0001* |
| P | Felimare picta | Doris pseudoargus | <.0001* |
| S | Felimare picta | Doris pseudoargus | <.0001* |
| Si | Felimare picta | Doris pseudoargus | <.0001* |
| Zn | Felimare picta | Doris pseudoargus | 0.0373* |
| Mechanical property | Species 1 | Species 2 | Wilcoxon method, p-value |
| H | Felimare picta | Doris pseudoargus | <.0001* |
| E | Felimare picta | Doris pseudoargus | <.0001* |

Supplementary Table 3. Results from the EDX analysis and nanoindentation (mean and standard deviation). For each species, atomic % of analyzed elements from each tooth type (data on single layers are pooled together) as well as elasticity modulus (GPa) and hardness (GPa) are given.

| Species | Tooth types | Element | Quantity of measurements | Mean | Standard deviation |
| --- | --- | --- | --- | --- | --- |
| Doris pseudoargus | Central | Ae | 128 | 7.92 | 5.34 |
| Doris pseudoargus | Lateral | Ae | 196 | 4.66 | 4.57 |
| Doris pseudoargus | Marginal | Ae | 221 | 4.86 | 6.09 |
| Felimare picta | Central | Ae | 144 | 6.09 | 8.08 |
| Felimare picta | Lateral | Ae | 144 | 5.83 | 7.46 |
| Felimare picta | Marginal | Ae | 122 | 6.45 | 8.96 |
| Doris pseudoargus | Central | Ca | 128 | 3.09 | 4.79 |
| Doris pseudoargus | Lateral | Ca | 196 | 2.33 | 3.32 |
| Doris pseudoargus | Marginal | Ca | 221 | 2.26 | 4.01 |
| Felimare picta | Central | Ca | 144 | 0.86 | 1.84 |
| Felimare picta | Lateral | Ca | 144 | 0.90 | 1.91 |
| Felimare picta | Marginal | Ca | 122 | 1.06 | 2.04 |
| Doris pseudoargus | Central | Cl | 128 | 0.29 | 0.59 |
| Doris pseudoargus | Lateral | Cl | 196 | 0.23 | 0.54 |
| Doris pseudoargus | Marginal | Cl | 221 | 0.24 | 0.82 |
| Felimare picta | Central | Cl | 144 | 0.68 | 0.67 |
| Felimare picta | Lateral | Cl | 144 | 0.70 | 0.67 |
| Felimare picta | Marginal | Cl | 122 | 0.53 | 0.63 |
| Doris pseudoargus | Central | Cu | 128 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Cu | 196 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Cu | 221 | 0.00 | 0.00 |
| Felimare picta | Central | Cu | 144 | 0.04 | 0.09 |
| Felimare picta | Lateral | Cu | 144 | 0.04 | 0.09 |
| Felimare picta | Marginal | Cu | 122 | 0.10 | 0.14 |
| Doris pseudoargus | Central | F | 128 | 1.75 | 1.79 |
| Doris pseudoargus | Lateral | F | 196 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | F | 221 | 0.06 | 0.20 |
| Felimare picta | Central | F | 144 | 0.00 | 0.00 |
| Felimare picta | Lateral | F | 144 | 0.00 | 0.00 |
| Felimare picta | Marginal | F | 122 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Fe | 128 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Fe | 196 | 0.04 | 0.02 |
| Doris pseudoargus | Marginal | Fe | 221 | 0.16 | 1.16 |
| Felimare picta | Central | Fe | 144 | 0.04 | 0.05 |
| Felimare picta | Lateral | Fe | 144 | 0.04 | 0.05 |
| Felimare picta | Marginal | Fe | 122 | 0.04 | 0.05 |
| Doris pseudoargus | Central | K | 128 | 0.71 | 0.96 |
| Doris pseudoargus | Lateral | K | 196 | 0.09 | 0.18 |
| Doris pseudoargus | Marginal | K | 221 | 0.10 | 0.25 |
| Felimare picta | Central | K | 144 | 0.17 | 0.28 |
| Felimare picta | Lateral | K | 144 | 0.15 | 0.25 |
| Felimare picta | Marginal | K | 122 | 0.15 | 0.28 |
| Doris pseudoargus | Central | Mg | 128 | 0.24 | 0.38 |
| Doris pseudoargus | Lateral | Mg | 196 | 0.90 | 0.46 |
| Doris pseudoargus | Marginal | Mg | 221 | 0.51 | 0.44 |
| Felimare picta | Central | Mg | 144 | 0.21 | 0.82 |
| Felimare picta | Lateral | Mg | 144 | 0.22 | 0.75 |
| Felimare picta | Marginal | Mg | 122 | 0.17 | 0.11 |
| Doris pseudoargus | Central | Na | 128 | 0.81 | 0.51 |
| Doris pseudoargus | Lateral | Na | 196 | 0.51 | 0.27 |
| Doris pseudoargus | Marginal | Na | 221 | 0.59 | 0.94 |
| Felimare picta | Central | Na | 144 | 0.72 | 0.40 |
| Felimare picta | Lateral | Na | 144 | 0.72 | 0.38 |
| Felimare picta | Marginal | Na | 122 | 0.53 | 0.50 |
| Doris pseudoargus | Central | P | 128 | 0.65 | 0.81 |
| Doris pseudoargus | Lateral | P | 196 | 0.13 | 0.35 |
| Doris pseudoargus | Marginal | P | 221 | 0.29 | 0.65 |
| Felimare picta | Central | P | 144 | 0.15 | 0.35 |
| Felimare picta | Lateral | P | 144 | 0.14 | 0.36 |
| Felimare picta | Marginal | P | 122 | 0.18 | 0.43 |
| Doris pseudoargus | Central | S | 128 | 0.24 | 0.50 |
| Doris pseudoargus | Lateral | S | 196 | 0.31 | 0.42 |
| Doris pseudoargus | Marginal | S | 221 | 0.24 | 0.48 |
| Felimare picta | Central | S | 144 | 0.44 | 0.49 |
| Felimare picta | Lateral | S | 144 | 0.45 | 0.50 |
| Felimare picta | Marginal | S | 122 | 0.34 | 0.34 |
| Doris pseudoargus | Central | Si | 128 | 0.13 | 0.29 |
| Doris pseudoargus | Lateral | Si | 196 | 0.13 | 0.61 |
| Doris pseudoargus | Marginal | Si | 221 | 0.16 | 0.49 |
| Felimare picta | Central | Si | 144 | 2.75 | 5.47 |
| Felimare picta | Lateral | Si | 144 | 2.46 | 4.69 |
| Felimare picta | Marginal | Si | 122 | 3.30 | 5.90 |
| Doris pseudoargus | Central | Zn | 128 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Zn | 196 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Zn | 221 | 0.24 | 0.36 |
| Felimare picta | Central | Zn | 144 | 0.02 | 0.12 |
| Felimare picta | Lateral | Zn | 144 | 0.01 | 0.06 |
| Felimare picta | Marginal | Zn | 122 | 0.07 | 0.12 |
| Doris pseudoargus | Central | H | 312 | 0.40 | 0.17 |
| Doris pseudoargus | Lateral | H | 313 | 0.37 | 0.19 |
| Doris pseudoargus | Marginal | H | 610 | 0.36 | 0.16 |
| Felimare picta | Central | H | 280 | 0.39 | 0.29 |
| Felimare picta | Lateral | H | 281 | 0.39 | 0.31 |
| Felimare picta | Marginal | H | 281 | 0.38 | 0.32 |
| Doris pseudoargus | Central | E | 312 | 8.94 | 4.44 |
| Doris pseudoargus | Lateral | E | 313 | 8.48 | 5.12 |
| Doris pseudoargus | Marginal | E | 610 | 8.66 | 3.91 |
| Felimare picta | Central | E | 280 | 8.45 | 5.36 |
| Felimare picta | Lateral | E | 281 | 8.28 | 5.58 |
| Felimare picta | Marginal | E | 281 | 8.03 | 5.62 |

Supplementary Table 4. Results from Kruskal-Wallis test and pairwise comparison by Wilcoxon method between the tooth types for the atomic % and mechanical properties (elasticity modulus [E] and hardness [H], both in GPa) for all layers pooled together are given. Orange p-values = highly significant differences, red p-values = significant differences, black = no significant differences..

| Species | Element or mechanical property | Structure 1 | Structure 2 | 1-Way Test, ChiSquare approximation |  |  | Wilcoxon method |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | ChiSquare | df | p-value | p-value |
| Doris pseudoargus | Ae | Marginal | Lateral | 98.0788 | 2 | <.0001* | 0.1244 |
|  |  | Lateral | Central |  |  |  | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  | Ca | Marginal | Central | 19.7890 | 2 | <.0001* | 0.0116* |
|  |  | Lateral | Central |  |  |  | 0.0101* |
|  |  | Marginal | Lateral |  |  |  | <.0001* |
|  | Cl | Lateral | Central | 9.1884 | 2 | 0.0101* | 0.6672 |
|  |  | Marginal | Central |  |  |  | 0.1384 |
|  |  | Marginal | Lateral |  |  |  | 0.0013* |
|  | F | Marginal | Lateral | 274.5165 | 2 | <.0001* | <.0001* |
|  |  | Lateral | Central |  |  |  | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  | Fe | Lateral | Central | 183.2890 | 2 | <.0001* | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  |  | Marginal | Lateral |  |  |  | 0.8780 |
|  | K | Marginal | Lateral | 89.8537 | 2 | <.0001* | 0.0360* |
|  |  | Lateral | Central |  |  |  | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  | Mg | Lateral | Central | 163.1544 | 2 | <.0001* | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  |  | Marginal | Lateral |  |  |  | <.0001* |
|  | Na | Marginal | Lateral | 53.1768 | 2 | <.0001* | 0.0003* |
|  |  | Lateral | Central |  |  |  | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  | P | Marginal | Lateral | 149.5602 | 2 | <.0001* | 0.0077* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  |  | Lateral | Central |  |  |  | <.0001* |
|  | S | Lateral | Central | 67.0865 | 2 | <.0001* | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  |  | Marginal | Lateral |  |  |  | <.0001* |
|  | Si | Lateral | Central | 8.8357 | 2 | 0.0121* | 0.0046* |
|  |  | Marginal | Central |  |  |  | 0.0171* |
|  |  | Margina | Lateral |  |  |  | 0.4399 |
|  | Zn | Marginal | Lateral | 147.9725 | 2 | <.0001* | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  |  | Lateral | Central |  |  |  | 1.0000 |
|  | H | Marginal | Lateral | 68.6456 | 2 | <.0001* | <.0001* |
|  |  | Marginal | Central |  |  |  | 0.4090 |
|  |  | Lateral | Central |  |  |  | <.0001* |
|  | E | Marginal | Lateral | 16.2696 | 2 | <.0001* | 0.0005* |
|  |  | Marginal | Central |  |  |  | 0.3340 |
|  |  | Lateral | Central |  |  |  | 0.0002* |
| Felimare picta | Ae | Lateral | Central | 2.6509 | 2 | 0.2657 | 0.9712 |
|  |  | Marginal | Lateral |  |  |  | 0.1732 |
|  |  | Marginal | Central |  |  |  | 0.1354 |
|  | Ca | Lateral | Central | 1.7565 | 2 | 0.4155 | 0.7576 |
|  |  | Marginal | Central |  |  |  | 0.2978 |
|  |  | Marginal | Lateral |  |  |  | 0.2171 |
|  | Cl | Lateral | Central | 17.0668 | 2 | 0.0002* | 0.6100 |
|  |  | Marginal | Central |  |  |  | 0.0003* |
|  |  | Marginal | Lateral |  |  |  | 0.0003* |
|  | Cu | Marginal | Lateral | 25.6058 | 2 | <.0001* | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  |  | Lateral | Central |  |  |  | 0.9285 |
|  | Fe | Lateral | Central | 0.4923 | 2 | 0.7818 | 0.8918 |
|  |  | Marginal | Central |  |  |  | 0.5972 |
|  |  | Marginal | Lateral |  |  |  | 0.4976 |
|  | K | Lateral | Central | 2.4309 | 2 | 0.2966 | 0.7522 |
|  |  | Marginal | Lateral |  |  |  | 0.2162 |
|  |  | Marginal | Central |  |  |  | 0.1462 |
|  | Mg | Marginal | Central | 3.0558 | 2 | 0.2170 | 0.0795 |
|  |  | Marginal | Lateral |  |  |  | 0.3125 |
|  |  | Lateral | Central |  |  |  | 0.4549 |
|  | Na | Lateral | Central | 14.5591 | 2 | 0.0007* | 0.7203 |
|  |  | Marginal | Lateral |  |  |  | 0.0011* |
|  |  | Marginal | Central |  |  |  | 0.0006* |
|  | P | Lateral | Central | 3.2971 | 2 | 0.1923 | 0.5437 |
|  |  | Marginal | Lateral |  |  |  | 0.2002 |
|  |  | Marginal | Central |  |  |  | 0.0800 |
|  | S | Lateral | Central | 12.8046 | 2 | 0.0017* | 0.8635 |
|  |  | Marginal | Central |  |  |  | 0.0019* |
|  |  | Marginal | Lateral |  |  |  | 0.0015* |
|  | Si | Marginal | Lateral | 2.5546 | 2 | 0.2788 | 0.1545 |
|  |  | Marginal | Central |  |  |  | 0.1645 |
|  |  | Lateral | Central |  |  |  | 0.9711 |
|  | Zn | Marginal | Lateral | 76.4033 | 2 | <.0001* | <.0001* |
|  |  | Marginal | Central |  |  |  | <.0001* |
|  |  | Lateral | Central |  |  |  | 0.0572 |
|  | H | Marginal | Central | 0.0241 | 2 | 0.9880 | 0.8884 |
|  |  | Marginal | Lateral |  |  |  | 0.7698 |
|  |  | Lateral | Central |  |  |  | 0.6829 |
|  | E | Lateral | Central | 8.7846 | 2 | 0.0124* | 0.1564 |
|  |  | Marginal | Lateral |  |  |  | 0.0288* |
|  |  | Marginal | Central |  |  |  | 0.0095* |

Supplementary Figure 1. Results from the EDX analysis. For each layer studied, atomic % of analyzed elements are given. For values, see Supplementary Table 5.

Supplementary Table 5. Results from the EDX analysis (mean and standard deviation) and nanoindentation. For each species, atomic % of analyzed elements, hardness [H] (GPa), and Young’s modulus [E] (GPa) from each tooth type and each layer are given.

| Species | Tooth type | Layer | Element or mechanical property | Quantity of measurements | Mean | Standard deviation |
| --- | --- | --- | --- | --- | --- | --- |
| Doris pseudoargus | Central | Inner layer | Ae | 88 | 5.61 | 2.80 |
| Doris pseudoargus | Central | Leading edge | Ae | 20 | 17.45 | 5.82 |
| Doris pseudoargus | Central | Trailing edge | Ae | 20 | 6.28 | 2.68 |
| Doris pseudoargus | Lateral | Inner layer | Ae | 156 | 3.01 | 1.31 |
| Doris pseudoargus | Lateral | Leading edge | Ae | 20 | 16.65 | 4.48 |
| Doris pseudoargus | Lateral | Trailing edge | Ae | 20 | 5.56 | 2.43 |
| Doris pseudoargus | Marginal | Inner layer | Ae | 181 | 3.34 | 4.46 |
| Doris pseudoargus | Marginal | Leading edge | Ae | 20 | 18.21 | 4.92 |
| Doris pseudoargus | Marginal | Trailing edge | Ae | 20 | 5.27 | 2.58 |
| Felimare picta | Central | Inner layer | Ae | 104 | 2.32 | 1.63 |
| Felimare picta | Central | Leading edge | Ae | 20 | 24.29 | 6.26 |
| Felimare picta | Central | Trailing edge | Ae | 20 | 7.45 | 2.99 |
| Felimare picta | Lateral | Inner layer | Ae | 104 | 2.29 | 1.47 |
| Felimare picta | Lateral | Leading edge | Ae | 20 | 22.91 | 4.73 |
| Felimare picta | Lateral | Trailing edge | Ae | 20 | 7.17 | 2.60 |
| Felimare picta | Marginal | Inner layer | Ae | 82 | 1.68 | 0.78 |
| Felimare picta | Marginal | Leading edge | Ae | 20 | 25.46 | 4.53 |
| Felimare picta | Marginal | Trailing edge | Ae | 20 | 7.04 | 2.94 |
| Doris pseudoargus | Central | Inner layer | Ca | 88 | 0.93 | 1.62 |
| Doris pseudoargus | Central | Leading edge | Ca | 20 | 11.87 | 5.62 |
| Doris pseudoargus | Central | Trailing edge | Ca | 20 | 3.82 | 2.52 |
| Doris pseudoargus | Lateral | Inner layer | Ca | 156 | 1.11 | 1.02 |
| Doris pseudoargus | Lateral | Leading edge | Ca | 20 | 10.41 | 3.92 |
| Doris pseudoargus | Lateral | Trailing edge | Ca | 20 | 3.80 | 2.45 |
| Doris pseudoargus | Marginal | Inner layer | Ca | 181 | 1.01 | 1.98 |
| Doris pseudoargus | Marginal | Leading edge | Ca | 20 | 12.40 | 4.35 |
| Doris pseudoargus | Marginal | Trailing edge | Ca | 20 | 3.42 | 2.44 |
| Felimare picta | Central | Inner layer | Ca | 104 | 0.07 | 0.08 |
| Felimare picta | Central | Leading edge | Ca | 20 | 5.17 | 1.49 |
| Felimare picta | Central | Trailing edge | Ca | 20 | 0.65 | 0.54 |
| Felimare picta | Lateral | Inner layer | Ca | 104 | 0.07 | 0.08 |
| Felimare picta | Lateral | Leading edge | Ca | 20 | 5.27 | 1.79 |
| Felimare picta | Lateral | Trailing edge | Ca | 20 | 0.82 | 0.52 |
| Felimare picta | Marginal | Inner layer | Ca | 82 | 0.04 | 0.03 |
| Felimare picta | Marginal | Leading edge | Ca | 20 | 5.25 | 1.67 |
| Felimare picta | Marginal | Trailing edge | Ca | 20 | 1.04 | 0.87 |
| Doris pseudoargus | Central | Inner layer | Cl | 88 | 0.03 | 0.02 |
| Doris pseudoargus | Central | Leading edge | Cl | 20 | 1.54 | 0.53 |
| Doris pseudoargus | Central | Trailing edge | Cl | 20 | 0.21 | 0.20 |
| Doris pseudoargus | Lateral | Inner layer | Cl | 156 | 0.03 | 0.03 |
| Doris pseudoargus | Lateral | Leading edge | Cl | 20 | 1.69 | 0.59 |
| Doris pseudoargus | Lateral | Trailing edge | Cl | 20 | 0.27 | 0.23 |
| Doris pseudoargus | Marginal | Inner layer | Cl | 181 | 0.09 | 0.71 |
| Doris pseudoargus | Marginal | Leading edge | Cl | 20 | 1.62 | 0.78 |
| Doris pseudoargus | Marginal | Trailing edge | Cl | 20 | 0.29 | 0.33 |
| Felimare picta | Central | Inner layer | Cl | 104 | 0.62 | 0.65 |
| Felimare picta | Central | Leading edge | Cl | 20 | 1.43 | 0.49 |
| Felimare picta | Central | Trailing edge | Cl | 20 | 0.20 | 0.20 |
| Felimare picta | Lateral | Inner layer | Cl | 104 | 0.62 | 0.61 |
| Felimare picta | Lateral | Leading edge | Cl | 20 | 1.55 | 0.55 |
| Felimare picta | Lateral | Trailing edge | Cl | 20 | 0.26 | 0.21 |
| Felimare picta | Marginal | Inner layer | Cl | 82 | 0.35 | 0.40 |
| Felimare picta | Marginal | Leading edge | Cl | 20 | 1.49 | 0.74 |
| Felimare picta | Marginal | Trailing edge | Cl | 20 | 0.28 | 0.33 |
| Doris pseudoargus | Central | Inner layer | Cu | 88 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Leading edge | Cu | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Trailing edge | Cu | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Inner layer | Cu | 156 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Leading edge | Cu | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Trailing edge | Cu | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Inner layer | Cu | 181 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Leading edge | Cu | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Trailing edge | Cu | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Inner layer | Cu | 104 | 0.05 | 0.11 |
| Felimare picta | Central | Leading edge | Cu | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Trailing edge | Cu | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Inner layer | Cu | 104 | 0.05 | 0.10 |
| Felimare picta | Lateral | Leading edge | Cu | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Trailing edge | Cu | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Inner layer | Cu | 82 | 0.15 | 0.15 |
| Felimare picta | Marginal | Leading edge | Cu | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Trailing edge | Cu | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Inner layer | F | 88 | 2.55 | 1.61 |
| Doris pseudoargus | Central | Leading edge | F | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Trailing edge | F | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Inner layer | F | 156 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Leading edge | F | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Trailing edge | F | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Inner layer | F | 181 | 0.07 | 0.22 |
| Doris pseudoargus | Marginal | Leading edge | F | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Trailing edge | F | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Inner layer | F | 104 | 0.00 | 0.00 |
| Felimare picta | Central | Leading edge | F | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Trailing edge | F | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Inner layer | F | 104 | 0.00 | 0.00 |
| Felimare picta | Lateral | Leading edge | F | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Trailing edge | F | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Inner layer | F | 82 | 0.00 | 0.00 |
| Felimare picta | Marginal | Leading edge | F | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Trailing edge | F | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Inner layer | Fe | 88 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Leading edge | Fe | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Trailing edge | Fe | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Inner layer | Fe | 156 | 0.05 | 0.02 |
| Doris pseudoargus | Lateral | Leading edge | Fe | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Trailing edge | Fe | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Inner layer | Fe | 181 | 0.19 | 1.28 |
| Doris pseudoargus | Marginal | Leading edge | Fe | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Trailing edge | Fe | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Inner layer | Fe | 104 | 0.06 | 0.05 |
| Felimare picta | Central | Leading edge | Fe | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Trailing edge | Fe | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Inner layer | Fe | 104 | 0.06 | 0.04 |
| Felimare picta | Lateral | Leading edge | Fe | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Trailing edge | Fe | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Inner layer | Fe | 82 | 0.06 | 0.05 |
| Felimare picta | Marginal | Leading edge | Fe | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Trailing edge | Fe | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Inner layer | K | 88 | 0.87 | 1.09 |
| Doris pseudoargus | Central | Leading edge | K | 20 | 0.57 | 0.37 |
| Doris pseudoargus | Central | Trailing edge | K | 20 | 0.12 | 0.13 |
| Doris pseudoargus | Lateral | Inner layer | K | 156 | 0.03 | 0.02 |
| Doris pseudoargus | Lateral | Leading edge | K | 20 | 0.46 | 0.33 |
| Doris pseudoargus | Lateral | Trailing edge | K | 20 | 0.13 | 0.20 |
| Doris pseudoargus | Marginal | Inner layer | K | 181 | 0.03 | 0.03 |
| Doris pseudoargus | Marginal | Leading edge | K | 20 | 0.67 | 0.55 |
| Doris pseudoargus | Marginal | Trailing edge | K | 20 | 0.12 | 0.12 |
| Felimare picta | Central | Inner layer | K | 104 | 0.11 | 0.24 |
| Felimare picta | Central | Leading edge | K | 20 | 0.52 | 0.31 |
| Felimare picta | Central | Trailing edge | K | 20 | 0.12 | 0.13 |
| Felimare picta | Lateral | Inner layer | K | 104 | 0.11 | 0.22 |
| Felimare picta | Lateral | Leading edge | K | 20 | 0.42 | 0.29 |
| Felimare picta | Lateral | Trailing edge | K | 20 | 0.12 | 0.20 |
| Felimare picta | Marginal | Inner layer | K | 82 | 0.04 | 0.05 |
| Felimare picta | Marginal | Leading edge | K | 20 | 0.60 | 0.47 |
| Felimare picta | Marginal | Trailing edge | K | 20 | 0.12 | 0.12 |
| Doris pseudoargus | Central | Inner layer | Mg | 88 | 0.28 | 0.45 |
| Doris pseudoargus | Central | Leading edge | Mg | 20 | 0.18 | 0.10 |
| Doris pseudoargus | Central | Trailing edge | Mg | 20 | 0.15 | 0.13 |
| Doris pseudoargus | Lateral | Inner layer | Mg | 156 | 1.07 | 0.33 |
| Doris pseudoargus | Lateral | Leading edge | Mg | 20 | 0.21 | 0.12 |
| Doris pseudoargus | Lateral | Trailing edge | Mg | 20 | 0.20 | 0.20 |
| Doris pseudoargus | Marginal | Inner layer | Mg | 181 | 0.58 | 0.45 |
| Doris pseudoargus | Marginal | Leading edge | Mg | 20 | 0.18 | 0.11 |
| Doris pseudoargus | Marginal | Trailing edge | Mg | 20 | 0.25 | 0.28 |
| Felimare picta | Central | Inner layer | Mg | 104 | 0.23 | 0.96 |
| Felimare picta | Central | Leading edge | Mg | 20 | 0.17 | 0.09 |
| Felimare picta | Central | Trailing edge | Mg | 20 | 0.13 | 0.12 |
| Felimare picta | Lateral | Inner layer | Mg | 104 | 0.23 | 0.87 |
| Felimare picta | Lateral | Leading edge | Mg | 20 | 0.19 | 0.11 |
| Felimare picta | Lateral | Trailing edge | Mg | 20 | 0.19 | 0.19 |
| Felimare picta | Marginal | Inner layer | Mg | 82 | 0.16 | 0.05 |
| Felimare picta | Marginal | Leading edge | Mg | 20 | 0.16 | 0.10 |
| Felimare picta | Marginal | Trailing edge | Mg | 20 | 0.23 | 0.24 |
| Doris pseudoargus | Central | Inner layer | Na | 88 | 0.84 | 0.55 |
| Doris pseudoargus | Central | Leading edge | Na | 20 | 0.85 | 0.31 |
| Doris pseudoargus | Central | Trailing edge | Na | 20 | 0.63 | 0.46 |
| Doris pseudoargus | Lateral | Inner layer | Na | 156 | 0.45 | 0.16 |
| Doris pseudoargus | Lateral | Leading edge | Na | 20 | 0.92 | 0.33 |
| Doris pseudoargus | Lateral | Trailing edge | Na | 20 | 0.60 | 0.45 |
| Doris pseudoargus | Marginal | Inner layer | Na | 181 | 0.58 | 1.02 |
| Doris pseudoargus | Marginal | Leading edge | Na | 20 | 0.76 | 0.32 |
| Doris pseudoargus | Marginal | Trailing edge | Na | 20 | 0.50 | 0.30 |
| Felimare picta | Central | Inner layer | Na | 104 | 0.74 | 0.41 |
| Felimare picta | Central | Leading edge | Na | 20 | 0.78 | 0.28 |
| Felimare picta | Central | Trailing edge | Na | 20 | 0.57 | 0.40 |
| Felimare picta | Lateral | Inner layer | Na | 104 | 0.74 | 0.39 |
| Felimare picta | Lateral | Leading edge | Na | 20 | 0.84 | 0.31 |
| Felimare picta | Lateral | Trailing edge | Na | 20 | 0.54 | 0.38 |
| Felimare picta | Marginal | Inner layer | Na | 82 | 0.51 | 0.57 |
| Felimare picta | Marginal | Leading edge | Na | 20 | 0.70 | 0.29 |
| Felimare picta | Marginal | Trailing edge | Na | 20 | 0.46 | 0.26 |
| Doris pseudoargus | Central | Inner layer | P | 88 | 0.71 | 0.89 |
| Doris pseudoargus | Central | Leading edge | P | 20 | 0.84 | 0.66 |
| Doris pseudoargus | Central | Trailing edge | P | 20 | 0.23 | 0.23 |
| Doris pseudoargus | Lateral | Inner layer | P | 156 | 0.04 | 0.07 |
| Doris pseudoargus | Lateral | Leading edge | P | 20 | 0.85 | 0.76 |
| Doris pseudoargus | Lateral | Trailing edge | P | 20 | 0.14 | 0.14 |
| Doris pseudoargus | Marginal | Inner layer | P | 181 | 0.23 | 0.62 |
| Doris pseudoargus | Marginal | Leading edge | P | 20 | 0.95 | 0.80 |
| Doris pseudoargus | Marginal | Trailing edge | P | 20 | 0.18 | 0.24 |
| Felimare picta | Central | Inner layer | P | 104 | 0.02 | 0.05 |
| Felimare picta | Central | Leading edge | P | 20 | 0.77 | 0.60 |
| Felimare picta | Central | Trailing edge | P | 20 | 0.21 | 0.20 |
| Felimare picta | Lateral | Inner layer | P | 104 | 0.02 | 0.05 |
| Felimare picta | Lateral | Leading edge | P | 20 | 0.77 | 0.69 |
| Felimare picta | Lateral | Trailing edge | P | 20 | 0.14 | 0.13 |
| Felimare picta | Marginal | Inner layer | P | 82 | 0.01 | 0.01 |
| Felimare picta | Marginal | Leading edge | P | 20 | 0.86 | 0.71 |
| Felimare picta | Marginal | Trailing edge | P | 20 | 0.18 | 0.24 |
| Doris pseudoargus | Central | Inner layer | S | 88 | 0.05 | 0.06 |
| Doris pseudoargus | Central | Leading edge | S | 20 | 1.21 | 0.67 |
| Doris pseudoargus | Central | Trailing edge | S | 20 | 0.14 | 0.18 |
| Doris pseudoargus | Lateral | Inner layer | S | 156 | 0.20 | 0.11 |
| Doris pseudoargus | Lateral | Leading edge | S | 20 | 1.33 | 0.68 |
| Doris pseudoargus | Lateral | Trailing edge | S | 20 | 0.11 | 0.15 |
| Doris pseudoargus | Marginal | Inner layer | S | 181 | 0.17 | 0.42 |
| Doris pseudoargus | Marginal | Leading edge | S | 20 | 1.07 | 0.43 |
| Doris pseudoargus | Marginal | Trailing edge | S | 20 | 0.10 | 0.14 |
| Felimare picta | Central | Inner layer | S | 104 | 0.37 | 0.37 |
| Felimare picta | Central | Leading edge | S | 20 | 1.12 | 0.63 |
| Felimare picta | Central | Trailing edge | S | 20 | 0.13 | 0.18 |
| Felimare picta | Lateral | Inner layer | S | 104 | 0.37 | 0.34 |
| Felimare picta | Lateral | Leading edge | S | 20 | 1.22 | 0.64 |
| Felimare picta | Lateral | Trailing edge | S | 20 | 0.10 | 0.14 |
| Felimare picta | Marginal | Inner layer | S | 82 | 0.25 | 0.08 |
| Felimare picta | Marginal | Leading edge | S | 20 | 0.98 | 0.38 |
| Felimare picta | Marginal | Trailing edge | S | 20 | 0.10 | 0.14 |
| Doris pseudoargus | Central | Inner layer | Si | 88 | 0.03 | 0.07 |
| Doris pseudoargus | Central | Leading edge | Si | 20 | 0.38 | 0.50 |
| Doris pseudoargus | Central | Trailing edge | Si | 20 | 0.31 | 0.35 |
| Doris pseudoargus | Lateral | Inner layer | Si | 156 | 0.03 | 0.02 |
| Doris pseudoargus | Lateral | Leading edge | Si | 20 | 0.78 | 1.79 |
| Doris pseudoargus | Lateral | Trailing edge | Si | 20 | 0.31 | 0.27 |
| Doris pseudoargus | Marginal | Inner layer | Si | 181 | 0.09 | 0.34 |
| Doris pseudoargus | Marginal | Leading edge | Si | 20 | 0.56 | 1.19 |
| Doris pseudoargus | Marginal | Trailing edge | Si | 20 | 0.39 | 0.28 |
| Felimare picta | Central | Inner layer | Si | 104 | 0.01 | 0.01 |
| Felimare picta | Central | Leading edge | Si | 20 | 14.33 | 5.38 |
| Felimare picta | Central | Trailing edge | Si | 20 | 5.43 | 2.62 |
| Felimare picta | Lateral | Inner layer | Si | 104 | 0.01 | 0.01 |
| Felimare picta | Lateral | Leading edge | Si | 20 | 12.64 | 3.35 |
| Felimare picta | Lateral | Trailing edge | Si | 20 | 5.00 | 2.41 |
| Felimare picta | Marginal | Inner layer | Si | 82 | 0.01 | 0.01 |
| Felimare picta | Marginal | Leading edge | Si | 20 | 15.42 | 3.32 |
| Felimare picta | Marginal | Trailing edge | Si | 20 | 4.63 | 2.74 |
| Doris pseudoargus | Central | Inner layer | Zn | 88 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Leading edge | Zn | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Trailing edge | Zn | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Inner layer | Zn | 156 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Leading edge | Zn | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Lateral | Trailing edge | Zn | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Inner layer | Zn | 181 | 0.29 | 0.38 |
| Doris pseudoargus | Marginal | Leading edge | Zn | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Marginal | Trailing edge | Zn | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Inner layer | Zn | 104 | 0.03 | 0.14 |
| Felimare picta | Central | Leading edge | Zn | 20 | 0.00 | 0.00 |
| Felimare picta | Central | Trailing edge | Zn | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Inner layer | Zn | 104 | 0.01 | 0.07 |
| Felimare picta | Lateral | Leading edge | Zn | 20 | 0.00 | 0.00 |
| Felimare picta | Lateral | Trailing edge | Zn | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Inner layer | Zn | 82 | 0.11 | 0.14 |
| Felimare picta | Marginal | Leading edge | Zn | 20 | 0.00 | 0.00 |
| Felimare picta | Marginal | Trailing edge | Zn | 20 | 0.00 | 0.00 |
| Doris pseudoargus | Central | Inner layer, all regions pooled together | H | 300 | 0.37 | 0.06 |
| Doris pseudoargus | Lateral | Inner layer, all regions pooled together | H | 300 | 0.34 | 0.06 |
| Doris pseudoargus | Marginal | Inner layer, all regions pooled together | H | 597 | 0.35 | 0.09 |
| Felimare picta | Central | Inner layer, all regions pooled together | H | 270 | 0.35 | 0.20 |
| Felimare picta | Lateral | Inner layer, all regions pooled together | H | 270 | 0.34 | 0.18 |
| Felimare picta | Marginal | Inner layer, all regions pooled together | H | 270 | 0.35 | 0.19 |
| Doris pseudoargus | Central | Inner layer, basis | H | 100 | 0.38 | 0.03 |
| Doris pseudoargus | Central | Inner layer, stylus | H | 100 | 0.36 | 0.07 |
| Doris pseudoargus | Central | Inner layer, tip | H | 100 | 0.39 | 0.08 |
| Doris pseudoargus | Lateral | Inner layer, basis | H | 100 | 0.29 | 0.02 |
| Doris pseudoargus | Lateral | Inner layer, stylus | H | 100 | 0.37 | 0.00 |
| Doris pseudoargus | Lateral | Inner layer, tip | H | 100 | 0.35 | 0.08 |
| Doris pseudoargus | Marginal | Inner layer, basis | H | 199 | 0.24 | 0.04 |
| Doris pseudoargus | Marginal | Inner layer, stylus | H | 199 | 0.41 | 0.02 |
| Doris pseudoargus | Marginal | Inner layer, tip | H | 199 | 0.39 | 0.07 |
| Doris pseudoargus | Central | Leading edge | H | 6 | 1.28 | 0.53 |
| Doris pseudoargus | Central | Trailing edge | H | 7 | 0.73 | 0.26 |
| Doris pseudoargus | Lateral | Leading edge | H | 8 | 1.42 | 0.66 |
| Doris pseudoargus | Lateral | Trailing edge | H | 7 | 0.66 | 0.23 |
| Doris pseudoargus | Marginal | Leading edge | H | 7 | 1.41 | 0.56 |
| Doris pseudoargus | Marginal | Trailing edge | H | 6 | 0.76 | 0.27 |
| Felimare picta | Central | Inner layer, basis | H | 90 | 0.22 | 0.02 |
| Felimare picta | Central | Inner layer, stylus | H | 90 | 0.21 | 0.05 |
| Felimare picta | Central | Inner layer, tip | H | 90 | 0.62 | 0.07 |
| Felimare picta | Lateral | Inner layer, basis | H | 90 | 0.21 | 0.03 |
| Felimare picta | Lateral | Inner layer, stylus | H | 90 | 0.24 | 0.02 |
| Felimare picta | Lateral | Inner layer, tip | H | 90 | 0.59 | 0.06 |
| Felimare picta | Marginal | Inner layer, basis | H | 90 | 0.20 | 0.03 |
| Felimare picta | Marginal | Inner layer, stylus | H | 90 | 0.24 | 0.01 |
| Felimare picta | Marginal | Inner layer, tip | H | 90 | 0.60 | 0.12 |
| Felimare picta | Central | Leading edge | H | 5 | 1.81 | 0.46 |
| Felimare picta | Central | Trailing edge | H | 6 | 1.03 | 0.19 |
| Felimare picta | Lateral | Leading edge | H | 6 | 2.16 | 0.20 |
| Felimare picta | Lateral | Trailing edge | H | 5 | 1.00 | 0.13 |
| Felimare picta | Marginal | Leading edge | H | 6 | 1.98 | 0.38 |
| Felimare picta | Marginal | Trailing edge | H | 5 | 1.04 | 0.15 |
| Doris pseudoargus | Central | Inner layer, all regions pooled together | E | 300 | 8.26 | 2.48 |
| Doris pseudoargus | Lateral | Inner layer, all regions pooled together | E | 300 | 7.66 | 2.92 |
| Doris pseudoargus | Marginal | Inner layer, all regions pooled together | E | 597 | 8.27 | 2.72 |
| Felimare picta | Central | Inner layer, all regions pooled together | E | 270 | 7.67 | 3.09 |
| Felimare picta | Lateral | Inner layer, all regions pooled together | E | 270 | 7.39 | 2.80 |
| Felimare picta | Marginal | Inner layer, all regions pooled together | E | 270 | 7.11 | 2.74 |
| Doris pseudoargus | Central | Inner layer, basis | E | 100 | 5.67 | 0.28 |
| Doris pseudoargus | Central | Inner layer, stylus | E | 100 | 7.80 | 0.81 |
| Doris pseudoargus | Central | Inner layer, tip | E | 100 | 11.31 | 1.18 |
| Doris pseudoargus | Lateral | Inner layer, basis | E | 100 | 4.89 | 0.18 |
| Doris pseudoargus | Lateral | Inner layer, stylus | E | 100 | 6.69 | 0.10 |
| Doris pseudoargus | Lateral | Inner layer, tip | E | 100 | 11.39 | 1.75 |
| Doris pseudoargus | Marginal | Inner layer, basis | E | 199 | 6.31 | 0.60 |
| Doris pseudoargus | Marginal | Inner layer, stylus | E | 199 | 6.62 | 0.18 |
| Doris pseudoargus | Marginal | Inner layer, tip | E | 199 | 11.89 | 1.46 |
| Doris pseudoargus | Central | Leading edge | E | 6 | 31.02 | 7.52 |
| Doris pseudoargus | Central | Trailing edge | E | 7 | 21.00 | 3.58 |
| Doris pseudoargus | Lateral | Leading edge | E | 8 | 33.71 | 6.68 |
| Doris pseudoargus | Lateral | Trailing edge | E | 7 | 22.06 | 3.29 |
| Doris pseudoargus | Marginal | Leading edge | E | 7 | 31.39 | 5.96 |
| Doris pseudoargus | Marginal | Trailing edge | E | 6 | 20.71 | 4.29 |
| Felimare picta | Central | Inner layer, basis | E | 90 | 5.16 | 0.44 |
| Felimare picta | Central | Inner layer, stylus | E | 90 | 6.06 | 0.34 |
| Felimare picta | Central | Inner layer, tip | E | 90 | 11.81 | 1.49 |
| Felimare picta | Lateral | Inner layer, basis | E | 90 | 4.98 | 0.47 |
| Felimare picta | Lateral | Inner layer, stylus | E | 90 | 6.03 | 0.12 |
| Felimare picta | Lateral | Inner layer, tip | E | 90 | 11.16 | 1.14 |
| Felimare picta | Marginal | Inner layer, basis | E | 90 | 4.82 | 0.45 |
| Felimare picta | Marginal | Inner layer, stylus | E | 90 | 5.91 | 0.20 |
| Felimare picta | Marginal | Inner layer, tip | E | 90 | 10.59 | 1.86 |
| Felimare picta | Central | Leading edge | E | 5 | 38.45 | 4.06 |
| Felimare picta | Central | Trailing edge | E | 6 | 20.39 | 1.34 |
| Felimare picta | Lateral | Leading edge | E | 6 | 41.08 | 3.80 |
| Felimare picta | Lateral | Trailing edge | E | 5 | 20.89 | 1.88 |
| Felimare picta | Marginal | Leading edge | E | 6 | 38.58 | 4.75 |
| Felimare picta | Marginal | Trailing edge | E | 5 | 21.15 | 1.65 |

Supplementary Table 6. Results from the Kruskal-Wallis test and pairwise comparison by Wilcoxon method between the outer layers and inner layer or between the different tooth regions for the atomic % and mechanical properties are given. Orange p-values = highly significant differences, red p-values = significant differences, black = no significant differences. E, Young’s modulus; h, hardness.

| Species | Tooth type | Element | Region 1 | Region 2 |  | 1-Way Test, ChiSquare approximation |  |  |  |  | Wilcoxon method |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | ChiSquare |  | df |  | p-value | p-value |
| Doris pseudoargus | Central | Ae | Leading edge | Inner layer |  | 48.4186 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.1675 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Ca | Leading edge | Inner layer |  | 65.5340 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Cl | Leading edge | Inner layer |  | 72.9844 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | F | Trailing edge | Leading edge |  | 84.4365 |  | 2 |  | <.0001* | 1.0000 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | K | Leading edge | Inner layer |  | 14.4277 |  | 2 |  | <.0001* | 0.4110 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0011* |
|  |  | Mg | Leading edge | Inner layer |  | 12.2782 |  | 2 |  | <.0001* | 0.0007* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.1409 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.1550 |
|  |  | Na | Leading edge | Inner layer |  | 2.7815 |  | 2 |  | 0.2489 | 0.4786 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.1135 |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.1485 |
|  |  | P | Leading edge | Inner layer |  | 10.6508 |  | 2 |  | 0.0049* | 0.1467 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0005* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0145* |
|  |  | S | Leading edge | Inner layer |  | 53.8300 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0200* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Si | Leading edge | Inner layer |  | 40.5064 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0002* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.5693 |
|  |  | H | Tip | Stylus |  | 33.0797 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Tip | Basis |  |  |  |  |  |  | <.0001* |
|  |  |  | Stylus | Basis |  |  |  |  |  |  | 0.2298 |
|  |  | E | Stylus | Basis |  | 254.8316 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Tip | Basis |  |  |  |  |  |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  | Lateral | Ae | Leading edge | Inner layer |  | 74.8132 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Ca | Leading edge | Inner layer |  | 77.7401 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Cl | Leading edge | Inner layer |  | 79.2103 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Fe | Trailing edge | Leading edge |  | 95.9001 |  | 2 |  | <.0001* | 1.0000 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | K | Leading edge | Inner layer |  | 55.4398 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0048* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0003* |
|  |  | Mg | Trailing edge | Leading edge |  | 86.6200 |  | 2 |  | <.0001* | 0.3103 |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | Na | Leading edge | Inner layer |  | 42.4009 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.1078 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0275* |
|  |  | P | Leading edge | Inner layer |  | 54.9388 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0007* |
|  |  | S | Leading edge | Inner layer |  | 67.0182 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | Si | Trailing edge | Inner layer |  | 52.1596 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.4988 |
|  |  | H | Stylus | Basis |  | 115.3400 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Tip | Basis |  |  |  |  |  |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | 0.0211* |
|  |  | E | Stylus | Basis |  | 257.8870 |  | 2 |  | <.0001* | <.0001* |
|  |  |  | Tip | Basis |  |  |  |  |  |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  | Marginal | Ae | Leading edge | Inner layer | 67.2933 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Ca | Leading edge | Inner layer | 79.0973 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Cl | Leading edge | Inner layer | 71.2773 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | K | Leading edge | Inner layer | 69.6977 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Mg | Trailing edge | Leading edge | 35.1900 |  | 2 |  | <.0001* |  | 0.8392 |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | Na | Leading edge | Inner layer | 22.7291 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0097* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0090* |
|  |  | P | Leading edge | Inner layer | 63.5834 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0001* |
|  |  | S | Leading edge | Inner layer | 49.0587 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0150* |
|  |  | Si | Trailing edge | Inner layer | 46.7234 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.4732 |
|  |  | Zn | Trailing edge | Leading edge | 28.6095 |  | 2 |  | <.0001* |  | 1.0000 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | 0.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0001* |
|  |  | H | Stylus | Basis | 353.3977 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Basis |  |  |  |  |  |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | 0.0010* |
|  |  | E | Tip | Basis | 387.4024 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  |  |  | Stylus | Basis |  |  |  |  |  |  | <.0001* |
| Felimare picta | Central | Ae | Leading edge | Inner layer | 83.6145 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Ca | Leading edge | Inner layer | 77.1709 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Cl | Leading edge | Inner layer | 60.1739 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | Cu | Trailing edge | Leading edge | 14.2152 |  | 2 |  | 0.0008* |  | 1.0000 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | 0.0068* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0068* |
|  |  | Fe | Trailing edge | Leading edge | 86.4515 |  | 2 |  | <.0001* |  | 1.0000 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | K | Leading edge | Inner layer | 38.0032 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.1204 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Na | Leading edge | Inner layer | 4.5235 |  | 2 |  | 0.1042 |  | 0.2345 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.1404 |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0718 |
|  |  | P | Leading edge | Inner layer | 77.3991 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0004* |
|  |  | S | Leading edge | Inner layer | 59.7762 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | Si | Leading edge | Inner layer | 88.5871 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | H | Tip | Basis | 180.7640 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  |  |  | Stylus | Basis |  |  |  |  |  |  | 0.0735 |
|  |  | E | Tip | Basis | 231.7960 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  |  |  | Stylus | Basis |  |  |  |  |  |  | <.0001* |
|  | Lateral | Ae | Leading edge | Inner layer | 84.9627 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Ca | Leading edge | Inner layer | 87.7170 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Cl | Leading edge | Inner layer | 51.5047 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0001* |
|  |  | K | Leading edge | Inner layer | 27.6786 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.7326 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0003* |
|  |  | Na | Leading edge | Inner layer | 6.0541 |  | 2 |  | 0.0485* |  | 0.0960 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0275* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.1044 |
|  |  | P | Leading edge | Inner layer | 54.2269 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0007* |
|  |  | S | Leading edge | Inner layer | 70.1817 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | Si | Leading edge | Inner layer | 91.2429 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | H | Tip | Basis | 205.8451 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  |  |  | Stylus | Basis |  |  |  |  |  |  | <.0001* |
|  |  | E | Tip | Basis | 238.2907 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  |  |  | Stylus | Basis |  |  |  |  |  |  | <.0001* |
|  | Marginal | Ae | Leading edge | Inner layer | 82.6348 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Ca | Leading edge | Inner layer | 83.6604 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Cl | Leading edge | Inner layer | 34.9918 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.5748 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Cu | Trailing edge | Leading edge | 38.5512 |  | 2 |  | <.0001* |  | 1.0000 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | K | Leading edge | Inner layer | 54.2690 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0003* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Mg | Trailing edge | Leading edge | 0.3227 |  | 2 |  | 0.8510 |  | 0.9461 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | 0.9192 |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.5291 |
|  |  | Na | Leading edge | Inner layer | 5.5532 |  | 2 |  | 0.0622 |  | 0.0419* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.4599 |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0102* |
|  |  | P | Leading edge | Inner layer | 84.2264 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | 0.0002* |
|  |  | S | Leading edge | Inner layer | 51.2244 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  | Si | Leading edge | Inner layer | 86.2440 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | <.0001* |
|  |  |  | Trailing edge | Leading edge |  |  |  |  |  |  | <.0001* |
|  |  | Zn | Trailing edge | Leading edge | 27.3434 |  | 2 |  | <.0001* |  | 1.0000 |
|  |  |  | Leading edge | Inner layer |  |  |  |  |  |  | 0.0001* |
|  |  |  | Trailing edge | Inner layer |  |  |  |  |  |  | 0.0001* |
|  |  | H | Tip | Basis | 215.4982 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001* |
|  |  |  | Stylus | Basis |  |  |  |  |  |  | <.0001* |
|  |  | E | Stylus | Basis | 239.1144 |  | 2 |  | <.0001* |  | <.0001* |
|  |  |  | Tip | Basis |  |  |  |  |  |  | <.0001* |
|  |  |  | Tip | Stylus |  |  |  |  |  |  | <.0001 |