Supporting Information for

Hydrogen-controlled structural reconstruction of palladium-bismuth oxide cluster to single atom alloy for low temperature CO Oxidation

Bing Nan,1,4 #* Lulu Li2 #, Yunan Li,4 Lingling Guo,1, 4 Meng Du,1, 4 Zhengwu Liu,4 Xin Tao,4 Chen, Tian,4 Zhenye Liang,4 Yanxing Zhang,3* Chao Ma,5 Lu Shen,6 Rui Si,4* Lina Li,1,4*

1 Shanghai Synchrotron Radiation Facility, Zhangjiang Laboratory, Shanghai Advanced Research Institute Shanghai, 201210, China

2 State Key Laboratory for Modification of Chemical Fibers and Polymer Materials, College of Environmental Science and Engineering, Donghua University, Shanghai 201620, China

3 School of Physics, Henan Normal University, Xinxiang, 453007, China

4 Shanghai Institute of Applied Physics, Chinese Academy of Sciences, Shanghai, 201204, China

5 Center for High Resolution Electron Microscopy, College of Materials Science and Engineering, Hunan University, Changsha 410082, China

6 Division of China, TILON Group Technology Limited, Shanghai 200090, China

# Bing Nan and Lulu Li contributed equally to this manuscript.

# *E-mail: nanb@sari.ac.cn, lilina@sinap.ac.cn, sirui@mail.sysu.edu.cn, zhangyanxing@htu.edu.cn.

Table S1. Bulk Pd and Bi concentration, temperature of reduction peaks (TR) and hydrogen consumption from H2TPR, BET specific surface areas (SBET), BJH pore volume (Vp), average clusters size (DTEM) for Pd/PdBi-SiO2 samples.

| Sample | Pd (wt.%)a | Bi (wt.%)a | TR (°C) | H2 (μmol g−1)b | SBET (m2/g)c | Vp (cm3/g)c | DTEM (nm)d |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SiO2 | — | — | — | — | 430 | 1.32 | — |
| 1Pd-SiO2 | 0.8 | — | 62 | 210α, 194β | 420 | 1.36 | 3.0±0.7 4.1±0.7e |
| 1Pd2Bi-SiO2 | 0.8 | 2.6 | 144, 366, 413 | 327α, 280β | 386 | 1.23 | 2.3±0.7 3.2±0.7e |
| 1Pd5Bi-SiO2 | 0.8 | 5.8 | 206, 395 | 829α, 797β | 355 | 1.17 | 2.1±0.5 3.1±0.5e |

a Determined by ICP-AES.; b Actual value of H2 consumptions (α) and theoretical values (β) of H2 consumption calculated according to Pd2+ → Pd0 and Bi3+ → Bi0; c From N2 adsorption/desorption experiments; d Statistic data from over 100 clusters on the basis of TEM images, e after CO oxidation.

Table S2. Oxidation state of palladium (δ) and Pd K-edge EXAFS fitting results (R: distance; CN: coordination number; σ2: Debye-Waller factor a; △E0: inner potential correction b) of Pd/PdBi-SiO2 samples.

| Sample | δ | Pd-O |  | Pd-Pd (metallic) |  | Pd-Pd (Pd-O-Pd) |  | Pd-Bi (Pd-O-Bi) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | R (Å) | CN | R (Å) | CN | R (Å) | CN | R (Å) | CN |
| 1Pd-SiO2 (fresh) | 1.9 | 2.04±0.02 | 4.2±0.6 | — | — | 3.12±0.01 | 5.0±0.9 | — | — |
| 1Pd2Bi-SiO2 (fresh) | 1.8 | 2.04±0.01 | 5.0±0.1 | — | — | 3.07±0.01 | 1.2±0.5 | 3.36±0.03 | 3.1±0.8 |
| 1Pd5Bi-SiO2 (fresh) | 1.8 | 2.04±0.01 | 4.4±0.4 | — | — | 3.08±0.02 | 2.1±0.9 | 3.37±0.04 | 2.6±1.1 |
| 1Pd-SiO2 (used) | 0.5 | 1.98±0.01 | 1.4±0.3 | 2.73±0.01 | 7.0±0.3 | — | — | — | — |
| 1Pd2Bi-SiO2 (used) | 0.3 | 2.00±0.01 | 1.4±0.3 | 2.74±0.01 | 4.0±0.5 | — | — | 3.36±0.02 | 3.3±1.0 |
| 1Pd5Bi-SiO2 (used) | 0.3 | 2.00±0.01 | 1.4±0.4 | 2.74±0.01 | 4.2±0.4 | — | — | — | — |

a D.W. = 0.003±0.001, 0.005±0.001 Å2 for all the analyzed PdO, PdPd/Bi shells, respectively; b△E0 = 10.3 (set) eV and -8.9±1.1 eV for all fresh and used Pd/PdBi-SiO2, respectively.

Table S3. Oxidation state of bismuth (δ) and Bi L3-edge EXAFS fitting results (R: distance; CN: coordination number; σ2: Debye-Waller factor a) of PdBi-SiO2 samples.

| Sample | δ | Bi-O |  | Metallic Bi-Pd |  | Bi-Bi |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | R (Å) | CN | R (Å) | CN | R (Å) | CN |
| 1Pd2Bi-SiO2 (fresh) | 3.0 | 2.14±0.01 | 2.3±0.1 | — | — | — | — |
| 1Pd5Bi-SiO2 (fresh) | 3.0 | 2.14±0.01 | 2.4±0.1 | — | — | 3.90±0.03 (BiOBi) | 1.3±0.4 |
| 1Pd2Bi-SiO2 (used) | 2.4 | 2.14±0.01 | 2.1±0.1 | 2.82±0.02 | 0.4±0.1 | 3.86±0.03 (BiOBi) | 1.1±0.4 |
| 1Pd5Bi-SiO2 (used) | 2.3 | 2.15±0.01 | 1.7±0.1 | 2.82±0.01 | 0.5±0.1 | 2.99±0.02 (metallic BiBi) 3.88±0.04 (BiOBi) | 0.6±0.2 0.9±0.4 |

a D.W. = 0.003±0.001, 0.006±0.002 Å2 for all the analyzed BiO, BiPd and BiBi shells, respectively.

Table S4. Testing conditions of Arrhenius plots (rw) for Pd/PdBi-SiO2 samples.

| 1Pd-SiO2 | 60,000 mL·gcat-1·h-1 |  | 1Pd2Bi-SiO2 | 180,000 mL·gcat-1·h-1 |  |
| --- | --- | --- | --- | --- | --- |
|  | Conv.(%) | rw(molCO·gcat-1·s-1) |  | Conv.(%) | rw(molCO·gcat-1·s-1) |
| 90°C | 3.8 | 0.3 | 90 | 9.1 | 2.1 |
| 100°C | 5.6 | 0.4 | 100 | 14.6 | 3.3 |
| 110°C | 6.3 | 0.5 | 110 | 21.3 | 4.9 |
| 1Pd5Bi-SiO2 | 178,000 mL·gcat-1·h-1 |  |  |  |  |
|  | Conv.(%) | rw(molCO·gcat-1·s-1) |  |  |  |
| 90°C | 5.4 | 1.2 |  |  |  |
| 100°C | 6.7 | 1.5 |  |  |  |
| 110°C | 9.0 | 2.0 |  |  |  |

Table S5. Temperature of 50% (T50%) and 90% (T90%) CO conversion, rates normalized by catalyst weight (r1), rates normalized by platinum or palladium amount (r2) and apparent activation energies (Ea) for the carbon monoxide oxidation reaction over Pd/PdBi-SiO2 samples.

| Sample | T50% | T90% | r1 (molCO·gcat-1·s-1) |  |  | r2 (mmolCO·molPd-1·s-1) |  |  | Ea (kJ/mol) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 90C | 100C | 110C | 90C | 100C | 110C |  |
| 1Pd-SiO2 | 150 | 170 | 0.3 | 0.4 | 0.5 | 4.0 | 5.3 | 6.6 | 603 |
| 1Pd2Bi-SiO2 | 107 | 122 | 2.1 | 3.3 | 4.9 | 27.8 | 43.7 | 64.9 | 351 |
| 1Pd5Bi-SiO2 | 124 | 139 | 1.2 | 1.5 | 2.0 | 15.9 | 19.9 | 26.5 | 401 |

Table S6. The fraction of different valence for palladium and bismuth species according to the linear combination fitting of EXAFS results.

|  | Pd2+ | Pd0 | Bi3+ | Bi0 |
| --- | --- | --- | --- | --- |
| 1Pd-SiO2 | 25% | 75% | − | − |
| 1Pd2Bi-SiO2 | 15% | 85% | 93% | 7% |
| 1Pd5Bi-SiO2 | 15% | 85% | 93% | 7% |

Table S7. Oxidation state of bismuth (δ) and Bi L3-edge EXAFS fitting results (R: distance; CN: coordination number; σ2: Debye-Waller factor a) of 1Pd1Bi-SiO2.

| sample | δ | Bi-O |  | Metallic Bi-Pd |  |
| --- | --- | --- | --- | --- | --- |
|  |  | R | CN | R | CN |
| 1Pd1Bi-fresh | 2.9 | 2.14±0.01 | 2.3±0.1 | − | − |
| 1Pd1Bi-110H2 | 2.4 | 2.14±0.01 | 1.4±0.1 | 2.82±0.02 | 0.4±0.1 |
| 1Pd1Bi-180H2 | 2.0 | 2.14±0.03 | 1.0±0.4 | 2.83±0.03 | 1.2±0.2 |
| 1Pd1Bi-180H2-used | 1.9 | 2.13±0.01 | 1.2±0.1 | 2.82±0.02 | 1.0±0.1 |

a D.W. = 0.003±0.001, 0.006±0.002 Å2 for all the analyzed BiO, BiPd shells, respectively.

Figure S1. Nitrogen adsorption measurements of Pd/PdBi-SiO2 and SiO2 samples: (a) adsorption-desorption isotherm and (b) BJH pore size distribution.

Figure S2. XRD patterns under “slow-scan” mode (scan rate: 1/min) for Pd/PdBi-SiO2 samples

Figure S3. TEM (a,c,e) and HRTEM (b,d,f) images of fresh Pd/PdBi-SiO2 samples: (a,b) 1Pd-SiO2; (c,d) 1Pd2Bi-SiO2; (e,f) 1Pd5Bi-SiO2.

Figure S4. Diameter histograms on metal oxide clusters of fresh (a) and used (b) Pd/PdBi-SiO2 samples on the basis of HAADF-STEM data.

Figure S5. The EDS elemental mapping of 1Pd-SiO2.

Figure S6. Linear combination fitting details on the Pd K edge XANES spectra of fresh (a,c,e) and used (b,d,f) PdBi-SiO2 samples: (a,b) 1Pd-SiO2, (c,d) 1Pd2Bi-SiO2, (e,f) 1Pd5Bi-SiO2.

| sample | Pd4O4 | Pd3BiO4 |
| --- | --- | --- |
| cohesive energy E (eV) | 23.65 | 24.08 |

Figure S7. The cohesive energy of P4O4 and Pd3BiO4.

Figure S8. (a) The “light off” profiles of Pd/PdBi-SiO2 catalysts with pretreatment at 300 °C under air and (b) CO oxidation of 1Pd-SiO2 with oxidative and reductive pretreatments.

Figure S9. TEM (a,c,e) and HRTEM (b,d,f) images of used PdBi-SiO2 samples: (a,b) 1Pd-SiO2; (c,d) 1Pd2Bi-SiO2; (e,f) 1Pd5Bi-SiO2.

Figure S10. Aberration-corrected HAADF-STEM images of used 1Pd-SiO2.

Figure S11. In-situ CO-TPR profiles of Pd/PdBi-SiO2 samples with pretreatment condition at 180 ºC for 30 mins in 5%H2/He.

Figure S12. In-situ CO-TPR profiles of Pd/PdBi-SiO2 samples after CO oxidation without air exposure.

Figure S13. The H2-TPR profiles of used Pd/PdBi-SiO2 at low temperature.

Figure S14. In-situ Bi L3 edge EXAFS results over PdBi-SiO2 samples at reduction temperature of 180 ºC

Figure S15. In-situ Pd K edge XAFS result over 1Pd1Bi-SiO2 at reduction temperature of 180 ºC

Figure S16. The cohesive energy of PdBi1 single atom alloy and Pd nanoparticle.

Figure S17. In-situ DRIFTS study of CO adsorption on 1Pd-SiO2 and 1Pd2Bi-SiO2 under different condition: (a,b) catalysts pretreated in situ at 300 °C under air, (c,d) catalysts at 180 °C under 5 vol.% H2/N2 flow, (e,f) after CO oxidation (CO flow rate: 30 mL min−1; catalyst mass: 20 mg; temperature: 100 °C)

Figure S18. In-situ DRIFTS study of CO adsorption on 2Bi-SiO2 with different pretreatment condition. The catalysts were pretreated in situ (a) at 300 °C under air and (b) at 180 °C under 5 vol.% H2/N2 flow in DRIFTS reaction cell before data collection (CO flow rate: 30 mL min−1; catalyst mass: 20 mg; temperature: 100 °C)

Figure S19. The total valence of palladium atom in PdBi1 single atom alloy.

Figure S20. The density of state for Pd nanoparticle and PdBi1 single atom alloy.