Supplementary Material

Photodegradation of 17α-ethinylestradiol on Ag3PO4 crystals treated at different temperatures

Luis F. G. Noletoa, Vitória E. M. Vieiraa, Francisco H. P. Lopesb, Lara K. Ribeiroc, Taisa C. M. Dantasb, Gustavo O. M. Gusmãob, Geraldo E. Luz Jr.a,b,*

a Departamento of Chemistry (DQ), Federal University of Piauí – UFPI, Teresina, PI 64049-550, Brazil

b PPGQ-GrEEnTec-DQ, State University of Piauí – UESPI, 2231 João Cabral Street, P.O. Box 381, Teresina, PI 64002-150, Brazil

c LIEC/CDMF, Departamento of Chemistry, Federal University of São Carlos, São Carlos-SP, Brazil

* Corresponding author.

Email address: geraldoeduardo@ccn.uespi.br (G. E. Luz Jr.)

Tel: +55 86 99983-9932.

Figure S1 – Schematic representation of the precipitation synthesis at room temperature of Ag3PO4.

Figure S2 – Rietveld refinement plots of the Ag3PO4 crystals obtained at room temperature (a) and thermally treated at 100 °C (b), 200 °C (c), 300 °C (d), 400 °C (e), and 500 °C (f).

Table S1 – Atomic coordinates and network parameters obtained by Rietveld refinement of the Ag3PO4 crystals at room temperature (a) and thermally treated at 100 °C (b), 200 °C (c), 300 °C (d), 400 °C (e), and 500 °C (f) comparing to ICSD card no. 14000 (g).

| Atoms | Wyckoff | Sites | X | Y | Z |
| --- | --- | --- | --- | --- | --- |
| a) Ag3PO4 (25°C) |  |  |  |  |  |
| Ag | 6d | -4.. | 0.25000 | 0.00000 | 0.50000 |
| P | 2a | 23. | 0.00000 | 0.00000 | 0.00000 |
| O | 8e | .3. | 0.14767 | 0.14767 | 0.14767 |
| Density = 6.511 g/cm3; *Rp: 17.7%; *Rwp: 16.7%; *Rexp: 10.96%; *Rbragg: 4.499%; *χ2: 2.33; *D-W(stat.): 1.0432; *D-W(esp.): 1.9443; Volume (Å)3: 217.24; Cell parameters a=b=c: 6.01151(3) Å e α=β=γ: 90 |  |  |  |  |  |
| b) Ag3PO4 (100°C) |  |  |  |  |  |
| Ag | 6d | -4.. | 0.25000 | 0.00000 | 0.50000 |
| P | 2a | 23. | 0.00000 | 0.00000 | 0.00000 |
| O | 8e | .3. | 0.14210 | 0.14210 | 0.14210 |
| Density = 6.520 g/cm3; Rp: 21.1%; Rwp: 19.1%; Rexp: 12.44%; Rbragg: 4.045%; χ2: 2.35; D-W(stat.): 0.9841; D-W(esp.): 1.9427; Volume (Å)3: 217.29; Cell parameters a=b=c: 6.0118(7) Å e α=β=γ: 90 |  |  |  |  |  |
| c) Ag3PO4 (200°C) |  |  |  |  |  |
| Ag | 6d | -4.. | 0.25000 | 0.00000 | 0.50000 |
| P | 2a | 23. | 0.00000 | 0.00000 | 0.00000 |
| O | 8e | .3. | 0.14662 | 0.14662 | 0.14662 |
| Density = 6.514 g/cm3; Rp: 17.2%; Rwp: 16.9%; Rexp: 10.90%; Rbragg: 3.246%; χ2: 2.40; D-W(stat.): 1.0369; D-W(esp.): 1.9443; Volume (Å)3: 217.25; Cell parameters a=b=c: 6.01158(3) Å e α=β=γ: 90 |  |  |  |  |  |
| d) Ag3PO4 (300°C) |  |  |  |  |  |
| Ag | 6d | -4.. | 0.25000 | 0.00000 | 0.50000 |
| P | 2a | 23. | 0.00000 | 0.00000 | 0.00000 |
| O | 8e | .3. | 0.14492 | 0.14492 | 0.14492 |
| Density = 6.409 g/cm3; Rp: 29.5%; Rwp: 23.7%; Rexp: 18.44%; Rbragg: 2.520%; χ2: 1.59; D-W(stat.): 1.3504; D-W(esp.): 1.9439; Volume (Å)3: 217.56; Cell parameters a=b=c: 6.01441(4) Å e α=β=γ: 90 |  |  |  |  |  |
| e) Ag3PO4 (400°C) |  |  |  |  |  |
| Ag | 6d | -4.. | 0.25000 | 0.00000 | 0.50000 |
| P | 2a | 23. | 0.00000 | 0.00000 | 0.00000 |
| O | 8e | .3. | 0.13989 | 0.13989 | 0.13989 |
| Density = 6.427 g/cm3; Rp: 23.3%; Rwp: 20.2%; Rexp: 13.46%; Rbragg: 3.974%; χ2: 2.25; *D-W(stat.):1.1056; D-W(esp.): 1.9439; Volume (Å)3: 217.40; Cell parameters a=b=c: 6.01294(3) Å e α=β=γ: 90 |  |  |  |  |  |
| f) Ag3PO4 (500°C) |  |  |  |  |  |
| Ag | 6d | 4.. | 0.25000 | 0.00000 | 0.50000 |
| P | 2a | 23. | 0.00000 | 0.00000 | 0.00000 |
| O | 8e | 3. | 0.15031 | 0.15031 | 0.15031 |
| Density = 6.577 g/cm3; Rp: 25.3%; Rwp: 21.7%; Rexp: 15.60%; Rbragg: 3.127%; χ2: 1.93; D-W(stat.): 1.2029; D-W(esp.): 1.9439; Volume (Å)3: 217.40; Cell parameters a=b=c: 6.01298(4) Å e α=β=γ: 90 |  |  |  |  |  |
| g) ICSD: 14000 |  |  |  |  |  |
| Ag | 6d | 4.. | 0.25000 | 0.00000 | 0.50000 |
| P | 2a | 23. | 0.00000 | 0.00000 | 0.00000 |
| O | 8e | 3. | 0.14860 | 0.14860 | 0.14860 |
| Density = 6.405 g/cm3; Volume (Å)3: 218.82; Cell parameters a=b=c: 6.026000 Å e α=β=γ: 90 |  |  |  |  |  |

*Rp = profile factor; *Rwp = weighted profile factor; *Rexp = expected weighted profile factor; *Rbraag = Bragg factor; χ2 = fit factor); *D-W(stat) = Durbin-Watsom statistical parameter and *D-W(esp) = expected Durbin-Watsom parameter.

Table S2 – Length and bond angles of [AgO4] and [PO4] clusters.

| Ag3PO4 | Bond length (Å) |  |  | Bond angles (°) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | AgO | PO | OPO |  | OAgO |  | AgOAg | AgOP |
|  |  |  |  |  | α | β |  |  |
| 25 °C | 2.373 | 1.547 | 109.5 |  | 150.23 | 150.2 | 101.72 | 116.42 |
| 100 °C | 2.373 | 1.547 | 109.5 |  | 150.23 | 150.2 | 101.72 | 116.4 |
| 200 °C | 2.373 | 1.547 | 109.5 |  | 150.23 | 150.2 | 101.72 | 116.4 |
| 300 °C | 2.374 | 1.548 | 109.47 |  | 150.23 | 150.2 | 101.72 | 116.4 |
| 400 °C | 2.374 | 1.548 | 109.5 |  | 150.23 | 150.2 | 101.72 | 116.4 |
| 500 °C | 2.374 | 1.548 | 109.5 |  | 150.23 | 150.2 | 101.72 | 116.4 |
| 14000* | 2.379 | 1.551 | 109.47 |  | 150.23 | 150.2 | 101.72 | 116.4 |

*Values obtained by ICSD card no. 14000 used in the Rietveld refinement

Figure S3 – TG (a) and DSC (b) curves of Ag3PO4 crystals.

Table S3 – Kinetic constants, correlation factor and Turnover frequency of the samples Ag3PO3 used in photodegradation of the EE2.6

| Ag3PO4 (ºC) | k a (min-1) | R b | TOF c (min-1) |
| --- | --- | --- | --- |
| 25 | 3.87x10-3 | 0.95280 | 1.62x10-4 |
| 100 | 2.66x10-3 | 0.90825 | 1.11x10-4 |
| 200 | 7.42x10-3 | 0.98479 | 3.11x10-4 |
| 300 | 5.04x10-3 | 0.99350 | 2.12x10-4 |
| 400 | 1.24x10-3 | 0.98046 | 5.19x10-5 |
| 500 | 6.64x10-3 | 0.80347 | 2.78x10-4 |

a- kinetic rate constants; b- correlation factor; c- turnover frequency

Figure S4 – EDX spectra for Ag3PO4 crystals at room temperature (a) and treated at 100 (b), 200 (c), 300 (d), 400 (e), and 500 °C (f).

Figure S5 – Particles distribution diagrams for Ag3PO4 crystals at room temperature (a) and treated at 100 (b) and 200 °C (c).

Figure S6 – Indirect band gap energy (Egap) of Ag3PO4 samples at room temperature (a) and treated at 100 °C (b), 200 °C (c), 300 °C (d), 400 °C (e), and 500 °C (f).