Table 1 Basic information about Qin Terra-Cotta Warriors painted films in Pit 2.

| No. of samples | excavation location | sample picture | sample description |
| --- | --- | --- | --- |
| a | T21G20:1 |  | The film is brown, thin, fragile, curling, cracked and covered with red paint. |
| b | K5:142 |  | The film is brown, thin, fragile, curling, cracked and covered with white paint. |
| C | K5:133 |  | The film is brown, thin, fragile, curling, cracked and covered with white paint. |
| d | K5:103 |  | The film is brown, thin, fragile, curling, cracked and covered with red paint. |
| e | T21G20:2 |  | The film is brown, thin, fragile, curling, cracked and covered with red paint. |
| f | K5:67 |  | The film is brown, thin, fragile, curling, cracked and covered with red paint. |

Table 2 The surface of the painted films observed under the ultra-depth-of-field microscope

| No. of samples | the surface of the films | the surface of the pigments |
| --- | --- | --- |
| a |  |  |
| b |  |  |
| C |  |  |
| d |  |  |
| e |  |  |
| f |  |  |

Table 3 Thickness and layers of the painted films

| No. of samples | Analytical results |
| --- | --- |
| a | Two layers. The red layer is 10.1um thick on average. The black layer is 20.6um thick on average. |
| b | Two layers. The white layer is 10.5um thick on average. The Black layer is 19.4um thick on average. |
| c | Two layers. The white layer is 10.3um thick on average. The black layer is 20.3um thick on average. |
| d | Two layers. The red layer is 9.6um thick on average. The black layer is 21.5um thick on average. |
| e | Two layers. The red layer is 9.9um thick on average. The black layer is 18.5um thick on average. |
| f | Two layers. The red layer is 10.0um thick on average. The black layer is 22.5um thick on average. |

Table 4 Main infrared absorption bands of painted films unearthed in Pit No. 2

Wavenumber（cm-1）; Assignment; Wavenumber（cm-1）; Assignment. 3442; v(O-H); 1250; vas（Ar-O-R）, v（Ar-OH）. 2929,2851; vas(CH2),v（CH2）; 1037; vas（Si-O-Si）. 1635; v(C=C）,δ( O-H ); 790,; γH （Ar1,2,4）, v（Si-O-Si）. 1556,1400; vas(COO),v（COO）; 779; γH（Ar1,2,3）, v（Si-O-Si）. Table 5 Table 5 Main infrared absorption bands of films in raw lacquer. Wavenumber（cm-1）; Assignment; Wavenumber（cm-1）; Assignment. 3460; v(O-H); 1500~1100; δ（O-H）,β（O-H）, V（ C-O）. 3017; v（C=H）; 994; γ(RHC=CH2）. 2927，2853; vas(CH2)，v（CH2）; 778、734; γH（Ar1,2,3）. 1610~1370; v（C=C）of benzene ring; 803; γH（ Ar 1,2,4）. 1475; δCH2; 863,831,734; γH（Ar1,3,5）..