Environmental Monitoring and Assessment

# Synthesis and characterization of g-C3N4 modified zeolite and its application as a methyl violet 6b cationic dye sorbent

# Somayeh Karimi and Mohammad Saraji*

# *Corresponding Author

# Mohammad Saraji, Department of Chemistry, Isfahan University of Technology, Isfahan 84156-83111, Iran.

# Email: saraji@iut.ac.ir, msaraji@ymail.com

Fig. 1 g-C3N4 structure

Fig. 2 Methyl violet 6b structure

Fig. 3 FT-IR spectrums from g-C3N4 and ZFG

Fig. 4 X-ray pattern of ZFG

Fig. 5 Elemental mapping from ZFG

Fig. 6  Freundlich (a) and Langmuir (b) isotherm plot

Fig. 7 Standard addition diagrams for real sample of MV (a) municipal wastewater (b) pesticide production (c) wastewater of paint factory and (d) textile industries

Table 1 The CCD matrix and corresponding removal efficiency of MV

| Run | A:pH | B:amount of adsorbent (g) | C:time(min) | D:concetratio(mg L-1) | Removal efficiency (R%) |
| --- | --- | --- | --- | --- | --- |
| 1 | 5 | 0.085 | 23 | 83 | 80.8 |
| 2 | 9 | 0.085 | 9 | 83 | 73.2 |
| 3 | 9 | 0.085 | 23 | 229 | 50.3 |
| 4 | 9 | 0.035 | 23 | 229 | 25.3 |
| 5 | 9 | 0.085 | 23 | 83 | 77.9 |
| 6 | 7 | 0.06 | 16 | 156 | 40.0 |
| 7 | 7 | 0.06 | 16 | 156 | 41.8 |
| 8 | 5 | 0.035 | 23 | 229 | 25.9 |
| 9 | 7 | 0.06 | 16 | 156 | 42.0 |
| 10 | 7 | 0.01 | 16 | 156 | 5.9 |
| 11 | 7 | 0.11 | 16 | 156 | 67.8 |
| 12 | 7 | 0.06 | 16 | 10 | 87.9 |
| 13 | 3 | 0.06 | 16 | 156 | 45.5 |
| 14 | 5 | 0.035 | 9 | 83 | 54.3 |
| 15 | 7 | 0.06 | 2 | 156 | 47.2 |
| 16 | 5 | 0.085 | 9 | 229 | 52.4 |
| 17 | 7 | 0.06 | 16 | 156 | 43.0 |
| 18 | 11 | 0.06 | 16 | 156 | 64.6 |
| 19 | 9 | 0.085 | 9 | 229 | 58.8 |
| 20 | 5 | 0.035 | 9 | 229 | 26.9 |
| 21 | 5 | 0.085 | 23 | 229 | 59.8 |
| 22 | 7 | 0.06 | 16 | 156 | 51.3 |
| 23 | 9 | 0.035 | 23 | 83 | 40.5 |
| 24 | 9 | 0.035 | 9 | 229 | 34.1 |
| 25 | 7 | 0.06 | 30 | 156 | 56.2 |
| 26 | 5 | 0.085 | 9 | 83 | 78.9 |
| 27 | 7 | 0.06 | 16 | 302 | 59.0 |
| 28 | 5 | 0.035 | 23 | 83 | 40.4 |
| 29 | 7 | 0.06 | 16 | 156 | 40.5 |
| 30 | 9 | 0.035 | 9 | 83 | 58.5 |

Table 2 Coded levels and experimental values of independent variables in central composite design

| variables | unite | Symbols | -α | -1 | 0 | +1 | +α |
| --- | --- | --- | --- | --- | --- | --- | --- |
| pH |  | A | 3 | 5 | 7 | 9 | 11 |
| Amount of adsorbent | mg | B | 10 | 35 | 60 | 85 | 1.1 |
| Contact time | min | C | 2 | 9 | 16 | 23 | 30 |
| Concentration of dye | mg L-1 | D | 10 | 83 | 156 | 229 | 302 |

Table 3 ANOVA for Quadratic model

| Source | Sum of squares | df | Mean square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 9442.18 | 8 | 1180.27 | 43.90 | < 0.0001 | Significant |
| A-pH | 58.36 | 1 | 58.36 | 2.17 | 0.1555 |  |
| B-adsorbent | 5107.90 | 1 | 5107.90 | 190.01 | < 0.0001 |  |
| C-time | 8.46 | 1 | 8.46 | 0.3147 | 0.5807 |  |
| D-concentration | 2963.72 | 1 | 2963.72 | 110.25 | < 0.0001 |  |
| BC | 139.40 | 1 | 139.40 | 5.19 | 0.0334 |  |
| A² | 317.28 | 1 | 317.28 | 11.80 | 0.0025 |  |
| C² | 208.78 | 1 | 208.78 | 7.77 | 0.0111 |  |
| D² | 875.23 | 1 | 875.23 | 32.56 | < 0.0001 |  |
| Residual | 564.53 | 21 | 26.88 |  |  |  |
| Lack of Fit | 523.24 | 16 | 32.70 | 3.96 | 0.0677 | not significant |
| Pure Error | 41.30 | 5 | 8.26 |  |  |  |
| Cor Total | 10006.72 | 29 |  |  |  |  |

Table 4 Statically parameters of model

| Std. Dev | 5.18 | R2 | 0.9436 |
| --- | --- | --- | --- |
| Mean | 51.34 | Adjusted R2 | 0.9221 |
| C.V. % | 10.30 | Predicted R2 | 0.8331 |
|  |  | Adeq precision | 25.97 |

Table 5 Comparison of experimental final result and predicted value by the model

| Analyte | Methyl violet 6b |
| --- | --- |
| Dye concentration (mg L-1) | 28.0 |
| Adsorbent amount (mg) | 10.0 |
| Contact time (min) | 2.0 |
| Predicted removal percentage | 89.0 |
| Experimental removal percentage | 86.0 ±2.8 |