Supplementary Information

Dissolved-Cl2 Triggered Redox Reaction Enables High-performance Perovskite Solar Cells

Yujie Luo1,2, Kaikai Liu1,2, Liu Yang1, Wenjing Feng,1 Lingfang Zheng,1 Lina Shen,1 Yongbin Jin,1 Zheng Fang,1 Peiquan Song,1 Wanjia Tian,1 Peng Xu,1 Yuqing Li,1 Chengbo Tian1, Liqaing Xie1,* & Zhanhua Wei1,*

1 Xiamen Key Laboratory of Optoelectronic Materials and Advanced Manufacturing, Institute of Luminescent Materials and Information Displays, College of Materials Science and Engineering, Huaqiao University, Xiamen 361021, P.R. China

2 These authors contributed equally to this work.

E-mails: lqxie@hqu.edu.cn; weizhanhua@hqu.edu.cn

Supplementary Fig. 1 | Test of CO2 in Cl2-CF using saturated barium hydroxide aqueous solution. When Ba(OH)2 was added into Cl2-CF and CF, a white precipitate of barium carbonate (BaCO3) was generated in Cl2-CF. In contrast, no obvious change was observed in CF.

Supplementary Fig. 2 | Test of Cl- in Cl2-CF using silver nitrate aqueous solution. When silver nitrate was added to Cl2-CF, it became turbid immediately.

Supplementary Fig. 3 | Moistened starch potassium iodide test paper was placed above the Cl2-CF solvent and turned blue, proving the existence of Cl2 in Cl2-CF.

Supplementary Fig. 4 | Photographs of perovskite precursor compounds dissolved in CF and Cl2-CF.

Supplementary Fig.5 | UV-vis absorption spectra of (a) PbI2 and (b) MAI dissolved in CF and Cl2-CF.

Supplementary Fig. 6 | UV-vis spectra of (a) MABr and (b) HABr dissolved in CF and Cl2-CF.

Supplementary Fig. 7 | UV-vis spectra of MACl dissolved in CF and Cl2-CF.

Supplementary Fig. 8 | SEM images for (a) PVSK, (b) PVSK-CF, and (c) PVSK-Cl2-CF. 2D AFM images of (d) PVSK, (e) PVSK-CF, and (f) PVSK-Cl2-CF. The scan area of the AFM images is 5 × 5 μm2. 3D AFM images of (g) PVSK, (h) PVSK-CF, and (i) PVSK-Cl2-CF. The scan area of the 3D images is 5 × 5 μm2.

Supplementary Fig. 9 | XRD patterns of PVSK, PVSK-CF, and PVSK-Cl2-CF. (a) 12° to 15°, (b) 12.2° to 13.0°, (c) 5° to 40°.

Supplementary Fig. 10 | SEM images of the bottom surface of (a) PVSK, (b) PVSK-CF, and (c) PVSK-Cl2-CF.

Supplementary Fig. 11 | SEM images for (a) PVSK, (b) PVSK-HABr/CF, and (c) PVSK-HABr/Cl2-CF. 2D AFM images of (d) PVSK, (e) PVSK-HABr/CF, and (f) PVSK-HABr/Cl2-CF (scan area: 5 × 5 μm2). 3D AFM images of (g) PVSK, (h) PVSK-HABr/CF, and (i) PVSK-HABr/Cl2-CF (scan area: 5 × 5 μm2).

Supplementary Fig. 12 | XRD patterns of PVSK, PVSK-HABr/CF, and PVSK-HABr/Cl2-CF and HA2FAPb2Br2I5.

Supplementary Fig. 13 | Azimuthally integrated scattering of grazing-incidence wide-angle X-ray scattering (GIWAXS) characterization.

Supplementary Fig. 14 | XPS for (a) Cl 2p and (b) Pb 4f spectra of PVSK, PVSK-HABr/CF, and PVSK-HABr/Cl2-CF.

Supplementary Fig. 15 | Tuac plot of (a) PVSK, (b) PVSK-HABr/CF, and (c) PVSK-HABr/Cl2-CF.

Supplementary Fig. 16 | Schematic illustration of the perovskite films for (a) PVSK, (b) PVSK-HABr/CF, and (c) PVSK-HABr/Cl2-CF.

Supplementary Fig. 17 | Cross-sectional SEM images of the (a) PVSK, (b) PVSK-HABr/CF, and (c) PVSK-HABr/Cl2-CF based devices.

Supplementary Fig. 18 | Statistics of (a) FF, and (b) JSC of the devices based on PVSK, PVSK-HABr/CF, and PVSK-HABr/Cl2-CF.

Supplementary Fig. 19 | IPCE spectra and the integrated JSC of the PVSK, PVSK-HABr/CF, and PVSK-HABr/Cl2-CF based perovskite device. (a) 300 to 900 nm, (b) 770 to 830 nm.

Supplementary Fig. 20 | J-V curves and hysteresis of the (a) PVSK, (b) PVSK-HABr/CF, and (c) PVSK-HABr/Cl2-CF based devices.

Supplementary Fig. 21 | Steady-state power output at the maximum power point of PVSK, PVSK-HABr/CF, and PVSK-HABr/Cl2-CF based devices.

Supplementary Table S1 | Fitted parameters of TRPL results of PVSK, PVSK-HABr/CF, and PVSK-HABr/ Cl2-CF perovskite film.

|  | 𝜏1 (ns) | 𝜏2 (ns) | A1 | A2 | 𝜏avg (ns) |
| --- | --- | --- | --- | --- | --- |
| PVSK | 188.8 | 901.3 | 498.7 | 1009.7 | 834.6 |
| PVSK-HABr/CF | 389.6 | 1176.8 | 377.9 | 880.0 | 1078.9 |
| PVSK-HABr/Cl2-CF | 342.8 | 1712.4 | 238.2 | 913.8 | 1644.5 |