Table I: Summary of works reporting cathodic electrodeposition potentiostatic-DC of cadmium chalogenide

| Electrolyte | Deposition conditions | substrate | Important findings | Ref. |
| --- | --- | --- | --- | --- |
| Acidic aqueous solution of CdSO4 and SeO2 |  | Titanium | - Polycrystalline films - Jsc = 7–10 mA·cm-2 Voc =450–500 mV | Hodes 1976 [12] |
| Aqueous complexing agent EDTA | Ed: -1.1 to -1.2V vs SCE | Au, Ti and Cd | - N–type - Photoresponse in white light (as deposited) Voc= 0.1–0.55 V Jsc= 0.25–3.1 mA·cm-2 | Kazacos 1980 [13] |
| Acquous electrolyte CdSO4, H2SO4 pH=2 | Ed: 0.4V to -0.7V | Au or Cu | - Polycrystalline CdSe of hexagonal structure - Homogeneous films and well adhered to the substrate | Kowalik 2016 [15] |
| Acqueous electrolyte: CdCl2, H2SeO3 | Ed: 1.2 V Two electrode system Td:40 min | Conducting glass | - N-type, polycrystalline deposits - Suitable for infrared detectors - Grain size: 300–750 nm - Gap: 2.1 eV –1.8 eV | Chowdhury 2011 [16] |
| non-acqueous bath |  | Stainless steel, Ti, FTO | - N-type polycrystalline, hexagonal phase - CdSe/FTO give better PV performance Jsc= 0.85 mA·cm-2 Voc = 356 mV Efficiency: 0.297% | Gudage 2007 [18] |
| Acqueous solution/salt additive: monosodium L-glutamate or choline chloride pH= 2.2 | Ed: -0.9V to -1.1V | Ti | - Better crystallized deposits after salt additive addition - The addition of monosodium L- glutamate improve the photoresponse of deposits Jsc: 3.738 mA·cm-2, 4.9 mA·cm-2 Voc: -426 mV, -291 mV FF: 0.41, 0.34 Efficiency: 0.29, 0.507 | Hamilikas 2015 [19] |
| Ionic liquid Reline | Ed: -0.6 V to -0.8V vs Pt pseudo reference | Conducting glass | - N-type CdS, CdSe and ZnS were deposited | Dale et al.(2007) [24] |