Effect of lignin and released acid on the gelation and aerogel fabrication of whole biomass in the lithium bromide molten salt hydrate system

Xu Guoa, Xinyu Caoa, Tianyuan Xiaoa,c, Minjie Houa, Changgeng Lia, Xueru Shenga, Yanzhu Guoa, Yanning Suna, Pedram Fatehib, Haiqiang Shia*

aLiaoning Key Lab of Lignocellulose chemistry and Biomaterialsbo, Liaoning Collaborative Innovation Center for Lignocellulosic Biorefinery, College of Light Industry and Chemical Engineering, Dalian Polytechnic University, Dalian, Liaoning 116034, China

bBiorefining Research Institute, Lakehead University, Thunder Bay, ON, Canada, P7B5E1

cCollege of Light Industry and Textile, Qiqihar University, Qiqihar 161000, People’s Republic of China

*Corresponding author. Liaoning Key Laboratory of Pulp and Paper Engineering, Dalian Polytechnic University, Dalian, 116034, China.

Tel.: +86 411 86332216; fax: +86 411 86323736

Email address: shihq@dlpu.edu.cn

1.1. Composition analysis

The organic components of the samples were determined according to the NREL method. A 0.3 g (od) sample was added to a pressure-resistant flask containing 3 mL of 72% sulfuric acid, which was then reacted at room temperature for 2h, and at 121°C for 1h following the addition of 84 mL of deionized water. After the reaction completion, it was filtered and the filtrate was used for the quantification of monosaccharides, organic acids, and acid-soluble lignin, and the solid fraction was used for the quantification of Klason lignin.

Monosaccharides were determined by high-performance liquid chromatography (HPLC) (Waters e2695, USA). The hydrolysate sample of 50 μL was filtered and degassed before injecting to the HPLC HPX 87H column. Sulfuric acid of 0.005 M was used as the mobile phase at a flow rate of 0.6 mL/min. Other HPLC conditions were the column and detector temperature of 60 °C, and elution time of 50 min. The average of duplicate tests was reported.

The acid-insoluble lignin was determined directly by the gravimetric method, while the acid-soluble lignin was determined spectrophotometrically. In brief, the absorbance of the hydrolysate at 205 nm was measured using a UV spectrophotometer (Cary300, VARIAN) to determine acid-soluble lignin. The hydrolysate was carefully diluted to ensure the value of absorbance fell in the range of 0.2–0.7. The acid-soluble lignin in the hydrolysate was calculated according to the Lambert-Beer law (A =εbc) and considering absorptivity (ε) to be 110 L/g/cm.

1.2. Determination of the degree of polymerization

1.2.1. Determination of the average degree of polymerization of lignin-free samples

The DP of lignin-free samples was estimated by the capillary viscometer method following GB/T 1548-2016 standard method. The lignin-free samples (0.25 g) were homogeneously dispersed in 25 mL of deionized water and subsequently dissolved in 50 mL of 0.5 M copper ethylenediamine (CED) for 10 min. The relative viscosity of the solution was measured using a Cannon-Fenske capillary viscometer at 25°C to provide the corresponding characteristic viscosity ([η] mL g-1). DP values were obtained from Eq. (1).

DP0.905=0.75[η]	(1)

where the constants of 0.905 and 0.75 were derived from empirical values for the cellulose-CED system.

1.2.2. Determination of the degree of polymerization of lignin-free aerogels

The lignin-free aerogels were ground with a ball mill at 1200 rpm for 5h so that they could be dispersed in water uniformly. Then, the average degree of polymerization was determined according to the procedure in 1.2.1.

1.2.3. Determination of the average degree of polymerization of carbohydrates in ungelatinized solutions

Ethanol was added (at 10/1 ethanol/solution ratio) to the ungelled solution of lignin-free samples and stirred with an electromagnetic stirrer at 350 rpm for 10 min. After stirring, the precipitated insoluble material was separated by centrifugation using a low-speed centrifuge (4000 rpm for 10 min). The insoluble material was then dried using a freeze dryer for 24 h. The average degree of polymerization of the dried carbohydrates was then determined using the procedure in 1.2.1.

1.3 Characterization of aerogels

1.3.1. Scanning electron microscope (SEM)

The internal network structure of the aerogel was observed using a scanning electron microscope (JSM-7800F) at the accelerating voltage of 20 kV. The aerogels were manually cross-sectioned and sliced, and the surface of aerogels was coated with a gold prior to analysis.

1.3.2. Pore structure and specific surface area analysis

The specific surface area of aerogels was determined under N2 adsorption conditions using a specific surface area and porosity analyzer (2020 PLUS HD88) at 170°C for 0.2 g of aerogel for 4 h.

1.3.3. Thermal gravimetric (TG) analysis

Approximately, 8 mg of aerogels were used for analyzing their thermal stability with a thermogravimetric analyzer (TGA Q500, TA). The test was carried out under nitrogen protection and a heating rate of 10°C/min to the temperature of 700°C.

1.3.4. Mechanical performance analysis

Mechanical performance of aerogels was assessed at room temperature using a universal testing machine (Instron 5965) following GB/T528-2009 standard method. The aerogel specimens were cut into a dumbbell shape and stretched at a rate of 20 mm/min until fracture to obtain tensile strength (Ts) and elastic modulus (E). Three sets of data were measured in parallel for each sample, and the results were averaged.