Tunable Full-color Room Temperature Phosphorescence of Two Single-Component Zinc(II) Complexes

Ying Mu1,3, Zhong-Xin Liu1,3, Xiao-Yu Fang2, Song-De Han1, Jie Pan1, Qi Wei1, Jin-Hua Li1*, and Guo-Ming Wang1*

1College of Chemistry and Chemical Engineering, Qingdao University, Shandong 266071, P. R. China

2College of Chemistry, Beijing Normal University, Beijing Key Laboratory of Energy Conversion and Storage Mate-rials, Beijing 100875, P. R. China

3These authors contributed equally: Ying Mu, Zhong-Xin Liu

*E-mail: jinhuali1978@163.com; gmwang_pub@163.com

Supplement Figure S1 The as-synthesized and simulated PXRD of QDU-21a and QDU-21b.

Supplement Figure S2 TGA curves of QDU-21a and QDU-21b.

Supplement Figure S3 Lifetime profiles of phosphorescence of QDU-21a monitored at wavelengths as indicated.

Supplement Figure S4 Lifetime profiles of phosphorescence of QDU-21b monitored at wavelengths as indicated.

Supplement Figure S5 Normalized phosphorescence excitation spectra of QDU-21a with emission at displayed wavelengths.

Supplement Figure S6 Photoluminescence emission spectra of tib in DMF solution with excitation at displayed wavelengths at 77 K.

Supplement Figure S7 Distances between n electron donors and tib moieties in compound QDU-21b.

Supplement Figure S8 Calculated HOMOs and LUMOs for QDU-21a.

Supplement Figure S9 Calculated HOMOs and LUMOs for QDU-21b.

Supplement Table S1. Crystallographic data for compounds QDU-21a and QDU-21b.

|  | QDU-21a | QDU-21b |
| --- | --- | --- |
| Formula | C16H13Br3N6O2Zn2 | C17H15Br3N6O2Zn2 |
| Fw | 691.79 | 705.82 |
| Crystal system | Triclinic | Triclinic |
| Space group | P-1 | P-1 |
| a/Å | 7.6363(8) | 9.3988(9) |
| b/Å | 9.6704(9) | 11.2030(10) |
| c/Å | 16.0119(14) | 11.4722(12) |
| α/° | 80.428(8) | 105.503(9) |
| β/° | 78.318(9) | 102.950(9) |
| γ/° | 67.690(10) | 91.019(7) |
| V/Å3 | 1066.02(19) | 1130.5(2) |
| Z | 2 | 2 |
| Dcalcd/g·cm-3 | 2.155 | 2.073 |
| (Mo-Kα)/mm-1 | 7.898 | 7.449 |
| F (000) | 664 | 680 |
| total reflns | 5681 | 5807 |
| unique reflns | 3758 | 3992 |
| Rint | 0.0390 | 0.0339 |
| Final R indices [I>2σ(I)] | R1 = 0.0659 wR2 = 0.1894 | R1 = 0.0436 wR2 = 0.0784 |
| R1, wR2 (all data) | R1 = 0.1022 wR2 = 0.2139 | R1 = 0.0752 wR2 = 0.0895 |
| GOF on F2 | 1.116 | 1.008 |

Supplement Table S2. Selected bond lengths (Å) and angles (o) for QDU-21a.

| Br(1)-Zn(1) Br(2)-Zn(2) Br(3)-Zn(2) N(1)-Zn(1) N(3)-Zn(2)#1 C(16)-O(1)-Zn(2) C(16)-O(2)-Zn(1) O(2)-Zn(1)-N(1) O(2)-Zn(1)-N(5)#2 N(1)-Zn(1)-N(5)#2 O(2)-Zn(1)-Br(1) N(1)-Zn(1)-Br(1) | 2.3825(15) 2.3558(19) 2.397(2) 1.995(8) 2.001(9) 125.7(7) 119.4(8) 113.4(3) 101.8(3) 113.4(3) 112.2(2) 105.0(2) | N(5)-Zn(1)#2 O(1)-Zn(2) O(2)-Zn(1) C(16)-O(2) C(16)-O(1) N(5)#2-Zn(1)-Br(1) N(3)#1-Zn(2)-O(1) N(3)#1-Zn(2)-Br(2) O(1)-Zn(2)-Br(2) N(3)#1-Zn(2)-Br(3) O(1)-Zn(2)-Br(3) Br(2)-Zn(2)-Br(3) | 1.996(8) 2.004(7) 1.971(7) 1.219(13) 1.237(14) 111.3(3) 103.2(3) 114.1(3) 105.8(3) 110.2(3) 111.0(2) 112.13(7) |
| --- | --- | --- | --- |

Symmetry transformations used to generate equivalent atoms: #1: -x+2, -y+1, -z; #2: -x+1, -y+1, -z+1.

Supplement Table S3. Selected bond lengths (Å) and angles (o) for QDU-21b.

| N(6)-Zn(2)#2 Zn(1)-O(2) Zn(1)-N(1) Zn(1)-Br(1) Br(3)-Zn(2) O(2)-Zn(1)-N(4)#1 O(2)-Zn(1)-N(1) N(4)#1-Zn(1)-N(1) O(2)-Zn(1)-Br(1) N(4)#1-Zn(1)-Br(1) N(1)-Zn(1)-Br(1) O(1)-Zn(2)-N(6)#3 | 2.012(5) 1.963(4) 2.038(5) 2.3427(11) 2.3941(9) 106.2(2) 93.69(18) 115.20(19) 118.98(14) 113.27(15) 108.25(15) 102.6(2) | Zn(2)-O(1) Zn(2)-Br(2) O(2)-C(16) O(1)-C(16) O(1)-Zn(2)-Br(2) N(6)#3-Zn(2)-Br(2) O(1)-Zn(2)-Br(3) N(6)#3-Zn(2)-Br(3) Br(2)-Zn(2)-Br(3) C(16)-O(2)-Zn(1) C(16)-O(1)-Zn(2) | 1.974(4) 2.3412(12) 1.260(7) 1.233(7) 106.83(14) 110.87(15) 112.66(12) 106.59(15) 116.45(4) 124.9(4) 139.8(4) |
| --- | --- | --- | --- |

Symmetry transformations used to generate equivalent atoms: #1: -x+2, -y, -z+2; #2: x-1, y-1, z-1; #3: x+1, y+1, z+1.

Supplement Table S4 Quantum efficiencies of QDU-21a and QDU-21b with different excitation wavelengths in crystalline powder under ambient conditions.

| Wavelength (nm) | QE (%) |  |
| --- | --- | --- |
|  | QDU-21a | QDU-21b |
| 280 | 6.9 | 5.5 |
| 300 | 4.7 | 4.1 |
| 320 | 11.3 | 8.9 |
| 340 | 13.8 | 10.1 |
| 360 | 12.5 | 10.9 |

Supplement Table S5 Phosphorescence lifetimes of QDU-21b crystalline powder under ambient conditions*.

| Wavelength (nm) | τ1 (ms) | A1 (%) | τ2 (ms) | A2 (%) | τ3 (ms) | A3 (%) | <τ> (ms) | χ² |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 280-490 | 4.2 | 28 | 15 | 36 | 58 | 36 | 27.4 | 1.30 |
| 310-510 | 3.6 | 19 | 18.6 | 46 | 71.2 | 35 | 34.2 | 1.29 |
| 340-525 | 4.3 | 12 | 19.4 | 37 | 63.7 | 51 | 40.3 | 1.29 |
| 370-540 | 4.1 | 18 | 19.1 | 44 | 72.6 | 38 | 36.5 | 1.29 |
| 400-555 | 5.3 | 24 | 21.3 | 44 | 80.7 | 32 | 30.5 | 1.27 |
| 430-570 | 6.0 | 40 | 39.6 | 60 |  |  | 26.1 | 1.18 |
| 460-590 | 1.6 | 36 | 17.1 | 64 |  |  | 11.5 | 1.25 |

*Determined from the fitting function of I(t) = A1e‐t/τ1+ A2e‐t/τ2+ A3e‐t/τ3 according to the phosphorescence decay curves.

Supplement Table S6 Distance (Å) between ring centroids in the two compounds.

| QDU-21a |  | QDU-21b |  |
| --- | --- | --- | --- |
| Cg(1) - Cg(2) #1 Cg(1) - Cg(3) #2 Cg(2) - Cg(2) #3 Cg(2)- Cg(2) #4 Cg(2) - Cg(4) #3 Cg(3) - Cg(1) #5 Cg(3) - Cg(3) #6 Cg(3) - Cg(4) #5 Cg(4) - Cg(1) #5 Cg(4) - Cg(2) #3 Cg(4) - Cg(3) #2 | 5.314(6) 4.175(6) 4.305(8) 5.496(8) 5.258(7) 4.174(6) 4.073(6) 5.976(6) 4.960(6) 5.257(7) 5.977(6) | Cg(1) - Cg(1) #1* Cg(1) - Cg(3) #2* Cg(1) - Cg(4) #1* Cg(2) - Cg(2) #3* Cg(2) - Cg(3) #4* Cg(3) - Cg(1) #2* Cg(3) - Cg(2) #4* Cg(3) - Cg(4) #2* Cg(4) - Cg(1) #1* Cg(4) - Cg(3) #2* Cg(4) - Cg(4) #2* | 3.685(4) 4.445(3) 4.922(3) 5.136(4) 4.902(3) 4.445(3) 4.903(3) 4.424(3) 4.922(3) 4.424(3) 5.740(3) |

Symmetry transformations used to generate equivalent rings: #1: 2-x, 1-y, -z; #2: 1+x, y, z; #3: 1-x, 1-y, -z; #4: 2-x, -y, -z; #5: -1+x, y, z; #6: 1-x, -y, 1-z; #1*: 1-x, -y, 2-z; #2*: 1-x, -y, 1-z; #3*: 2-x, -1-y, 1-z; #4*: 1-x, -1-y, 1-z.