Efficient adsorption of methyl orange and methylene blue dyes by a novel carbazole-based hyper-crosslinked porous polymer

Yan Hea*, Zhulei Guoa, Mingfan Chen a, Sicheng Wan a, Nan Peng a, Xiaolei Fua, Dingzhong Yuana, Bing Naa

a Jiangxi Province Key Laboratory of Polymer Micro/Nano Manufacturing and Devices, School of Chemistry, Biology and Materials Science, East China University of Technology, Nanchang, 330013, China.

1.Figures:

Fig. S1 the TEM image of porous polymer HCP-CP

Fig. S2 (a)XRD of HCP-CP, TG curve of HCP-CP (b)

Fig. S3 Langmuir(a) and Freundlich(b) isotherms of MO and MB adsorption by HCP-CP

Fig. S4 The selectivity of HCP-CP at different dyes concertation

Fig. S5 The maximum adsorption capacity of different dyes by the polymer HCP-CP

2.Tables:

Table S1 The property of porosity of microporous HCP-CP

| Polymer | SABETa (m2 g-1) | SALb (m2 g-1) | Vtc (cm3 g-1)c | Vmd (cm3 g-1)c | %Vm/Vt |
| --- | --- | --- | --- | --- | --- |
| HCP-CP | 486.7 | 491.8 | 0.323 | 0.183 | 57 |

Table S2 The parameters of pseudo-first-order kinetic models and pseudo-second-order kinetic models

| kinetic parameter | pseudo-first-order kinetic models |  |  | pseudo-second-order kinetic models |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| MO | k1/(min-1) | qe(mg/g) | R2 | k2/(g·mg-1·min-1) | qe(mg/g) | R2 |
|  | 0.03243 | 93.57 | 0.975 | 0.00142 | 96.15 | 0.999 |
| MB | 0.02346 | 185.68 | 0.813 | 0.00062 | 192.31 | 0.998 |

Table S3 The parameters of isotherm adsorption Langmuir and Freundlich model

| Dyes | Temperature | qe,exp (mg·g-1) | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | qm (mg·g-1) | KL | R2 | KF | n | R2 |
| MB | 25℃ | 751.88 | 731.76 | 0.059 | 0.996 | 149.24 | 3.66 | 0.966 |
|  | 35℃ | 787.41 | 771.38 | 0.093 | 0.998 | 204.09 | 4.32 | 0.938 |
|  | 45℃ | 884.96 | 868.54 | 0.099 | 0.998 | 206.81 | 3.89 | 0.953 |
| MO | 25℃ | 274.73 | 253.79 | 0.036 | 0.998 | 52.79 | 3.57 | 0.971 |
|  | 35℃ | 303.03 | 276.52 | 0.033 | 0.994 | 56.77 | 3.64 | 0.968 |
|  | 45℃ | 349.65 | 315.91 | 0.033 | 0.995 | 59.56 | 3.35 | 0.917 |