Hydrogen storage and sensing ability of group 8B transition metal−doped B12N12 nanocages: A DFT investigation

Wandee Rakrai a, Chanukorn Tabtimsai a, Chatthai Kaewtong b, Sopis Chuekachang c, Somchai Keawwangchai d, Tasawan Keawwangchai d, Banchob Wanno b,d,*

a Computational Chemistry Center for Nanotechnology and Department of Chemistry, Faculty of Science and Technology, Rajabhat Maha Sarakham University, Maha Sarakham, 44000, Thailand

b Multidisciplinary Research Unit of Pure and Applied Chemistry, Department of Chemistry and Center of Excellence for Innovation in Chemistry, Faculty of Science, Mahasarakham University, Maha Sarakham, 44150, Thailand

c Department of Science and Mathematics, Faculty of Industry and Technology, Rajamangala University of Technology Isan, Sakon Nakhon Campus, Sakon Nakhon, 47160 Thailand

d Supramolecular Chemistry Research Unit, Faculty of Science, Mahasarakham University, Maha Sarakham 44150, Thailand

Table S1

The selected geometrical parameters of pristine and TM−doped B12N12.

| Species | Bond a | Bond lengths b | Bond a | Bond angles c |
| --- | --- | --- | --- | --- |
| B12N12 | B3─N1 | 1.509 | N1─B3─N2 | 95.7 |
|  | B3─N2 | 1.509 | N2─ B3─N3 | 124.4 |
|  | B3─N3 | 1.433 | N3─ B3─N1 | 124.4 |
| FeB11N12 | TM─N1 | 1.893 | N1─TM─N2 | 76.7 |
|  | TM─N2 | 1.893 | N2─TM─N3 | 103.9 |
|  | TM─N3 | 1.834 | N3─TM─N1 | 103.9 |
| CoB11N12 | TM─N1 | 1.868 | N1─TM─N2 | 77.0 |
|  | TM─N2 | 1.868 | N2─TM─N3 | 103.7 |
|  | TM─N3 | 1.817 | N3─TM─N1 | 103.7 |
| NiB11N12 | TM─N1 | 1.972 | N1─TM─N2 | 71.8 |
|  | TM─N2 | 1.972 | N2─TM─N3 | 105.9 |
|  | TM─N3 | 1.906 | N3─TM─N1 | 105.9 |
| RuB11N12 | TM─N1 | 2.034 | N1─TM─N2 | 71.1 |
|  | TM─N2 | 2.024 | N2─TM─N3 | 96.5 |
|  | TM─N3 | 1.925 | N3─TM─N1 | 96.4 |
| RhB11N12 | TM─N1 | 2.015 | N1─TM─N2 | 71.1 |
|  | TM─N2 | 2.015 | N2─TM─N3 | 98.2 |
|  | TM─N3 | 1.964 | N3─TM─N1 | 98.2 |
| PdB11N12 | TM─N1 | 2.054 | N1─TM─N2 | 69.6 |
|  | TM─N2 | 2.054 | N2─TM─N3 | 102.6 |
|  | TM─N3 | 2.110 | N3─TM─N1 | 102.6 |
| OsB11N12 | TM─N1 | 2.032 | N1─TM─N2 | 70.2 |
|  | TM─N2 | 2.033 | N2─TM─N3 | 98.4 |
|  | TM─N3 | 1.928 | N3─TM─N1 | 98.4 |
| IrB11N12 | TM─N1 | 2.025 | N1─TM─N2 | 70.2 |
|  | TM─N2 | 2.025 | N2─TM─N3 | 100.1 |
|  | TM─N3 | 1.958 | N3─TM─N1 | 100.1 |
| PtB11N12 | TM─N1 | 2.056 | N1─TM─N2 | 69.3 |
|  | TM─N2 | 2.056 | N2─TM─N3 | 105.0 |
|  | TM─N3 | 2.076 | N3─TM─N1 | 105.0 |

a N1, N2, and N3 are atoms on the B12N12 which are deﬁned in Fig.1.

b B─N and TM─N bond lengths are in angstrom (Å).

c N─B─N and N─TM─N bond angles are in degrees (°).

Table S2

The selected geometrical parameters of pristine and TM−doped B12N12.

| Species | Bond a | Bond lengths b | Bond a | Bond angles c |
| --- | --- | --- | --- | --- |
| B12N12 | N3─B1 | 1.509 | B1─N3─B2 | 83.6 |
|  | N3─B2 | 1.509 | B2─N3─B3 | 114.0 |
|  | N3─B3 | 1.433 | B3─N3─B1 | 114.0 |
| FeB12N11 | TM─B1 | 2.036 | B1─TM─B2 | 62.2 |
|  | TM─B2 | 2.036 | B2─TM─B3 | 84.0 |
|  | TM─B3 | 1.935 | B3─TM─B1 | 84.0 |
| CoB12N11 | TM─B1 | 1.947 | B1─TM─B2 | 67.2 |
|  | TM─B2 | 1.947 | B2─TM─B3 | 84.8 |
|  | TM─B3 | 1.900 | B3─TM─B1 | 84.8 |
| NiB12N11 | TM─B1 | 2.004 | B1─TM─B2 | 59.8 |
|  | TM─B2 | 2.004 | B2─TM─B3 | 93.0 |
|  | TM─B3 | 1.974 | B3─TM─B1 | 93.0 |
| RuB12N11 | TM─B1 | 2.108 | B1─TM─B2 | 59.3 |
|  | TM─B2 | 2.108 | B2─TM─B3 | 81.6 |
|  | TM─B3 | 1.993 | B3─TM─B1 | 81.6 |
| RhB12N11 | TM─B1 | 2.046 | B1─TM─B2 | 63.2 |
|  | TM─B2 | 2.046 | B2─TM─B3 | 82.3 |
|  | TM─B3 | 1.982 | B3─TM─B1 | 82.3 |
| PdB12N11 | TM─B1 | 2.104 | B1─TM─B2 | 59.1 |
|  | TM─B2 | 2.104 | B2─TM─B3 | 89.2 |
|  | TM─B3 | 2.088 | B3─TM─B1 | 89.2 |
| OsB12N11 | TM─B1 | 2.099 | B1─TM─B2 | 61.9 |
|  | TM─B2 | 2.099 | B2─TM─B3 | 81.8 |
|  | TM─B3 | 2.001 | B3─TM─B1 | 81.8 |
| IrB12N11 | TM─B1 | 2.048 | B1─TM─B2 | 63.9 |
|  | TM─B2 | 2.048 | B2─TM─B3 | 83.7 |
|  | TM─B3 | 1.981 | B3─TM─B1 | 83.8 |
| PtB12N11 | TM─B1 | 2.083 | B1─TM─B2 | 61.4 |
|  | TM─B2 | 2.083 | B2─TM─B3 | 91.0 |
|  | TM─B3 | 2.051 | B3─TM─B1 | 91.0 |

a B1, B2, and B3 are atoms on the B12N12 which are deﬁned in Fig.1.

b TM─B bond lengths are in Å.

c B─TM─B bond angles are in °.

Table S3

The selected geometrical parameters of H2 molecule adsorbed on TM−doped B12N12.

| Species | Bond a | Bond lengths b | Bond a | Bond angles c | H─H b |
| --- | --- | --- | --- | --- | --- |
| H2/FeB11N12 | TM─N1 | 1.904 | N1─TM─N2 | 76.5 | 0.757 |
|  | TM─N2 | 1.887 | N2─TM─N3 | 101.9 |  |
|  | TM─N3 | 1.845 | N3─TM─N1 | 104.2 |  |
| H2/CoB11N12 | TM─N1 | 1.872 | N1─TM─N2 | 76.7 | 0.756 |
|  | TM─N2 | 1.877 | N2─TM─N3 | 103.3 |  |
|  | TM─N3 | 1.843 | N3─TM─N1 | 100.9 |  |
| H2/NiB11N12 | TM─N1 | 1.989 | N1─TM─N2 | 71.1 | 0.751 |
|  | TM─N2 | 1.991 | N2─TM─N3 | 104.3 |  |
|  | TM─N3 | 1.907 | N3─TM─N1 | 104.2 |  |
| H2/RuB11N12 | TM─N1 | 2.045 | N1─TM─N2 | 70.5 | 0.774 |
|  | TM─N2 | 2.045 | N2─TM─N3 | 94.7 |  |
|  | TM─N3 | 1.929 | N3─TM─N1 | 94.7 |  |
| H2/RhB11N12 | TM─N1 | 2.023 | N1─TM─N2 | 70.9 | 0.772 |
|  | TM─N2 | 2.021 | N2─TM─N3 | 95.1 |  |
|  | TM─N3 | 1.985 | N3─TM─N1 | 98.3 |  |
| H2/PdB11N12 | TM─N1 | 2.013 | N1─TM─N2 | 65.7 | 0.769 |
|  | TM─N2 | 2.417 | N2─TM─N3 | 96.2 |  |
|  | TM─N3 | 2.013 | N3─TM─N1 | 93.4 |  |
| H2/OsB11N12 | TM─N1 | 2.091 | N1─TM─N2 | 69.8 | 0.889 |
|  | TM─N2 | 2.013 | N2─TM─N3 | 98.3 |  |
|  | TM─N3 | 1.942 | N3─TM─N1 | 92.7 |  |
| H2/IrB11N12 | TM─N1 | 2.032 | N1─TM─N2 | 70.2 | 0.833 |
|  | TM─N2 | 2.036 | N2─TM─N3 | 94.3 |  |
|  | TM─N3 | 1.992 | N3─TM─N1 | 100.6 |  |
| H2/PtB11N12 | TM─N1 | 2.431 | N1─TM─N2 | 65.1 | 0.807 |
|  | TM─N2 | 2.009 | N2─TM─N3 | 93.9 |  |
|  | TM─N3 | 2.014 | N3─TM─N1 | 96.5 |  |

a N1, N2, and N3 are atoms on the B12N12 which are deﬁned in Fig.1.

b B─N bond lengths, TM─N bond lengths, H─H bond lengths, and adsorption distances between H2 and TM atoms of TMdoped B12N12 are in Å.

c N─B─N and N─TM─N bond angles are in °.

Table S4

The selected geometrical parameters of H2 molecule adsorbed on TM−doped B12N12.

| Species | Bond a | Bond lengths b | Bond a | Bond angles c | H─H b |
| --- | --- | --- | --- | --- | --- |
| H2/FeB12N11 | TM─B1 | 2.040 | B1─TM─B2 | 62.1 | 0.785 |
|  | TM─B2 | 2.042 | B2─TM─B3 | 82.4 |  |
|  | TM─B3 | 1.964 | B3─TM─B1 | 83.2 |  |
| H2/CoB12N11 | TM─B1 | 1.955 | B1─TM─B2 | 66.6 | 0.779 |
|  | TM─B2 | 1.955 | B2─TM─B3 | 83.0 |  |
|  | TM─B3 | 1.932 | B3─TM─B1 | 83.0 |  |
| H2/NiB12N11 | TM─B1 | 2.000 | B1─TM─B2 | 60.9 | 0.779 |
|  | TM─B2 | 2.011 | B2─TM─B3 | 85.2 |  |
|  | TM─B3 | 1.972 | B3─TM─B1 | 93.7 |  |
| H2/RuB12N11 | TM─B1 | 2.111 | B1─TM─B2 | 58.9 | 0.771 |
|  | TM─B2 | 2.111 | B2─TM─B3 | 80.8 |  |
|  | TM─B3 | 2.027 | B3─TM─B1 | 80.8 |  |
| H2/RhB12N11 | TM─B1 | 2.051 | B1─TM─B2 | 62.8 | 0.765 |
|  | TM─B2 | 2.051 | B2─TM─B3 | 81.3 |  |
|  | TM─B3 | 2.008 | B3─TM─B1 | 81.3 |  |
| H2/PdB12N11 | TM─B1 | 2.109 | B1─TM─B2 | 58.3 | 0.759 |
|  | TM─B2 | 2.109 | B2─TM─B3 | 87.4 |  |
|  | TM─B3 | 2.088 | B3─TM─B1 | 87.0 |  |
| H2/OsB12N11 | TM─B1 | 2.119 | B1─TM─B2 | 58.8 | 0.779 |
|  | TM─B2 | 2.120 | B2─TM─B3 | 82.0 |  |
|  | TM─B3 | 2.005 | B3─TM─B1 | 82.1 |  |
| H2/IrB12N11 | TM─B1 | 2.055 | B1─TM─B2 | 63.3 | 0.785 |
|  | TM─B2 | 2.055 | B2─TM─B3 | 82.6 |  |
|  | TM─B3 | 2.016 | B3─TM─B1 | 82.6 |  |
| H2/PtB12N11 | TM─B1 | 2.089 | B1─TM─B2 | 60.6 | 0.761 |
|  | TM─B2 | 2.089 | B2─TM─B3 | 88.8 |  |
|  | TM─B3 | 2.046 | B3─TM─B1 | 88.8 |  |

a B1, B2, and B3 are atoms on the B12N12 which are deﬁned in Fig.1.

b N─B bond lengths, TM─B bond lengths, H─H bond lengths, and adsorption distances between H2 and TM atoms of TMdoped B12N12 are in Å.

c B─TM─B bond angles are in °.

Table S5

The highest occupied molecular orbital energies (EHOMO), the lowest unoccupied molecular orbital energies (ELUMO), energy gaps (Eg), changes of energy  gaps (Eg), percentage change of energy gaps (Eg), electronic chemical potential (), electronegativity (), chemical hardness (), electrophilicity (), and softness (S) partial charge transfers (PCTs) of 2H2 molecule adsorbed on the pristine and TM−doped B12N12, computed at the B3LYP/LanL2DZ level of theory.

| Species | EHOMOa | ELUMOa | Ega | Ega | %Eg | a | a | a | a | Sa | PCTsb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2H2/B12N12 | -7.848 | -1.905 | 5.943 | 0.004 | 0.07 | -4.876 | 4.876 | 2.971 | 4.001 | 0.168 | 0.011 |
| 2H2/FeB11N12 | -6.405 | -3.911 | 2.494 | -1.541 | -161.59 | -5.158 | 5.158 | 1.247 | 10.668 | 0.401 | 0.229 |
| 2H2/RuB11N12 | -6.799 | -3.545 | 3.255 | -0.023 | -0.71 | -5.172 | 5.172 | 1.627 | 8.219 | 0.307 | 0.346 |
| 2H2/OsB11N12 | -6.218 | -3.101 | 3.117 | 0.107 | 3.32 | -4.659 | 4.659 | 1.559 | 6.964 | 0.321 | 0.512 |
| 2H2/CoB11N12 | -7.216 | -4.074 | 3.143 | 0.174 | 5.24 | -5.645 | 5.645 | 1.571 | 10.140 | 0.318 | 0.225 |
| 2H2/RhB11N12 | -7.029 | -3.878 | 3.152 | 0.069 | 2.13 | -5.454 | 5.454 | 1.576 | 9.437 | 0.317 | 0.330 |
| 2H2/IrB11N12 | -6.966 | -3.824 | 3.142 | 0.038 | 1.20 | -5.395 | 5.395 | 1.571 | 9.265 | 0.318 | 0.502 |
| 2H2/NiB11N12 | -7.013 | -5.451 | 1.561 | 0.079 | 4.80 | -6.232 | 6.232 | 0.781 | 24.874 | 0.640 | 0.142 |
| 2H2/PdB11N12 | -6.825 | -4.445 | 2.380 | -1.365 | -134.57 | -5.635 | 5.635 | 1.190 | 13.340 | 0.420 | 0.236 |
| 2H2/PtB11N12 | -5.426 | -3.656 | 1.770 | 0.139 | 7.28 | -4.541 | 4.541 | 0.885 | 11.648 | 0.565 | 0.404 |
| 2H2/FeB12N11 | -7.369 | -2.842 | 4.527 | -0.019 | -0.43 | -5.106 | 5.106 | 2.264 | 5.758 | 0.221 | 0.311 |
| 2H2/RuB12N11 | -6.947 | -2.745 | 4.202 | 0.455 | 9.77 | -4.846 | 4.846 | 2.101 | 5.589 | 0.238 | 0.246 |
| 2H2/OsB12N11 | -6.760 | -2.688 | 4.072 | 0.019 | 0.45 | -4.724 | 4.724 | 2.036 | 5.480 | 0.246 | 0.354 |
| 2H2/CoB12N11 | -7.320 | -2.896 | 4.423 | -0.010 | -0.23 | -5.108 | 5.108 | 2.212 | 5.899 | 0.226 | 0.354 |
| 2H2/RhB12N11 | -7.214 | -2.564 | 4.651 | -0.070 | -1.54 | -4.889 | 4.889 | 2.325 | 5.140 | 0.215 | 0.246 |
| 2H2/IrB12N11 | -7.299 | -2.862 | 4.437 | -0.054 | -1.23 | -5.080 | 5.080 | 2.218 | 5.817 | 0.225 | 0.342 |
| 2H2/NiB12N11 | -5.525 | -2.288 | 3.237 | -0.587 | -22.13 | -3.907 | 3.907 | 1.619 | 4.714 | 0.309 | 0.278 |
| 2H2/PdB12N11 | -5.025 | -2.352 | 2.672 | -0.373 | -16.24 | -3.689 | 3.689 | 1.336 | 5.091 | 0.374 | 0.164 |
| 2H2/PtB12N11 | -4.992 | -2.249 | 2.742 | -0.508 | -22.74 | -3.621 | 3.621 | 1.371 | 4.780 | 0.365 | 0.200 |

a In eV., b In e.

Table S6

The highest occupied molecular orbital energies (EHOMO), the lowest unoccupied molecular orbital energies (ELUMO), energy gaps (Eg), changes of energy  gaps (Eg), percentage change of energy gaps (Eg), electronic chemical potential (), electronegativity (), chemical hardness (), electrophilicity (), and softness (S) partial charge transfers (PCTs) of 3H2 molecule adsorbed on the pristine and TM−doped B12N12, computed at the B3LYP/LanL2DZ level of theory.

| Species | EHOMOa | ELUMOa | Ega | Ega | %Eg | a | a | a | a | Sa | PCTsb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3H2/B12N12 | -7.826 | -1.876 | 5.949 | -0.002 | -0.041 | -4.851 | 4.851 | 2.975 | 3.955 | 0.168 | 0.024 |
| 3H2/FeB11N12 | -7.161 | -3.687 | 3.473 | -2.520 | -264.269 | -5.424 | 5.424 | 1.737 | 8.471 | 0.288 | 0.416 |
| 3H2/RuB11N12 | -6.318 | -2.491 | 3.827 | -0.595 | -18.415 | -4.405 | 4.405 | 1.913 | 5.070 | 0.261 | 0.654 |
| 3H2/OsB11N12 | -6.819 | -1.666 | 5.152 | -1.928 | -59.794 | -4.243 | 4.243 | 2.576 | 3.494 | 0.194 | 0.929 |
| 3H2/CoB11N12 | -6.203 | -6.301 | -0.098 | 3.415 | 102.954 | -6.252 | 6.252 | -0.049 | -398.962 | -10.208 | 0.402 |
| 3H2/RhB11N12 | -6.921 | -3.357 | 3.564 | -0.344 | -10.681 | -5.139 | 5.139 | 1.782 | 7.409 | 0.281 | 0.550 |
| 3H2/IrB11N12 | -6.773 | -2.638 | 4.135 | -0.955 | -30.047 | -4.706 | 4.706 | 2.068 | 5.355 | 0.242 | 0.858 |
| 3H2/NiB11N12 | -6.998 | -5.288 | 1.710 | -0.070 | -4.248 | -6.143 | 6.143 | 0.855 | 22.069 | 0.585 | 0.240 |
| 3H2/PdB11N12 | -5.677 | -4.754 | 0.922 | 0.092 | 9.091 | -5.215 | 5.215 | 0.461 | 29.487 | 1.084 | 0.251 |
| 3H2/PtB11N12 | -5.398 | -3.691 | 1.707 | 0.202 | 10.603 | -4.544 | 4.544 | 0.854 | 12.097 | 0.586 | 0.408 |
| 3H2/FeB12N11 | -7.331 | -1.999 | 5.332 | -0.825 | -18.290 | -4.665 | 4.665 | 2.666 | 4.081 | 0.188 | 0.624 |
| 3H2/RuB12N11 | -7.061 | -1.706 | 5.355 | -0.698 | -14.989 | -4.384 | 4.384 | 2.677 | 3.589 | 0.187 | 0.547 |
| 3H2/OsB12N11 | -7.104 | -1.631 | 5.473 | -1.382 | -33.797 | -4.367 | 4.367 | 2.736 | 3.485 | 0.183 | 0.817 |
| 3H2/CoB12N11 | -7.331 | -1.794 | 5.537 | -1.124 | -25.472 | -4.563 | 4.563 | 2.769 | 3.760 | 0.181 | 0.716 |
| 3H2/RhB12N11 | -7.225 | -1.767 | 5.457 | -0.877 | -19.155 | -4.496 | 4.496 | 2.729 | 3.704 | 0.183 | 0.483 |
| 3H2/IrB12N11 | -7.245 | -1.641 | 5.604 | -1.221 | -27.859 | -4.443 | 4.443 | 2.802 | 3.523 | 0.178 | 0.684 |
| 3H2/NiB12N11 | -5.487 | -2.252 | 3.235 | -0.585 | -22.051 | -3.869 | 3.869 | 1.618 | 4.628 | 0.309 | 0.288 |
| 3H2/PdB12N11 | -5.020 | -2.348 | 2.672 | -0.373 | -16.215 | -3.684 | 3.684 | 1.336 | 5.080 | 0.374 | 0.169 |
| 3H2/PtB12N11 | -4.987 | -2.240 | 2.747 | -0.512 | -22.920 | -3.614 | 3.614 | 1.373 | 4.754 | 0.364 | 0.204 |

a In eV., b In e.

Table S7

The highest occupied molecular orbital energies (EHOMO), the lowest unoccupied molecular orbital energies (ELUMO), energy gaps (Eg), changes of energy gaps (Eg), percentage change of energy gaps (Eg), electronic chemical potential (), electronegativity (), chemical hardness (), electrophilicity (), and softness (S) partial charge transfers (PCTs) of 4H2 molecule adsorbed on the pristine and TM−doped B12N12, computed at the B3LYP/LanL2DZ level of theory.

| Species | EHOMO | ELUMO | Eg | Eg | %Eg |  |  |  |  | S | PCTs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 4H2/B12N12 | -7.817 | -1.868 | 5.949 | -0.002 | -0.032 | -4.843 | 4.843 | 2.974 | 3.942 | 0.168 | 0.027 |
| 4H2/FeB11N12 | -6.954 | -3.650 | 3.303 | -2.350 | -246.433 | -5.302 | 5.302 | 1.652 | 8.511 | 0.303 | 0.419 |
| 4H2/RuB11N12 | -6.447 | -2.643 | 3.804 | -0.572 | -17.700 | -4.545 | 4.545 | 1.902 | 5.431 | 0.263 | 0.653 |
| 4H2/OsB11N12 | -6.821 | -1.651 | 5.170 | -1.945 | -60.334 | -4.236 | 4.236 | 2.585 | 3.472 | 0.193 | 0.931 |
| 4H2/CoB11N12 | -7.053 | -3.618 | 3.434 | -0.118 | -3.544 | -5.335 | 5.335 | 1.717 | 8.289 | 0.291 | 0.407 |
| 4H2/RhB11N12 | -6.923 | -3.361 | 3.563 | -0.342 | -10.630 | -5.142 | 5.142 | 1.781 | 7.422 | 0.281 | 0.552 |
| 4H2/IrB11N12 | -6.765 | -2.603 | 4.162 | -0.982 | -30.894 | -4.684 | 4.684 | 2.081 | 5.271 | 0.240 | 0.859 |
| 4H2/NiB11N12 | -6.959 | -5.344 | 1.614 | 0.026 | 1.560 | -6.151 | 6.151 | 0.807 | 23.438 | 0.619 | 0.246 |
| 4H2/PdB11N12 | -7.183 | -3.896 | 3.287 | -2.272 | -223.921 | -5.539 | 5.539 | 1.643 | 9.335 | 0.304 | 0.276 |
| 4H2/PtB11N12 | -7.093 | -2.975 | 4.118 | -2.209 | -115.662 | -5.034 | 5.034 | 2.059 | 6.153 | 0.243 | 0.430 |
| 4H2/FeB12N11 | -7.345 | -2.021 | 5.324 | -0.816 | -18.109 | -4.683 | 4.683 | 2.662 | 4.119 | 0.188 | 0.626 |
| 4H2/RuB12N11 | -6.469 | -1.682 | 4.787 | -0.130 | -2.787 | -4.076 | 4.076 | 2.393 | 3.470 | 0.209 | 0.587 |
| 4H2/OsB12N11 | -7.086 | -1.625 | 5.461 | -1.371 | -33.524 | -4.355 | 4.355 | 2.731 | 3.473 | 0.183 | 0.821 |
| 4H2/CoB12N11 | -7.338 | -1.780 | 5.558 | -1.145 | -25.934 | -4.559 | 4.559 | 2.779 | 3.739 | 0.180 | 0.721 |
| 4H2/RhB12N11 | -7.228 | -1.765 | 5.463 | -0.883 | -19.286 | -4.497 | 4.497 | 2.732 | 3.701 | 0.183 | 0.489 |
| 4H2/IrB12N11 | -7.242 | -1.619 | 5.624 | -1.241 | -28.312 | -4.431 | 4.431 | 2.812 | 3.491 | 0.178 | 0.688 |
| 4H2/NiB12N11 | -5.518 | -2.292 | 3.227 | -0.576 | -21.723 | -3.905 | 3.905 | 1.613 | 4.726 | 0.310 | 0.291 |
| 4H2/PdB12N11 | -5.023 | -2.346 | 2.677 | -0.378 | -16.452 | -3.685 | 3.685 | 1.339 | 5.071 | 0.373 | 0.174 |
| 4H2/PtB12N11 | -4.993 | -2.260 | 2.733 | -0.499 | -22.336 | -3.626 | 3.626 | 1.367 | 4.811 | 0.366 | 0.203 |

a In eV., b In e.

Fig. S1. The optimized structures of (a) 2H2/FeB11N12, (b) 2H2/CoB11N12, (c) 2H2/NiB11N12, (d) 2H2/RuB11N12, (e) 2H2/RhB11N12, (f) 2H2/PdB11N12, (g) 2H2/OsB11N12, (h) 2H2/IrB11N12, and (i) 2H2/PtB11N12.

Fig. S2. The optimized structures of (a) 2H2/FeB12N11, (b) 2H2/CoB12N11, (c) 2H2/NiB12N11, (d) 2H2/RuB12N11, (e) 2H2/RhB12N11, (f) 2H2/PdB12N11, (g) 2H2/OsB12N11, (h) 2H2/IrB12N11, and (i) 2H2/PtB12N11.

Fig. S3. The optimized structures of (a) 3H2/FeB11N12, (b) 3H2/CoB11N12, (c) 3H2/NiB11N12, (d) 3H2/RuB11N12, (e) 3H2/RhB11N12, (f) 3H2/PdB11N12, (g) 3H2/OsB11N12, (h) 3H2/IrB11N12, and (i) 3H2/PtB11N12.

Fig. S4. The optimized structures of (a) 3H2/FeB12N11, (b) 3H2/CoB12N11, (c) 3H2/NiB12N11, (d) 3H2/RuB12N11, (e) 3H2/RhB12N11, (f) 3H2/PdB12N11, (g) 3H2/OsB12N11, (h) 3H2/IrB12N11, and (i) 3H2/PtB12N11.

Fig. S5. The optimized structures of (a) 4H2/FeB11N12, (b) 4H2/CoB11N12, (c) 4H2/NiB11N12, (d) 4H2/RuB11N12, (e) 4H2/RhB11N12, (f) 4H2/PdB11N12, (g) 4H2/OsB11N12, (h) 4H2/IrB11N12, and (i) 4H2/PtB11N12.

Fig. S6. The optimized structures of (a) 4H2/FeB12N11, (b) 4H2/CoB12N11, (c) 4H2/NiB12N11, (d) 4H2/RuB12N11, (e) 4H2/RhB12N11, (f) 4H2/PdB12N11, (g) 4H2/OsB12N11, (h) 4H2/IrB12N11, and (i) 4H2/PtB12N11.

Fig. S7. The DOSs of H2 adsorbed on (a) FeB11N12, (b) CoB11N12, (c) NiB11N12, (d) RuB11N12, (e) RhB11N12, (f) PdB11N12, (g) OsB11N12, (h) IrB11N12, and (i) PtB11N12.

Fig. S8. The DOSs of H2 adsorbed on (a) FeB12N11, (b) CoB12N11, (c) NiB12N11, (d) RuB12N11, (e) RhB12N11, (f) PdB12N11, (g) OsB12N11, (h) IrB12N11, and (i) PtB12N11.