
Supplementary Material

Analyses of variance

Tables S1 and S2 present the analysis of variance for the photocatalytic degradation of HA and FAH, respectively.

Table S1 Analysis of variance for humic acid degradation.
	Source
	df
	Adj SS
	Adj MS
	F-value
	P-value

	Regression
	4
	0.078088
	0.019522
	33.98
	0.001

	[ZnO–TiO2]
	1
	0.007812
	0.007812
	13.60
	0.014

	Replicate
	1
	0.007840
	0.007840
	13.65
	0.014

	[ZnO–TiO2]*[ZnO–TiO2]
	1
	0.018922
	0.018922
	32.94
	0.002

	[ZnO–TiO2]*[pH]
	1
	0.043513
	0.043513
	75.74
	0.000

	Error
	5
	0.002873
	0.000575
	
	

	Total
	9
	0.080960
	
	
	



S =  0.0239687. R2 = 96.45%. Adjusted R2 = 93.61%. Predicted R2 = 86.03%

Table S2  Analysis of variance for fulvic acid + humin degradation.
	Source
	df
	Adj SS
	Adj MS
	F-value
	P-value

	Regression
	4
	0.043080
	0.010770
	149.58
	0.000

	[ZnO–TiO2]
	1
	0.028800
	0.028800
	400.00
	0.000

	Replicate
	1
	0.007840
	0.007840
	108.89
	0.000

	[ZnO–TiO2]*[ZnO–TiO2]
	1
	0.003240
	0.003240
	45.00
	0.001

	[ZnO–TiO2]*[pH]
	1
	0.003200
	0.003200
	44.44
	0.001

	Error
	5
	0.000360
	0.000072
	
	

	Total
	9
	0.043440
	
	
	



S = 0.0084853. R2 = 99.17%. Adjusted R2 = 98.51%. Predicted R2 = 96.94%.

