Strong-coupled Co0.85Se/rGO composite as high-efficient electrocatalyst for oxygen evolution

Zhongbao Fenga,b, Lili Renc, Yanting Liud, Bo Gaoa,b

aKey Laboratory for Ecological Metallurgy of Multimetallic Mineral (Ministry of Education), Northeastern University, Shenyang 110819, PR China

bSchool of Metallurgy, Northeastern University, Shenyang, Liaoning 110819, PR China

cShenyang Aircraft Industry (Group) Co. Ltd., Shenyang, 410007, China

dZhongye Changtian International Engineering Co. Ltd., Changsha, 110034, China

Fig. S1 CV curves of a) Co0.85Se/rGO, b) Co0.85Se, c) NF in the capacitance current range at various scan rates

Fig. S2 LSV plots of Co0.85Se/rGO and Co0.85Se normalized by ECSA in 1.0 M KOH electrolyte

Fig. S3 a) SEM image of Co0.85Se /rGO after 24 h OER long-term stability test, b) capacitive current densities of fresh and used Co0.85Se/rGO after OER long-term stability as a function of scan rate (Δj = |ja - jc|/2)

Fig. S4 Adhesive force measurements of the gas bubbles towards Co0.85Se surface

Table S1 Comparision of OER performance of Co0.85Se/rGO with other non-noble metal-based electrocatalysts.

| Samples | Electrolyte | η (mV)@ j (mA cm-2 ) | Tafel slope (mV dec-1) | Working electrode | Ref. |
| --- | --- | --- | --- | --- | --- |
| CoSe2-DFe-VCo | 1.0 M KOH | ≈400@100 | 53.5 | Glassy carbon | [S] |
| CoSe2 | 1.0 M KOH | 284@10 | 46.3 | Glassy carbon | [S] |
| CoSe2 | 1.0 M KOH | 310@10 | 40.1 | Glassy carbon | [S] |
| O–CoSe2 | 1.0 M KOH | 252@10 | 62 | Glassy carbon | [S] |
| CoSe@NCNT/NCN | 1.0 M KOH | 301@10 | 75 | Glassy carbon | [S] |
| CoSe2-NCNT NSA | 1.0 M KOH | 290@10 | 50.9 | Carbon cloth | [S] |
| CoSe2 | 1.0 M KOH | 287@10 | 54.3 | Glassy carbon | [S] |
| o-CoSe2-O | 1.0 M KOH | 251@10 | 73 | Glassy carbon | [S] |
| Co0.85Se/rGO | 1.0 M KOH | 274@100 243@10 | 26.5 | NF | This work |

References

[S]	Y. Dou, C.T. He, L. Zhang, H. Yin, M. Al-Mamun, J. Ma, H. Zhao, Approaching the activity limit of CoSe2 for oxygen evolution via Fe doping and Co vacancy, Nat. Commun., 2020, 11, 1-9. .

[S]	Y. Zhang, C. Zhang, Y. Guo, D. Liu, Y. Yu, B. Zhang, Selenium vacancy-rich CoSe2 ultrathin nanomeshes with abundant active sites for electrocatalytic oxygen evolution. J. Mate. Chem. A, 2019, 7, 2536-2540.

[S]	C. Zhang, B. Tang, X. Gu, L. Feng, Surface chemical state evaluation of CoSe2 catalysts for the oxygen evolution reaction, Chem. Commun., 2019, 55, 10928-10931.

[S]	B. Jia, Z. Xue, Q. Liu, Q. Liu, K. Liu, M. Liu, T.S. Chan, Y. Li, Z. Li, C.Y. Su, G. Li, Hierarchical nanotubes constructed from CoSe2 nanorods with an oxygen-rich surface for an efficient oxygen evolution reaction, J. Mater. Chem. A, 2019, 7, 15073-15078.

[S]	M. Yang, Y. Yang, K. Wang, S. Li, F. Feng, K. Lan, P. Jiang, X. Huang, H. Yang, R. Li, Facile synthesis of CoSe nanoparticles encapsulated in N-doped carbon nanotubes-grafted N-doped carbon nanosheets for water splitting, Electrochim. Acta, 2020,.337, 135685.

[S]	W. Liu, D. Zheng, L. Zhang, R. Yin, X. Xu, W. Shi, F. Wu, X. Cao, X. Lu, Bioinspired interfacial engineering of a CoSe2 decorated carbon framework cathode towards temperature-tolerant and flexible Zn–air batteries, Nanoscale, 2021, 13, 3019-3026.

[S]	Z. Li, Z. Jiang, W. Zhu, C. He, P. Wang, X. Wang, T. Li, L. Tian, Facile preparation of CoSe2 nano-vesicle derived from ZIF-67 and their application for efficient water oxidation, Appl. Sur. Sci., 2020, 504, 144368.

[S]	X. Wang, L. Zhuang, Y. Jia, H. Liu, X. Yan, L. Zhang, D. Yang, Z. Zhu, X. Yao, Plasma-triggered synergy of exfoliation, phase transformation, and surface engineering in cobalt diselenide for enhanced water oxidation, Angew. Chem. Int.l Edit., 2018, 57, 16421-16425.

Corresponding author. E-mail address: fengzb@smm.neu.edu.cn (Z.B. Feng)