Supporting Information

NOx Removal and Copper Recovery from the Leaching process for Waste Printed Circuit Boards: Performance Evaluation and Potential Environmental Impact Assessment

Tse-Lun Chen1,2, Yen-Syun Chen1, Po-Chi Tseng1, Yi-Hung Chen3, Ching-Hsiang Hsu4, and Pen-Chi Chiang1,*

1 Graduate Institute of Environmental Engineering, National Taiwan University, 10673, Taipei, Taiwan.

2 Institute of Environmental Engineering, ETH Zürich, Zürich 8093, Switzerland

3 Department of Chemical Engineering and Biotechnology, National Taipei University of Technology, 10608, Taipei, Taiwan.

4 UWin Nanotech Company Limited., 236, New Taipei City, Taiwan.

The number of figures: 6

The number of tables: 3

Text S1:

In this study, 2.5 grams of copper foil were used in each batch experiment and the theoretical NOx produced per batch was 0.0159 mol that calculated according to eq. S1:

2.5 (g)63 (gmol)×2 (mol)1 (mol)=0.0159 mol    (S1)

The stoichiometric ratio of H2O2(l), ClO2(l), and O3(g) to react with NOx are 1.5, 0.6 and 1.0, respectively. The corresponding oxidants/NOx ratios were 2.0, 1.0 and 1.5. Thus, the volumes of h H2O2(l), ClO2(l) added in each run were 0.28 mL and 53.67 mL based on the calculations as follows:

[H2O2]=35.510034 (g/mol)×1.1 (cm3g)=9.5×103 M   (S2)

VH2O2=0.00161 mol/11.49 mol/L×1000mLL×2=0.28 mL   (S3)

ClO2=0.2g67.45gmol100 g×1 cm3g×1000 cm31 L=0.029 M   (S4)

VClO2=0.00161 mol/0.030mol/L×1000mLL×1=53.67 mL   (S5)

On the other hand, note that ozone was added continuously through the ozone generator,

[O3]=83.8 g148gmol1 m3×1 m31000 L=0.00175 M   (S6)

QO3=0.0159 mol/0.00175mol/L×1000mLL×1.535 (min=39.4 mL/min  (S7)

Fig. S1 Copper recovery and NOx emissions control process for WPCB treatment.

Fig. S2 System boundary of copper recovery and NOx emissions control during WPCB treatment to assessing the environmental impact. (Assumptions: functional unit is recovery of 1,000 g refined copper with NOx removal ratio of 85%, nitric acid recovery ratio of 80%, and copper recovery ratio of 100%)

Fig. S3 Boxplot of NOx, NO and NO2 concentration during copper leaching.

Fig. S4 Time dependent pH variation of (a) H2O2(aq), (b) ClO2(aq), and (c) O3(g) with different concentration of NaOH(aq).

Fig. S5 NOx emissions mass contents during the crushed and sieved WPCB of HNO3(l) leaching. (Experimental conditions: 5 g WPCB with nitric acid leaching, RPB was operating at β = 131 and G/L ratio = 0.83 with 0.06 M NaOH(aq) addition)

Fig. S6 (a) Comparison between actual (experimental) and predicted value, (b) Contour plot for removal efficiency for G/L ratio = 0.83, and (c) 3-D response surface plot for NOx removal efficiency in G/L ratio = 0.83.

Table S1. Data inventory of input and output materials.

| Process | Materials/utilities | Consumption | Outputs |
| --- | --- | --- | --- |
| Crush | WPCB | 2,280 g | WPCB powder |
|  | Crusher | 0.8 kWh |  |
| Sieving | WPCB powder | 2,280 g | WPCB powder |
|  | Sieve sorter | 0.25 kWh |  |
| Copper leaching by HNO3(l) | WPCB powder | 2,000 g | Copper nitrate solution Glass fiber powder Epoxy resin powder |
|  | Tap water | 4.02 L |  |
|  | 68 vol.% HNO3(l) | 2.68 L |  |
| Filtration | Pump | 0.25 kWh |  |
| NOx removal using an RPB reactor | RPB reactor | 1.6 kWh | Waste water |
|  | Auxiliary equipment | 1.2 kWh |  |
|  | Tap water | 1.6 L |  |
| Copper nitrate Reduction | NaOH(g) | 90.45 g | Copper powder Iron nitrate solution |
|  | Tap water | 2.01 L |  |
|  | Iron powders | 1,500 g |  |
|  | Mixing heater | 3.2 kWh |  |
| Filtration | Pump | 0.25 kWh |  |
| Drying | Heater | 0.6 kWh | Dried copper powder |
| Refinement | Microwave oven | 5.5 kWh | Refined copper |

Table S2. ANOVA results of establishing response surface model.

| Source | Sum of Squares | Df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 6624.12 | 6 | 1104.02 | 47.76 | < 0.0001 | significant |
| A-CNaOH | 1522.39 | 1 | 1522.39 | 65.85 | < 0.0001 |  |
| B-β | 7.49 | 1 | 7.49 | 0.3239 | 0.0007 |  |
| C-G/L | 440.89 | 1 | 440.89 | 19.07 | 0.0011 |  |
| AC | 437.15 | 1 | 437.15 | 18.91 | 0.0012 |  |
| B² | 157.50 | 1 | 157.50 | 6.81 | 0.0243 |  |
| C² | 163.00 | 1 | 163.00 | 7.05 | 0.0224 |  |
| Residual | 254.30 | 11 | 23.12 |  |  |  |
| Lack of Fit | 254.30 | 9 | 28.26 |  |  |  |
| Pure Error | 0.0000 | 2 | 0.0000 |  |  |  |
| Cor Total | 6878.42 | 17 |  |  |  |  |

Table S3. Input-output results from LCA analysis under three scenarios as the functional unit of 1 kg copper recovery from WPCB (Scenario 1: Copper recovery of 100% without NOx removal process, scenario 2: Copper recover ratio of 100% with NOx removal ratio of 85%, scenario 3: copper recover ratio of 95% with NOx removal ratio of 85%, and scenario 4: copper recovery ratio of 80% with NOx removal ratio of 85%)

|  | items | units | Scenario 1 | Scenario 2 | Scenario 3 | Scenario 4 |
| --- | --- | --- | --- | --- | --- | --- |
| Input | WPCB | kg | 2.28 | 2.28 | 2.4 | 2.85 |
|  | Tap water | kg | 6 | 3.4 | 3.58 | 4.25 |
|  | Electricity | kWh | 10.85 | 13.65 | 14.37 | 17.1 |
|  | Iron powder | kg | 1.5 | 1.5 | 1.58 | 1.88 |
|  | Nitric acid | kg | 0.9 | 0.18 | 0.19 | 0.23 |
|  | NaOH(s) | kg | 0.9 | 2.18 | 2.29 | 2.73 |
|  | O3(g) | kg | - | 0.12 | 0.13 | 0.15 |
|  | NOx(g) | kg | 0.0481 | -0.041 | -0.043 | -0.05 |
| Output | Refined copper | kg | 1 | 1 | 1 | 1 |
|  | Waste water | kg | 5.0 | 3.4 | 3.8 | 4.25 |
|  | NOx(g) | kg | 0.0481 | 0.0071 | 0.0074 | 0.0089 |
|  | Glass fiber powder (waste) | kg | 0.5 | 0.5 | 0.53 | 0.63 |
|  | Epoxy resin powder (waste) | kg | 0.4 | 0.4 | 0.42 | 0.50 |