Supporting information

Reaction Mechanism of Methyl Trifluoroacetate (CH3TFA) with Lithium Polysulfides (Li2S6) in Gas and Solvent Phase

Meera Cheviri, Senthilkumar Lakshmipathi

Department of physics, Bharathiar University, Coimbatore 641046, Tamil Nadu, INDIA

Senthilkumar Lakshmipathi: Email: lsenthilkumar@buc.edu.in

Table S1. The bonding parameters for the reactant complex RC and intermediate complex IC1.

| Polymer molecule | Bond name | Bond length (Å) | ρ (a.u.) | 2ρ (a.u.) |
| --- | --- | --- | --- | --- |
| RC | Li8-O13 | 1.944 | 0.0095 | 0.1907 |
|  | Li8-S4 | 2.383 | 0.0018 | 0.1052 |
|  | Li8-S3 | 2.636 | 0.0023 | 0.0604 |
|  | Li7-S4 | 2.372 | 0.0022 | 0.1081 |
|  | Li7-S3 | 2.362 | 0.0021 | 0.1108 |
| IC1 | Li7-O13 | 1.837 | 0.0137 | 0.2782 |
|  | Li8-O12 | 1.936 | 0.0088 | 0.2092 |
|  | Li7-S4 | 2.306 | 0.0016 | 0.1273 |
|  | Li7-S3 | 2.674 | 0.0026 | 0.0542 |
|  | Li8-S6 | 2.484 | 0.0021 | 0.0826 |
|  | Li8-S1 | 2.651 | 0.0023 | 0.0543 |

Table S2. The bonding parameters for the reactant complex IC2 and product P1

| Polymer molecule | Bond name | Bond length (Å) | ρ (a.u.) | 2ρ (a.u.) |
| --- | --- | --- | --- | --- |
| IC2 | Li8-O12 | 1.854 | 0.0113 | 0.2690 |
|  | Li7-O13 | 1.838 | 0.0119 | 0.2806 |
|  | Li7-O24 | 2.011 | 0.0073 | 0.1499 |
|  | Li8-S3 | 2.593 | 0.0023 | 0.0633 |
|  | Li8-S4 | 2.462 | 0.0014 | 0.0840 |
|  | Li7-S4 | 2.483 | 0.0020 | 0.0756 |
| P1 | Li8-O12 | 1.952 | 0.0076 | 0.1993 |
|  | Li8-O13 | 1.935 | 0.0080 | 0.2093 |
|  | Li7-O24 | 1.957 | 0.0073 | 0.1946 |
|  | Li7-O23 | 1.945 | 0.0076 | 0.2022 |
|  | Li8-S6 | 2.677 | 0.0023 | 0.0503 |
|  | Li8-S3 | 2.613 | 0.0025 | 0.0605 |
|  | Li7-S2 | 2.739 | 0.0021 | 0.0433 |
|  | Li7-S4 | 2.747 | 0.0018 | 0.0430 |

Figure S1. IRC diagram for a) TS1 and b) TS2 transition states

Table S3. The bonding parameters for the reactant complex RCDME and product IC1DME

| Polymer molecule | Bond name | Bond length (Å) | ρ (a.u.) | 2ρ (a.u.) |
| --- | --- | --- | --- | --- |
| RCDME | Li8-O13 | 1.927 | 0.0106 | 0.2084 |
|  | Li8-S3 | 2.470 | 0.0025 | 0.0860 |
|  | Li8-S4 | 2.411 | 0.0020 | 0.0986 |
|  | Li7-S3 | 2.369 | 0.0017 | 0.1090 |
|  | Li7-S4 | 2.456 | 0.0023 | 0.0890 |
| IC1DME | Li7-O13 | 2.046 | 0.0052 | 0.1437 |
|  | Li7-O12 | 2.031 | 0.0054 | 0.1500 |
|  | Li7-S4 | 2.424 | 0.0019 | 0.0898 |
|  | Li7-S3 | 2.659 | 0.0025 | 0.0544 |
|  | Li8-S2 | 2.816 | 0.0014 | 0.0365 |
|  | Li8-S4 | 2.385 | 0.0011 | 0.0989 |

Table S4. The bonding parameters for the intermediate complex IC2DME and product P1DME

| Polymer molecule | Bond name | Bond length (Å) | ρ (a.u.) | 2ρ (a.u.) |
| --- | --- | --- | --- | --- |
| IC2DME | Li8-O13 | 2.136 | 0.0041 | 0.1115 |
|  | Li8-O12 | 1.999 | 0.0062 | 0.1637 |
|  | Li7-O13 | 1.863 | 0.1198 | 0.2479 |
|  | Li7-O24 | 1.993 | 0.0078 | 0.1600 |
|  | Li8-S1 | 2.674 | 0.0018 | 0.0466 |
|  | Li8-S6 | 2.542 | 0.0016 | 0.0680 |
|  | Li7-S4 | 2.412 | 0.0017 | 0.0950 |
| P1DME | Li8-O12 | 1.993 | 0.0072 | 0.1763 |
|  | Li8-O13 | 2.023 | 0.0064 | 0.1612 |
|  | Li7-O23 | 1.994 | 0.0073 | 0.1767 |
|  | Li7-O24 | 2.010 | 0.0067 | 0.1679 |
|  | Li8-S6 | 2.777 | 0.0021 | 0.0410 |
|  | Li8-S3 | 2.697 | 0.0026 | 0.0519 |
|  | Li7-S2 | 2.747 | 0.0022 | 0.0441 |
|  | Li7-S4 | 2.681 | 0.0026 | 0.0535 |

Figure S2. IRC diagram for a) TS1 and b) TS2 transition states.

Table S5. The reaction energy (E) for Step 2 and Step 4 reactions in gas phase CCSD(T) method.

| Complex | E (kcal/mol) | Complex | E (kcal/mol) |
| --- | --- | --- | --- |
|  | Step 2 |  | Step 4 |
| RC | 0.00 | IC2 | 0.00 |
| TS1 | 53.53 | TS2 | 66.31 |
| IC1 | -27.08 | P1 | -2.76 |

Table S6. The reaction energy (E) for Step 2 and Step 4 reactions in DME using CCSD(T) method.

| Complex | E (kcal/mol) | Complex | E (kcal/mol) |
| --- | --- | --- | --- |
|  | Step 2 |  | Step 4 |
| RCDME | 0.00 | IC2DME | 0.00 |
| TS1DME | 54.99 | TS2DME | 64.06 |
| IC1DME | -13.17 | P1DME | -6.02 |