Heterogenization of water-soluble porphyrins in Ti/TiO2 nanotubes electrodes: experimental and theoretical insights for atrazine degradation

Ana Luísa Almeida Lagea, Juliana Martins Ribeirob, Tairine Fernanda da Silva Magalhãesc, Elaine Maria de Souza-Fagundesb, Mateus Fernandes Venânciod, Michelle Fernanda Brugnerac, Dayse Carvalho da Silva Martinsa

a Departamento de Química, Instituto de Ciências Exatas, Universidade Federal de Minas Gerais, 31270-901, Belo Horizonte, MG, Brazil

b Departamento de Fisiologia e Biofísica, Instituto de Ciências Biológicas, Universidade Federal de Minas Gerais, 31270-901, Belo Horizonte, MG, Brazil

c Departamento de Química, Instituto de Ciências Exatas, Universidade Federal do Mato Grosso, 78060-900, Cuiabá, MT, Brazil

dDepartamento de Físico-Química, Instituto de Química, Universidade Federal da Bahia, Campus Universitário de Ondina, 40170-110, Salvador, BA, Brazil

Corresponding author: Dayse Carvalho da Silva Martins

E-mail: daysequimica@ufmg.br

Supplementary Material

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure S1. ﻿UV–vis spectra of (a) pure Ti/TiO2, (b) Ti/TiO2-H2P, (c) Ti/TiO2-MnP1, and (d) Ti/TiO2-MnP2 electrodes; the corresponding ﻿plot’s for band gap energy data obtained from diffuse reflectance (inset) of each electrode.

Figure S2. ﻿ Photocurrent vs. potential curves obtained (a) without irradiation and for (b) Ti/TiO2 bare, (c) Ti/TiO2-H2P, (d) Ti/TiO2-MnP1, and (e) Ti/TiO2-MnP2 under UV illumination in 0.01 mol L-1 NaCl, scan rate = 10 mV s-1.

Table S1. Atrazine degradation through the photolysis, photocatalysis (PC), and  photoelectrocatalysis (PEC) reactions mediated by porphyrin-modified Ti-TiO2 electrodes after 60 minutes.

| Systems | Atrazine degradation (%) |
| --- | --- |
| Photolysis | 92 |
| Ti/TiO2 (PC) | 86 |
| Ti/TiO2-H2P (PC) | 80 |
| Ti/TiO2-MnP1 (PC) | 92 |
| Ti/TiO2-MnP2 (PC) | 89 |
| Ti/TiO2 (PEC) | 91 |
| Ti/TiO2-H2P (PEC) | 91 |
| Ti/TiO2-H2P (PEC) (in surface water) | 91 |
| Ti/TiO2-MnP1 (PEC) | 87 |
| Ti/TiO2-MnP2 (PEC) | 74 |

Table S2. The kinetics plots for first-order or second order for atrazine degradation light-mediated through photolysis (PH), photocatalysis (PC), and photoelectrocatalysis (PEC) in the presence of Ti/TiO2 or Ti/TiO2-porphyrins electrodes

| System | Kinetics plots |
| --- | --- |
| Photolysis (PH) |  |
| Ti/TiO2 (PC) |  |
| Ti/TiO2-MnP1 (PC) |  |
| Ti/TiO2-MnP2 (PC) |  |
| Ti/TiO2 (PEC) |  |
| Ti/TiO2-MnP1 (PEC) |  |
| Ti/TiO2-MnP2 (PEC) |  |
| Ti/TiO2-H2P (PC) |  |
| Ti/TiO2-H2P (PEC) |  |
| Ti/TiO2-H2P (PEC) (in surface water) |  |

Table S3. Photo(electron)catalytic systems for atrazine degradation.

| Methods | Catalyst | Conditions | Atrazine degradation (%)a | Kinetic constantsa | Orderb | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Photoelectrocatalysis | TiO2 nanotube arrays | Illumination intensity of 80 mW cm−2, magnetic stirring, 0.01 M Na2SO4 as the electrolyte. The initial [atrazine] was 10 mg L−1. | ~ 50 (60 min) | 0.704 h-1 | Pseudo-first | Lu et al. (2008) |
| Photoelectrocatalysis | B-doped (1.5 at.%) TiO2 nanotube arrays |  | ~ 65 (60 min) | 0.863 h-1 | Pseudo-first | Lu et al. (2008) |
| Photoelectrocatalysis | B-doped (3.8 at.%) TiO2 nanotube arrays |  | ~ 65 (60 min) | 0.907 h-1 | Pseudo-first | Lu et al. (2008) |
| Photoelectrocatalysis | B-doped (3.1 at.%) TiO2 nanotube arrays |  | ~ 65 (60 min) | 1.08 h-1 | Pseudo-first | Lu et al. (2008) |
| Photocatalysis only | B-doped (3.1 at.%) TiO2 nanotube arrays |  | ~ 55% (60 min) | 0.705 h-1 | nd | Lu et al. (2008) |
| Photolysis only | B-doped (3.1 at.%) TiO2 nanotube arrays |  | ~ 35% (60 min) | 0.420 h-1 | nd | Lu et al. (2008) |
| Electrochemical only | B-doped (3.1 at.%) TiO2 nanotube arrays |  | < 5 (60 min) | 0.0186 h-1 | nd | Lu et al. (2008) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays | 500 W xenon lamp irradiation, magnetic stirring. The initial [atrazine] was 5 mg L−1. | ~ 15 (60 min) ~ 22 (120 min) | 0.0054 min-1 (pH = 2; current of 0.02A; 0.1 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays |  | ~ 22 (60 min) ~ 45 (120 min) | 0.0037min-1 (pH = 4; current of 0.02A; 0.1 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays | 500 W xenon lamp irradiation, magnetic stirring. The initial [atrazine] was 5 mg L−1. | ~ 50 (60 min) ~75 (120 min) | 0.0084 min-1 or 0.01168 min-1 (pH = 6; current of 0.02A; 0.1 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays |  | ~ 10 (60 min) ~ 22 (120 min) | 0.0025 min-1 or 0.01151 (pH = 8; current of 0.02A; 0.1 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays | 500 W xenon lamp irradiation, magnetic stirring. The initial [atrazine] was 5 mg L−1. | ~ 17 (60 min) ~ 25 (120 min) | 0.00222 min-1 (pH = 6; current of 0.01A; 0.1 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays |  | ~ 37 (60 min) ~ 60 (120 min) | 0.076 min-1 (pH = 6; current of 0.04A; 0.1 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays | 500 W xenon lamp irradiation, magnetic stirring. The initial [atrazine] was 5 mg L−1. | ~ 25 (60 min) ~ 48 (120 min) | 0.00414 min-1 (pH = 6; current of 0.06A; 0.1 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays |  | ~ 17 (60 min) ~ 30 (120 min) | 0.0032 min-1 (pH = 6; current of 0.06A; 0.01 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays | 500 W xenon lamp irradiation, magnetic stirring. The initial [atrazine] was 5 mg L−1. | ~ 32 (60 min) ~ 55 (120 min) | 0.00686 min-1 (pH = 6; current of 0.06A; 0.05 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | Boron-fluorine co-doped TiO2 nanotube arrays |  | ~ 27 (60 min) ~ 43 (120 min) | 0.00487 min-1 (pH = 6; current of 0.06A; 0.5 M Na2SO4 as the electrolyte) | nd | Wang et al (2019a) |
| Photoelectrocatalysis | TiO2 nanotubes | Light intensity: 100 mW cm-2, 0.1 M Na2SO4; The initial [atrazine] was 2 ppm; - 1.3 eV. | 73.1 (300 min) | 0.265 h-1 | nd | Wang et al (2019b) |
| Photoelectrocatalysis | Pd quantum dots modified TiO2 nanotubes |  | 99.5 (300 min) | 1.036 h-1 | Pseudo-first | Wang et al (2019b) |
| Electrochemical only | TiO2 nanotubes | 0.1 M Na2SO4; The initial [atrazine] was 2 ppm; - 1.3 eV. | ~ 59 (300 min) | ~ 0.170 h-1 | nd | Wang et al (2019b) |
| Electrochemical only | Pd quantum dots modified TiO2 nanotubes |  | 96.0 (300 min) | 0.604 h-1 | Pseudo-first | Wang et al (2019b) |
| Photoelectrocatalysis | Pd quantum dots modified TiO2 nanotubes | 0.1 M Na2SO4; The initial [atrazine] was 2 ppm; - 0.5 eV. | 24.1 (300 min) | 0.060 h-1 | Pseudo-first | Wang et al (2019b) |
| Electrochemical only | Pd quantum dots modified TiO2 nanotubes |  | 2.3 (300 min) | 0.006 h-1 | Pseudo-first | Wang et al (2019b) |
| Photoelectrocatalysis | Pd quantum dots modified TiO2 nanotubes | 0.1 M Na2SO4; The initial [atrazine] was 2 ppm; - 0.9 eV. | 83.9 (300 min) | 0.329 h-1 | Pseudo-first | Wang et al (2019b) |
| Electrochemical only | Pd quantum dots modified TiO2 nanotubes |  | 32.6 (300 min) | 0.092 h-1 | Pseudo-first | Wang et al (2019b) |
| Photoelectrocatalysis | Pd quantum dots modified TiO2 nanotubes | 0.1 M Na2SO4; The initial [atrazine] was 2 ppm; - 1.5 eV. | 93.4 (300 min) | 0.541 h-1 | Pseudo-first | Wang et al (2019b) |
| Electrochemical only | Pd quantum dots modified TiO2 nanotubes |  | 97.6 (300 min) | 0.791 h-1 | Pseudo-first | Wang et al (2019b) |
| Photocatalysis only | Pd quantum dots modified TiO2 nanotubes | 0.1 M Na2SO4; The initial [atrazine] was 2 ppm. | 17.8 (300 min) | 0.032 h-1 | nd | Wang et al (2019b) |
| Photocatalysis only | Ti/TiO2 | UV radiation using a Hg lamp; the initial [atrazine] was 3.0 x 10-5 M; 0.05 M NaCl. | 86 (60 min) | 54.357 L mol-1 s-1 | Second | This work |
|  | Ti/TiO2-H2P |  | 80 (60 min) | 32.881 L mol-1 s-1 | Second | This work |
|  | Ti/TiO2-MnP1 |  | 92 (60 min) | 0.0006 s-1 | First | This work |
|  | Ti/TiO2-MnP2 |  | 89 (60 min) | 0.0005 s-1 | First | This work |
| Photoelectrocatalysis | Ti/TiO2 |  | 91 (60 min) | 90.832 L mol-1 s-1 | Second | This work |
|  | Ti/TiO2-H2P |  | 91 (60 min) | 94.077 L mol-1 s-1 | Second | This work |
|  | Ti/TiO2-MnP1 |  | 87 (60 min) | 58.383 L mol-1 s-1 | Second | This work |
|  | Ti/TiO2-MnP2 |  | 74 (60 min) | 0.0004 s-1 | First | This work |
|  | Ti/TiO2-H2P in surface water |  | 91 (60 min) | 0.0006 s-1 | First | This work |

a (~) was used since the data were collected by the presented graphs by visual deduction; b “nd”: not described by the authors.

References

Lu N, Zhao H, Li J et al (2008) ﻿Characterization of boron-doped TiO2 nanotube arrays prepared by electrochemical method and its visible light activity. Sep Purif Technol. ﻿Doi:10.1016/j.seppur.2008.03.021

Wang HX, Zhu LN, Gui FG (2019a) ﻿Photoelectrocatalytic degradation of atrazine by boron-fluorine co-doped TiO2 nanotube arrays. Environ Sci Pollut Res. ﻿https://doi.org/10.1007/s11356-018-2569-y

Wang H, Li J, Shi H et al (2019b) Enhanced photoelectrocatalytic reduction and removal of atrazine: effect of co-catalyst and cathode potential. ACS Appl Mater Interfaces. DOI: 10.1021/acsami.9b12139