Electronic Supplementary Information

Photocatalysis of bifunctional Cr- and Fe-doped CeO2 nanoparticles toward selective oxidation of 
5-hydroxymethylfurfural and decomposition of 
high-density polyethylene

Jeong-Woo Nam,a,‡ Vy Ngoc Pham,b,‡ Jeong Min Ha,a Minjeong Shin,c,* Hangil Lee,b,* and Young-Sang Youna,*

aDepartment of Chemistry, Yeungnam University, Daehak-ro 280, Gyeongsan, Gyeongbuk 38541, Republic of Korea, bDepartment of Chemistry, Sookmyung Women's University, Seoul 04310, Republic of Korea, cSchool of Chemistry and Energy, Sungshin Women's University, 55, Dobong-ro 76 ga-gil, Gangbuk-gu, Seoul 01133, Republic of Korea

*Corresponding Author

E-mail : mshin@sungshin.ac.kr (M. Shin), easyscan@sookmyung.ac.kr (H. Lee), 
ysyoun@yu.ac.kr (Y.-S. Youn)

‡These authors contributed equally.

Figure S1. STEM-EDS data of (a) CeO2, (b) Cr@CeO2, and (c) Fe@CeO2 NPs.

Figure S2. SEM images of pristine HDPE (a) before and (b) after UV light exposure, and those of HDPE irradiated with UV light in the presence of (c) CeO2, (d) Cr@CeO2, and (e) Fe@CeO2 NPs, in which the estimated average particle sizes were 18.5, 17.6, 14.0, 10.0, and 10.4 μm, respectively.

Figure S3. FT-IR spectra obtained from pristine HDPE before and after exposure to UV light; the transmittance at peak A was measured as 45.2 and 48.9 %, respectively.