Layer-by-Layer Assembly of Cationic Guar Gum, Cellulose Nanocrystals and Hydroxypropyl methylcellulose based Multilayered Composite Films

Arun Sainia, Deepak Sharmab, Yuanyuan Xiaa, Aman Sainic, Xiangyu Youa, Ying Sud, Lihong Chene, Chandravati Yadava,* and Xinping Lia,*

aShaanxi Provincial Key Laboratory of Papermaking Technology and Specialty Paper Development, College of Bioresources Chemical and Materials Engineering, Shaanxi University of Science & Technology, Xi'an, Shaanxi 710021, China

bChemistry and Bioprospecting Division, Forest Research Institute (Indian Council of Forestry Research and Education) Dehradun, Uttarakhand 248006, India

cDepartment of Chemistry, Maharaj Singh College, Chaudhary Charan Singh University, Meerut, Uttar Pradesh 250001, India

dKey Laboratory of Auxiliary Chemistry and Technology for Chemical Industry, Ministry of Education, Shaanxi University of Science & Technology, Xi'an, Shaanxi 710021, China

eFront-line Science and Technology Transfer Institute, Shaanxi University of Science & Technology, Xi'an, Shaanxi 710021, China

Fig. S1. Schematic of mixed-acid assisted hydrothermal process for the preparation of carboxylated cellulose nanocrystals (cCNCs).

Fig. S2. (A) TEM image of cCNCs and (B) AFM images of cCNCs (a) topography image, 3D image and (a’) phase image

Table S1. Solvent uptake ability of CGg/cCNCs/HPMC multilayer composite film.

| Time (h) | Solvent uptake (wt%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Water | Acetone | THF | DMAc |
| 6 | 542.13 | 1.03 | 5.14 | 3.13 |
| 12 | n.a. | 3.08 | 9.60 | 5.31 |
| 24 | n.a. | 4.19 | 11.51 | 14.76 |
| 48 | n.a. | 6.73 | 13.34 | 16.95 |