2D/2D g-C3N4/BiOCl with oxygen vacancy heterostructure by grinding for improved visible-light-driven photocatalyst

Jianhua Hou 1 ⁎, Haoyi Wang 1, Rongrong Qin 2, Qikai Zhang 2, Di Wu 3, Zhenhua Hou3⁎, Wei Yang 4, Muhammad Tahir, 5 Asif Hussain 1, Weiqin Yin 1, Yongcai Zhang 1, Xiaozhi Wang1 ⁎

1 College of Environmental Science and Engineering, Yangzhou University, Yangzhou, 225000, China

2.  Beijing Xinfeng Aerospace Equipment Co., Ltd, Beijing, 100854, China

3 Jiangxi Xinda Hangke New Materials Technology Co., Ltd, Nanchang, 330096, China

4 Beijing System Design Institute of Electro-Mechanic Engineering, Beijing,100005, China

5 Department of Physics, Division of Science & Technology, University of Education, Lahore, Pakistan

∗ Corresponding author, E-mail address: jhhou@yzu.edu.cn (J. Hou), houzhenhualove@126.com (Z. Hou), xzwang@yzu.edu.cn (X.Wang)

Experimental section

1. Materials

Analysis of pure grades of dicyandiamide (C2H4N4), thiourea (CH4N2S), RhB, methyl orange (MO), Bismuth nitrate pentahydrate (Bi(NO3)3 5H2O) and Potassium chloride (KCl)were purchased from Sinopagic Chemical Reagents Co., LTD. Carbon dioxide (CO2) ≥ 99.99% purchased from Nanjing Special Gas Co., LTD.

2. Characterization

On the AXS D-8 ADVANCE, X-ray diffraction (XRD) was performed using Cu K radiation (= 1.5406 Å) with a 5 ͦ Hz scanning rate. TENSOR27 spectrometer was used to study FT-IR (Fourier Transform Infrared Spectroscopy) spectra. Brunauer-Emmett-Teller technique was used to estimate the surface area and pore size using (ASAP 2460, Micromeritics). X-ray photoelectrons spectroscopy (XPS) was utilized to figure out the chemical structure of the material and the surface element state (ESCALAB 250Xi, Thermo Fisher Scientific). Employing scanning electron microscopy (SEM) (Hitachi, S-4800) with high-resolution transmission electron microscopy (HRTEM), the surface nanostructures and morphology of the prepared trials were examined at high resolution with (Tecnai G2 F30S-Twin, FEI). A300-10/12 Bruker EPR spectrometer was used to study EPR (electron paramagnetic resonance). Investigation of optical properties was done using UV–visible diffuse reflectance spectroscopy (UV–vis DRS) (TU-1901, PERSEE). Renishaw in Via was used to investigate photoluminescence (PL). The FLS980 Series of Fluorescence Spectrometers was used in conjunction with a 325 nm pulsed laser diode to measure time-resolved photoluminescence (TRPL) decay curves. By using a typical three-electrode system of Ag/AgCl as the reference electrode, ITO conductive glass containing 5 mg of catalyst sample as the working electrode in 0.2 M Na2SO4 solution, and Pt as the counter electrode, the transient photo-current response and EIS (electrochemical impedance spectra) were tested. The AC voltage was 5 mV; the EIS frequency ranged from 0.01 to 100000 Hz.

Fig. S1 plots of (ahv)1/2 versus hv of all samples.

Fig. S2 SEM images of (a) BOC, (b) CN/BOC-2, (c) CN/BOC-5 and (d) CN/BOC-10.

Fig. S3 (a) Photocatalytic degradation and (b) -ln(C/C0) of RhB.

Table S1 Comparison of photocatalytic degradation of CN/BOC-5 (g-C3N4/ BiOCl-5) with other photocatalysts.

| Photocatalyst | Ccatalyst |  | Cdye | Degradation efficiency | Light source (Xe lamp) | Ref. |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| g-C3N4/Bi5O7I |  | 1.0 g·L-1 | MO, 6.5 mg·L-1 | 270 min, ca. 98% | 500 W, λ > 420 nm |  | S1 |
| floating porous g-C3N4 |  | 2 g/L | TC, 5 mg·L-1 | 240 min, ca. 70% | 300 W,λ > 420 nm |  | S2 |
| BiOI(001)/ g-C3N4 (002) |  | 1.0 g·L-1 | RhB, 100 mg·L-1 | 240 min, ca. 90% | 300 W, λ > 420 nm |  | S3 |
| 10%Bi-Ox-CN |  | 1.0 g·L-1 | TC,20 mg L−1 | 180 min, ca. 90% | 350 W,λ > 420 |  | S4 |
| CeO2/g-C3N4-3 |  | 1.0 g·L-1 | BPA, 10 mg·L-1 | 80 min, ca. 94% | 300 W, λ > 420 nm |  | S5 |
| BiOI/g-C3N4/CeO2 |  | 1.6 g·L-1 | TC, 20 mg·L-1 | 120 min, ca. 90% | 300 W, λ > 420 nm |  | S6 |
| g-C3N4/MnO2/GO |  | 0.5 g g·L-1 | TC,10 mg/L | 60 min, 91.4% min | 300 W, λ > 420 nm |  | S7 |
| ZnO-g-C3N4-Go |  | 0.3 g·L-1 | RhB, 10 mg·L-1 | 100min, 98% | 350 W |  | S8 |
| H2O2+3 %Fe- MOF/C3N4 |  | 0.375 g·L-1 | TC, 10 mg/L | 60 min, 100% | 300 W, (λ > 420 nm) |  | S9 |
| G/CN-Co (3%) |  | 0.5 g·L-1 | MB, 10 mg·L-1 | 210 min, ca. 97% | 300 W, λ > 420 nm |  | S10 |
| g-C3N4/BiOCl |  | 0.2 g·L-1 | RhB, (0.02 mmol/L) | 120 min 96% | LED (5 W) |  | S11 |
| BiOCl/g-C3N4 nanosheets |  | 1 g·L-1 | RhB,10 mg/L | 80 min, 96% | 300 W, λ > 420 nm |  | S12 |
| rich OVs-BiOCl |  | 1 g·L-1 | TC, 10 mg L-1 | 40 min, < 70% | 500W,λ>420nm |  | S13 |
| CN/BOC-5 |  | 0.4 g·L-1 | RhB, 10 mg L-1, TC, 10 mg L-1 | 60 min, 87.5% 120 min, 89.8% | 500W, λ > 420 nm |  | Thiswork |

Table S2 Comparison of CO2 reduction performance of CN/BOC-5 (g-C3N4/ BiOCl-5) with other g-C3N4-based systems

| Photocatalyst | Light source |  | Reaction medium | Performance (µmol g-1 h-1) | Ref. |
| --- | --- | --- | --- | --- | --- |
| OCN-Tube |  | λ > 420 nm 350 W Xe lamp | CO2 gas and H2O vapor | 0.88, CH3OH | S14 |
| P-CeO2/g-C3N4 |  | 300 W Xe lamp | CO2 gas and H2O vapor | 0.523 ,CO, | S15 |
| g-C3N4/WO3 |  | 500W Xe lamp | CO2 gas and H2O vapor | 0.83, CO | S16 |
| g-C3N4/Ag/ m-CeO2 |  | 8 W UV-light lamp | 0.1M NaOH/TEOA | 0.74 ,CO 1.94, CH4 | S17 |
| B-doped 12-FLTC/BCN |  | 300 W Xe lamp | CO2 gas and H2O vapor | 2.88, CO | S18 |
| Alkali-decorated g-C3N4 |  | 300 W Xe lamp (λ≥420 nm) | CO2 reduction | 0.90,CO, 0.28, CH4, 0.68, CH3OH | S19 |
| Ti3C2/porous g-C3N4 |  | 300 W Xe lamp: (λ>420 nm) | CO2 gas and 15 mL H2O | CO: trace CH4:0.99 μmol g -1 h -1 | S20 |
| g-C3N4/LaFeO3 |  | 300 W Xe lamp | CO2 gas and H2O vapor | 5, CO 1.25, CH4 | S21 |
| CN/BOC-5 |  | 300W Xe lamp | CO2 gas and H2O vapor | 2.00, CO | This work |

References

[S1] Wang Q, Li Y, Huang L, Zhang F, Wang H, Wang C, Zhang Y, Xie M, Li H (2019) Enhanced photocatalytic degradation and antibacterial performance by GO/CN/BiOI composites under LED light. Appl Surf Sci (497):143753.

[S2] Tang J, Wang J, Tang L, Feng C, Zhu X, Yi Y, Feng H, Yu J, Ren X (2022) Preparation of floating porous g-C3N4 photocatalyst via a facile one-pot method for efficient photocatalytic elimination of tetracycline under visible light irradiation. Chem Eng J( 430):132669.

[S3] Yang Y, Bian Z, Zhang L, Wang H (2022) Bi@BiOx(OH)y modified oxidized g-C3N4 photocatalytic removal of tetracycline hydrochloride with highly effective oxygen activation. J Hazard Mater (427):127866.

[S4] Tian N, Huang H, Wang S, Zhang T, Du X, Zhang Y (2020) Facet-charge induced coupling dependent interfacial photocharge separation: A case of BiOI/g-C3N4 p-n junction. Appl Catal B (267) 118697.

[S5] Ma R, Zhang S, Li L, Gu P, Wen T, Khan A, Li S, Li B, Wang S, Wang X (2019) Enhanced Visible-Light-Induced Photoactivity of Type-II CeO2/g‑C3N4 Nanosheet toward Organic Pollutants Degradation. ACS Sustain Chem Eng(7): 9699-9708.

[S6] Jiang X, Lai S, Xu W, Fang J, Chen X, Beiyuan J, Zhou X, Lin K, Liu J, Guan G, (2019) Novel ternary BiOI/g-C3N4/CeO2 catalysts for enhanced photocatalytic degradation of tetracycline under visible-light radiation via double charge transfer process. J Alloys Compd (809): 151804.

[S7] Du C, Zhang Z, Tan S, Yu G, Chen H, Zhou L, Yu L, Su Y, Zhang Y, Deng F, Wang S (2021) Construction of Z-scheme g-C3N4/MnO2/GO ternary photocatalyst with enhanced photodegradation ability of tetracycline hydrochloride under visible light radiation. Environ Res (200): 111427.

[S8] Zhang J, Li J, Liu X (2021) Ternary nanocomposite ZnO-g-C3N4-Go for enhanced photocatalytic degradation of RhB. Opt Mater (119): 111351.

[S9] Pan Y, Hu X, Bao M, Li F, Li Y, Lu J (2021) Fabrication of MIL-Fe (53)/modified g-C3N4 photocatalyst synergy H2O2 for degradation of tetracycline. Sep Purif Technol (279):119661.

[S10] Yang X, Tian Z, Chen Y, Huang H, Hu J (2020) One-pot calcination preparation of graphene/g-C3N4-Co photocatalysts with enhanced visible light photocatalytic activity. Int J Hydrog Energy (45):12889-12902.

[S11] Zhang R, Niu S, Xiang J, Zheng J, Jiang Z, Guo C (2021) Band-potential fluctuation in C3N4/BiOCl hetero-junction for boosting photo-catalytic activity. Sep Purif Technol (261):118258.

[S12] Zhang X, An D, Feng D, Liang F, Chen Z, Liu W, Yang Z, Xian M (2019) In situ surfactant-free synthesis of ultrathin BiOCl/g-C3N4 nanosheets for enhanced visible-light photodegradation of rhodamine B. Appl Surf Sci( 476):706-715.

[S13] Yang C, He Y, Zhong J, Li J (2022) hotocatalytic performance of rich OVs-BiOCl modified by polyphenylene sulfide, Adv Powder Technol (33): 103427.

[S14] Fu J, Zhu B, Jiang C, Cheng B, You W, Yu J (2017) Hierarchical Porous O-Doped g-C3N4 with Enhanced Photocatalytic CO2 Reduction Activity. Small (13) 1603938.

[S15] Li W, Jin L, Gao F, Wan H, Pu Y, Wei X, Chen C, Zou W, Zhang C, L Dong, (2021) Advantageous roles of phosphate decorated octahedral CeO2 {111}/g-C3N4 in boosting photocatalytic CO2 reduction: charge transfer bridge and Lewis basic site. Appl Catal B(294): 120257.

[S16] Huang S, Long Y, Ruan S, Zeng Y (2019) Enhanced Photocatalytic CO2 Reduction in Defect-Engineered Z-Scheme WO3–x/g-C3N4 Heterostructures. ACS Omega (4):15593-15599.

[S17] Wang H, Guan J, Li J, Li X, Ma C, Huo P, Yan Y (2020) Fabricated g-C3N4/Ag/m-CeO2 composite photocatalyst for enhanced photoconversion of CO2. Appl Surf Sci(506):144931.

[S18] Wang H, Tang Q, Wu Z (2021) Construction of Few-Layer Ti3C2 MXene and Boron-Doped g-C3N4 for Enhanced Photocatalytic CO2 Reduction. ACS Sustain Chem Eng(9): 8425-8434.

[S19] Sun Z, Fischer J, Li Q, Hu J, Q Tang, Wang H, Wu Z, Hankel M, Searles D, Wang L (2017) Enhanced CO2 photocatalytic reduction on alkali-decorated graphitic carbon nitride. Appl Catal B (216):146-155.

[S20] Hu J, Ding J, Zhong, Q (2021) Ultrathin 2D Ti3C2 MXene Co-Catalyst Anchored on Porous g-C3N4 for Enhanced Photocatalytic CO2 Reduction under Visible-Light Irradiation. J Colloid Interface Sci (582):647-657.

[S21] Khan I, Luo M, Guo L, Khan S, Shah S, Khan I, Khan A, Wang C, Ai B, Zaman S (2022) Synthesis of phosphate-bridged g-C3N4/LaFeO3 nanosheets Z-scheme nanocomposites as efficient visible photocatalysts for CO2 reduction and malachite green degradation, Appl Catal A-Gen, (629): 118418.