Supplementary Information

Iron phosphide nanocrystals for highly active and stable heterogeneous catalysis of liquid-phase hydrogenation of nitrile

Tomohiro Tsuda,a Min Sheng,a Hiroya Ishikawa,a Seiji Yamazoe,b Jun Yamasaki,c Sho Yamaguchi,a Tomoo Mizugaki,a,d Takato Mitsudomea,e*

aDepartment of Materials Engineering Science, Graduate School of Engineering Science, Osaka University, 1-3 Machikaneyama, Toyonaka, Osaka 560-8531, Japan

bDepartment of Chemistry, Tokyo Metropolitan University, 1-1 Minami Osawa, Hachioji, Tokyo 192-0397, Japan

cResearch Center for Ultra-High Voltage Electron Microscopy, Osaka University, 7-1, Mihogaoka, Ibaraki, Osaka 567-0047, Japan

dInnovative Catalysis Science Division, Institute for Open and Transdisciplinary Research Initiatives, Osaka University, Suita, Osaka 565-0871, Japan

ePRESTO, Japan Science and Technology Agency, 4-1-8 Honcho, Kawaguchi, Saitama 333-0012, Japan

*Correspondence to: mitsudom@cheng.es.osaka-u.ac.jp

Table of Contents

1. Characterization and kinetic study

Supplementary Fig. 1 	Size distribution histograms (length and width) of Fe2P NCs.

Supplementary Fig. 2 	EDX analysis of the Fe2P NC in the areas marked by the yellow squares.

Supplementary Fig. 3 	P 2p XPS spectrum of Fe2P NCs.

Supplementary Fig. 4 	TEM images of Fe2P NC/TiO2, Fe2P NC/C, and Fe2P NC/SiO2 catalysts before and after the reaction.

Supplementary Fig. 5	Fe 2p XPS spectra of Fe2P NC/TiO2 before and after the reaction.

Supplementary Fig. 6	Arrhenius plot of the hydrogenation of benzonitrile using Fe2P NC/TiO2.

Supplementary Fig. 7 	Dependency of the initial reaction rate on the concentration of benzonitrile and the partial pressure of H2 using Fe2P NC/TiO2.

Supplementary Fig. 8 	H2–D2 exchange reactions of Fe2P NCs, Fe2P NC/TiO2, Fe2P NC/C, and Fe2P NC/ SiO2.

Supplementary Fig. 9		EXAFS fitting curves in k-space and R-space of Fe foil, bulk Fe2P, Fe2P NCs, and Fe2P NC/TiO2.

Supplementary Table 1	ICP-AES elemental analyses of Fe2P NCs and Fe2P NC/TiO2

Supplementary Table 2	Curve-fitting results of Fe K-edge EXAFS for Fe foil, bulk Fe2P, Fe2P NCs, and Fe2P NC/TiO2

2. Comparison of the catalytic activity of Fe2P NC/TiO2 with the previously reported catalyst

Supplementary Scheme 1 Comparison of the catalytic activity of Fe2P NC/TiO2 with the previously reported Fe catalyst for the nitrile hydrogenation reaction.

3. Product identification

4. 1H and 13C NMR spectra

5. References

1. Characterization and kinetic study

Supplementary Fig. 1|Size distribution histograms of Fe2P NCs. (left) Length and (right) width of Fe2P NC.

Supplementary Fig. 2|EDX analysis of the Fe2P NCs. The yellow squares indicate the analysis areas.

Supplementary Fig. 3|P 2p XPS spectrum of Fe2P NCs. The solid line is the obtained spectrum. The dashed lines indicate the result of the curve-fitting.

Supplementary Fig. 4|TEM images of supported Fe2P NC. (a, b) Fe2P NC/TiO2, (c, d) Fe2P NC/C, and (e, f) Fe2P NC/SiO2 catalysts before (left panels) and after (right panels) the reaction.

Supplementary Fig. 5|Fe 2p XPS spectra of Fe2P NC/TiO2. Before (orange line) and after (magenta line) the reaction.

Supplementary Fig. 6|Arrhenius plot of the hydrogenation of benzonitrile using Fe2P NC/TiO2. Reaction conditions: Fe2P NC/TiO2 (0.1 g, Fe: 1.9 mol%), benzonitrile (2 mmol), 2-propanol (3 mL), H2 (4 MPa), 432–453 K, 2 h.

Supplementary Fig. 7|Dependency of the initial reaction rate on the concentration of benzonitrile and the partial pressure of H2 using Fe2P NC/TiO2. a, Double logarithm plots of the concentration of benzonitrile and the initial reaction rate. b, Double logarithm plots of the partial pressure of H2 and the initial reaction rate. Reaction conditions: Fe2P NC/TiO2 (0.1 g, Fe: 1.9–15.2 mol%), benzonitrile (0.25–2 mmol), 2-propanol (3 mL), H2 (1–4 MPa), 453 K, 2 h.

Supplementary Fig. 8|H2–D2 exchange experiments. Yellow, orange, light blue, and yellow green show the results obtained by Fe2P NCs, Fe2P NC/TiO2, Fe2P NC/C, and Fe2P NC/SiO2, respectively.

Supplementary Fig. 9|Curve-fitting analysis of Fe K-edge EXAFS spectra of Fe foil, bulk Fe2P, Fe2P NCs, and Fe2P NC/TiO2. EXAFS fitting curves in (left) k-space and (right) R-space of (right blue) Fe foil, (yellow green) bulk Fe2P, (yellow) Fe2P NCs, and (orange) Fe2P NC/TiO2. The solid lines are the obtained spectra. The dashed lines show the fitting curves.

Supplementary Table 1|ICP-AES elemental analyses of Fe2P NCs and Fe2P NC/TiO2

| Sample | Element | Amount (wt%) | Fe/P (molar ratio) |
| --- | --- | --- | --- |
| Fe2P NCs | Fe | 76.6 | 2.09 |
|  | P | 20.4 |  |
| Fe2P NC/TiO2 before reaction | Fe | 2.30 | 1.62 |
|  | P | 0.79 |  |
| Fe2P NC/TiO2 after reaction | Fe | 2.11 | 1.56 |
|  | P | 0.75 |  |

Supplementary Table 2|Curve-fitting results of Fe K-edge EXAFS for Fe foil, bulk Fe2P, Fe2P NCs, and Fe2P NC/TiO2

| Sample | Shell | CNa | r (Å)b | D.W.c | R factor (%) |
| --- | --- | --- | --- | --- | --- |
| Fe foil | Fe–Fe | 7.3 ± 0.2 | 2.48 ± 0.02 | 0.006 ± 0.002 | 2.4 |
|  |  | 4.5 ± 0.2 | 2.86 ± 0.03 | 0.007 ± 0.003 |  |
| bulk Fe2P | Fe–P | 0.5 ± 0.1 | 2.24 ± 0.04 | 0.001 ± 0.001 | 10.5 |
|  | Fe–Fe | 1.8 ± 0.1 | 2.56 ± 0.03 | 0.003 ± 0.002 |  |
|  | Fe–Fe | 0.8 ± 0.2 | 2.69 ± 0.03 | 0.001 ± 0.001 |  |
| Fe2P NCs | Fe–P | 2.2 ± 0.2 | 2.23 ± 0.04 | 0.006 ± 0.004 | 5.0 |
|  | Fe–Fe | 3.7 ± 0.3 | 2.65 ± 0.03 | 0.011 ± 0.005 |  |
| Fe2P NC/TiO2 | Fe–P | 1.4 ± 0.2 | 2.22 ± 0.04 | 0.003 ± 0.002 | 6.1 |
|  | Fe–Fe | 4.2 ± 0.2 | 2.63 ± 0.03 | 0.010 ± 0.004 |  |

aCoordination number. bBond distance. cDebye–Waller factor.

2. Comparison of catalytic activity of Fe2P NC/TiO2 with the previously reported catalyst

Supplementary Scheme 1|Comparison of the catalytic activity of Fe2P NC/TiO2 with the previously reported Fe catalyst for the nitrile hydrogenation reaction.

3. Product identification

All reaction products were characterized by GC and NMR spectroscopy. The 1H and 13C NMR chemical shifts of the products agreed with those of authentic samples or previously reported values.

benzylamine hydrochloride (2a) [S2]

1H NMR (DMSO-d6, 400 MHz): δ = 8.49 (br s, 3H), 7.51–7.49 (m, 2H), 7.43–7.35 (m, 3H), 4.00 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 134.07, 128.88, 128.51, 128.35, 42.12.

o-methylbenzylamine hydrochloride (2b) [S3]

1H NMR (DMSO-d6, 400 MHz): δ = 8.59 (br s, 3H), 7.46–7.43 (m, 1H), 7.33–7.21 (m, 3H), 3.98 (s, 2H), 2.36 (s, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 136.64, 132.33, 130.26, 129.20, 128.41, 126.03, 39.39, 18.83.

m-methylbenzylamine hydrochloride (2c) [S3]

1H NMR (DMSO-d6, 400 MHz): δ = 8.45 (s, 3H), 7.32–7.28 (m, 3H), 7.20–7.18 (m, 1H), 3.96 (s, 2H), 2.32 (s, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 137.68, 133.98, 129.45, 128.94, 128.47, 125.91, 42.07, 20.92.

p-methylbenzylamine hydrochloride (2d) [S3]

1H NMR (DMSO-d6, 400 MHz): δ = 8.38 (s, 3H), 7.37 (d, J = 8.4 Hz, 2H), 7.22 (d, J = 8.4 Hz, 2H), 3.95 (s, 2H), 2.30 (s, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 137.64, 131.00, 128.97, 128.85, 41.80, 20.67.

p-tert-butylbenzylamine hydrochloride (2e) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.36 (s, 3H), 7.45–7.40 (m, 4H), 3.96 (s, 2H), 1.28 (s, 9H); 13C NMR (DMSO-d6, 100 MHz): δ = 150.95, 131.16, 128.68, 125.29, 41.82, 34.30, 31.02.

o-methoxybenzylamine hydrochloride (2f) [S2]

1H NMR (DMSO-d6, 400 MHz): δ = 8.17 (br s, 3H), 7.40–7.36 (m, 2H), 7.07–7.06 (m, 1H), 6.99–6.96 (m, 1H), 3.95 (q, J = 6.0 Hz, 2H), 3.83 (s, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 157.20, 130.30, 130.25, 121.60, 120.30, 110.93, 55.51, 37.69.

m-methoxybenzylamine hydrochloride (2g) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.62 (br s, 3H), 7.33–7.29 (m, 1H), 7.19 (s, 1H), 7.07–7.05 (m, 1H), 6.94–6.92 (m, 1H), 3.97 (s, 2H), 3.77 (s, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 159.29, 135.56, 129.62, 120.95, 114.48, 113.92, 55.19, 42.05.

p-methoxybenzylamine hydrochloride (2h) [S5]

1H NMR (DMSO-d6, 400 MHz): δ = 8.40 (s, 3H), 7.43 (d, J = 8.4 Hz, 2H), 6.96 (d, J = 8.4 Hz, 2H), 3.93 (s, 2H), 3.79 (s, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 159.22, 130.40, 125.86, 113.79, 55.07, 41.51.

o-chlorobenzylamine hydrochloride (2i) [S2]

1H NMR (DMSO-d6, 400 MHz): δ = 8.66 (br s, 3H), 7.68–7.63 (m, 1H), 7.56–7.52 (m, 1H), 7.45–7.41 (m, 2H), 4.12 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 132.86, 131.62, 130.65, 130.34, 129.45, 127.49, 39.43.

m-chlorobenzylamine hydrochloride (2j) [S3]

1H NMR (DMSO-d6, 400 MHz): δ = 8.63 (br s, 3H), 7.65 (s, 1H), 7.50–7.43 (m, 3H), 4.03 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 136.52, 133.04, 130.41, 128.91, 128.31, 127.75, 41.46.

p-chlorobenzylamine hydrochloride (2k) [S7]

1H NMR (DMSO-d6, 400 MHz): δ = 8.55 (br s, 3H), 7.58–7.47 (m, 4H), 4.01 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 133.11, 133.08, 130.95, 128.47, 41.35.

p-bromobenzylamine hydrochloride (2l) [S7]

1H NMR (DMSO-d6, 400 MHz): δ = 8.53 (br s, 3H), 7.63 (d, J = 8.0 Hz, 2H), 7.46 (d, J = 8.0 Hz, 2H), 4.00 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 133.53, 131.39, 131.24, 121.66, 41.42.

p-fluorobenzylamine hydrochloride (2m) [S2, S8]

1H NMR (DMSO-d6, 400 MHz): δ = 8.47 (br s, 3H), 7.59–7.54 (m, 2H), 7.28–7.23 (m, 2H), 4.01 (q, J = 6.0 Hz, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 162.07 (d, J = 244.0 Hz), 131.34 (d, J = 8.6 Hz), 130.36 (d, J = 2.9 Hz), 115.35 (d, J = 21.9 Hz), 41.38.

2,4-difluorobenzylamine hydrochloride (2n) [S9]

1H NMR (D2O, 400 MHz): δ = 7.46–7.40 (m, 1H), 7.04–6.97 (m, 2H), 4.17 (s, 2H); 13C NMR (D2O, 100 MHz): δ = 165.05 (dd, J = 246.9, 12.4 Hz), 162.75 (dd, J = 247.9, 12.4 Hz), 134.08 (dd, J = 10.4, 4.7 Hz), 117.40 (dd, J = 15.2, 3.8 Hz), 113.65 (dd, J = 22.0, 3.8 Hz), 105.84 (dd, J = 25.7, 25.7 Hz), 38.19 (d, J = 3.8 Hz).

3,4-dichlorobenzylamine hydrochloride (2o) [S7]

1H NMR (CD3OD, 400 MHz): δ = 7.70 (s, 1H), 7.64 (d, J = 8.4 Hz, 1H), 7.43 (d, J = 8.4 Hz, 1H), 4.15 (s, 2H); 13C NMR (CD3OD, 100 MHz): δ = 135.02, 134.31, 133.97, 132.32, 132.29, 130.00, 43.14.

p-(trifluoromethyl)benzylamine hydrochloride (2p) [S5]

1H NMR (DMSO-d6, 400 MHz): δ = 8.48 (s, 3H), 7.81 (d, J = 8.0 Hz, 2H), 7.72 (d, J = 8.0 Hz, 2H), 4.14 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 138.76, 129.71, 128.62 (q, J = 31.5 Hz), 125.42 (q, J = 3.8 Hz), 122.76, 41.64.

p-aminobenzylamine hydrochloride (2q) [S10, S11]

1H NMR (DMSO-d6, 400 MHz): δ = 8.46 (br s, 3H), 7.53 (d, J = 8.4 Hz, 2H), 7.30 (d, J = 8.4 Hz, 2H), 4.00 (q, J = 6.0 Hz, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 134.70, 131.84, 130.31, 121.90, 41.63.

p-(N,N-dimethylamino)benzylamine hydrochloride (2r) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.29 (br s, 3H), 7.36 (d, J = 8.0 Hz, 2H), 6.95 (br s, 2H), 3.90 (q, J = 5.2 Hz, 2H), 2.94 (s, 6H); 13C NMR (DMSO-d6, 100 MHz): δ = 148.01, 130.22, 115.32, 41.94, 41.70.

p-(methylthio)benzylamine hydrochloride (2s) [S1]

1H NMR (DMSO-d6, 400 MHz): δ = 8.32 (br s, 3H), 7.42 (d, J = 8.4 Hz, 2H), 7.30 (d, J = 8.4 Hz, 2H), 3.97 (s, 2H), 2.51–2.50 (m, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 138.72, 130.40, 129.58, 125.83, 41.75, 14.59.

p-phenyoxybenzylamine hydrochloride (2t) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.43 (s, 3H), 7.53–7.51 (m, 2H), 7.43–7.39 (m, 2H), 7.19–7.15 (m, 1H), 7.05–7.00 (m, 4H), 3.99 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 156.83, 156.34, 130.97, 130.11, 129.04, 123.69, 118.72, 118.49, 41.56.

3,4-methylenedioxybenzylamine hydrochloride (2u) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.29 (br s, 3H), 7.09 (s, 1H), 6.97–6.93 (m, 2H), 6.04 (s, 2H), 3.92 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 147.28, 127.59, 122.83, 109.40, 108.26, 101.20, 42.02.

2-phenylethaneamine hydrochloride (2v) [S12]

1H NMR (DMSO-d6, 400 MHz): δ = 8.07 (br s, 3H), 7.35–7.31 (m, 2H), 7.27–7.25 (m, 3H), 3.04–2.99 (m, 2H), 2.92–2.88 (m, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 137.32, 128.54, 128.51, 126.60, 39.79, 32.86.

p-phenylbenzylamine hydrochloride (2w) [S4, S13]

1H NMR (DMSO-d6, 400 MHz): δ = 8.61 (br s, 3H), 7.73–7.59 (m, 6H), 7.50–7.46 (m, 2H), 7.40–7.37 (m, 1H), 4.06 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 140.20, 139.52, 133.28, 129.58, 128.98, 127.68, 126.77, 126.69, 41.82.

1-naphthalenemethylamine hydrochloride (2x) [S14]

1H NMR (DMSO-d6, 400 MHz): δ = 8.39 (br s, 3H), 8.16–8.14 (m, 1H), 8.03–7.98 (m, 2H), 7.67–7.55 (m, 4H), 4.53 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 133.23, 130.64, 129.94, 129.11, 128.66, 127.27, 126.74, 126.26, 125.35, 123.42, 38.94.

4-picolylamine hydrochloride (2y) [S11]

1H NMR (DMSO-d6, 400 MHz): δ = 9.06 (br s, 3H), 8.92 (d, J = 6.4 Hz, 2H), 8.08 (d, J = 6.4 Hz, 2H), 4.33 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 151.68, 143.29, 125.77, 41.03.

3-picolylamine hydrochloride (2z) [S15]

1H NMR (DMSO-d6, 400 MHz): δ = 8.95 (s, 1H), 8.83–8.81 (m, 1H), 8.68 (br s, 3H), 8.47–8.43 (m, 1H), 7.92–7.88 (m, 1H), 4.21 (q, J = 6.0 Hz, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 145.11, 143.70, 142.77, 133.34, 126.26, 39.02.

5-aminomethylindole (2aa) [S16, S17]

1H NMR (DMSO-d6, 400 MHz): δ = 10.95 (s, 1H), 7.43 (s, 1H), 7.33–7.27 (m, 2H), 7.04 (d, J = 8.4 Hz, 1H), 6.35 (s, 1H), 3.78 (br s, 2H), 1.78 (br s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 134.85, 127.54, 125.18, 121.04, 118.12, 110.95, 100.82, 46.30.

furfurylamine hydrochloride (2bb) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.50 (br s, 3H), 7.73–7.72 (m, 1H), 6.56–6.55 (m, 1H), 6.50–6.49 (m, 1H), 4.06 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 147.59, 143.71, 111.04, 110.43, 35.10.

2-thiophenemethylamine hydrochloride (2cc) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.57 (br s, 3H), 7.58–7.57 (m, 1H), 7.29–7.28 (m, 1H), 7.08–7.06 (m, 1H), 4.21 (s, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 135.33, 129.08, 127.24, 127.20, 36.62.

1-pentanamine hydrochloride (2dd) [S18]

1H NMR (DMSO-d6, 400 MHz): δ = 8.04 (s, 3H), 2.73 (t, J = 7.6 Hz, 2H), 1.56–1.54 (m, 2H), 1.30–1.28 (m, 4H), 0.87–0.86 (m, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 38.55, 27.86, 26.47, 21.50, 13.60.

1-octanamine hydrochloride (2ee) [S3]

1H NMR (DMSO-d6, 400 MHz): δ = 8.06 (br s, 3H), 2.73 (t, J = 8.0 Hz, 2H), 1.57–1.51 (m, 2H), 1.32–1.19 (m, 10H), 0.88–0.85 (m, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 38.61, 31.08, 28.41, 28.35, 26.84, 25.78, 21.99, 13.87.

1-decanamine hydrochloride (2ff) [S19]

1H NMR (DMSO-d6, 400 MHz): δ = 7.75 (br s, 3H), 2.75 (t, J = 7.2 Hz, 2H), 1.54–1.50 (m, 2H), 1.28–1.22 (m, 14H), 0.86 (t, J = 7.2 Hz, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 38.78, 31.20, 28.81, 28.76, 28.62, 28.46, 26.91, 25.74, 22.03, 13.91.

1-dodecanamine hydrochloride (2gg) [S6]

1H NMR (DMSO-d6, 400 MHz): δ = 7.80 (br s, 3H), 2.75 (t, J = 7.2 Hz, 2H), 1.54–1.49 (m, 2H), 1.31–1.22 (m, 18H), 0.86 (t, J = 7.2 Hz, 3H); 13C NMR (DMSO-d6, 100 MHz): δ = 38.78, 31.27, 29.01, 28.99, 28.91, 28.81, 28.69, 28.50, 26.97, 25.78, 22.07, 13.95.

3-ethoxypropanamine hydrochloride (2hh) [Consistent with an authentic sample prepared from a commercial 2hh]

1H NMR (DMSO-d6, 400 MHz): δ = 8.18 (s, 3H), 3.44–3.40 (m, 4H), 2.81 (t, J = 7.2 Hz, 2H), 1.85–1.79 (m, 2H), 1.11 (t, J = 7.2 Hz, 3H); 13C NMR (DMSO-d6, 100 MHz): δ =66.67, 65.31, 36.48, 27.20, 15.06.

neopentylamine hydrochloride (2ii) [S18]

1H NMR (DMSO-d6, 400 MHz): δ = 7.97 (br s, 3H), 2.60 (s, 2H), 0.95 (s, 9H); 13C NMR (DMSO-d6, 100 MHz): δ = 49.72, 30.15, 26.85.

cyclopropanemethylamine hydrochloride (2jj) [S15]

1H NMR (DMSO-d6, 400 MHz): δ = 8.10 (br s, 3H), 2.68–2.62 (m, 2H), 1.08–0.98 (m, 1H), 0.58–0.46 (m, 2H), 0.38–0.27 (m, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 43.41, 8.52, 3.77.

cyclohexanemethylamine hydrochloride (2kk) [S4]

1H NMR (DMSO-d6, 400 MHz): δ = 8.09 (s, 3H), 2.60 (d, J = 6.8 Hz, 2H), 1.76–1.56 (m, 6H), 1.20–1.10 (m, 3H), 0.95–0.87 (m, 2H); 13C NMR (DMSO-d6, 100 MHz): δ = 44.30, 35.33, 29.75, 25.61, 25.01.

1-adamantanemethylamine hydrochloride (2ll) [S20, S21]

1H NMR (DMSO-d6, 400 MHz): δ = 7.96 (s, 3H), 2.46 (s, 2H), 1.96 (s, 3H), 1.69–1.52 (m, 12H); 13C NMR (DMSO-d6, 100 MHz): δ = 49.84, 38.82, 36.05, 31.55, 27.32.

m-xylylenediamine dihydrochloride (2mm) [S21]

1H NMR (DMSO-d6, 400 MHz): δ = 8.35 (s, 6H), 7.53–7.49 (m, 4H), 4.03 (s, 4H); 13C NMR (DMSO-d6, 100 MHz): δ = 134.36, 129.53, 129.00, 128.72, 42.09.

p-xylylenediamine dihydrochloride (2nn) [S22]

1H NMR (DMSO-d6, 400 MHz): δ = 8.60 (s, 6H), 7.53 (s, 4H), 4.01 (s, 4H); 13C NMR (DMSO-d6, 100 MHz): δ = 134.15, 129.01, 41.69.

1,8-octanediamine dihydrochloride (2oo) [S22]

1H NMR (DMSO-d6, 400 MHz): δ = 7.90 (br s, 6H), 2.75 (t, J = 7.6 Hz, 4H), 1.58–1.51 (m, 4H), 1.34–1.26 (m, 8H); 13C NMR (DMSO-d6, 100 MHz): δ = 38.70, 28.24, 26.88, 25.66.

1,10-decanediamine dihydrochloride (2pp) [S22]

1H NMR (DMSO-d6, 400 MHz): δ = 7.97 (br s, 6H), 2.73 (t, J = 8.0 Hz, 4H), 1.58–1.51 (m, 4H), 1.32–1.23 (m, 12H); 13C NMR (DMSO-d6, 100 MHz): δ = 38.86, 28.84, 28.65, 27.09, 25.99.

4. 1H and 13C NMR spectra

1H NMR spectrum of benzylamine hydrochloride (2a)

13C NMR spectrum of benzylamine hydrochloride (2a)

1H NMR spectrum of o-methylbenzylamine hydrochloride (2b)

13C NMR spectrum of o-methylbenzylamine hydrochloride (2b)

1H NMR spectrum of m-methylbenzylamine hydrochloride (2c)

13C NMR spectrum of m-methylbenzylamine hydrochloride (2c)

1H NMR spectrum of p-methylbenzylamine hydrochloride (2d)

13C NMR spectrum of p-methylbenzylamine hydrochloride (2d)

1H NMR spectrum of p-tert-butylbenzylamine hydrochloride (2e)

13C NMR spectrum of p-tert-butylbenzylamine hydrochloride (2e)

1H NMR spectrum of o-methoxybenzylamine hydrochloride (2f)

13C NMR spectrum of o-methoxybenzylamine hydrochloride (2f)

1H NMR spectrum of m-methoxybenzylamine hydrochloride (2g)

13C NMR spectrum of m-methoxybenzylamine hydrochloride (2g)

1H NMR spectrum of p-methoxybenzylamine hydrochloride (2h)

13C NMR spectrum of p-methoxybenzylamine hydrochloride (2h)

1H NMR spectrum of o-chlorobenzylamine hydrochloride (2i)

13C NMR spectrum of o-chlorobenzylamine hydrochloride (2i)

1H NMR spectrum of m-chlorobenzylamine hydrochloride (2j)

13C NMR spectrum of m-chlorobenzylamine hydrochloride (2j)

1H NMR spectrum of p-chlorobenzylamine hydrochloride (2k)

13C NMR spectrum of p-chlorobenzylamine hydrochloride (2k)

1H NMR spectrum of p-bromobenzylamine hydrochloride (2l)

13C NMR spectrum of p-bromobenzylamine hydrochloride (2l)

1H NMR spectrum of p-fluorobenzylamine hydrochloride (2m)

13C NMR spectrum of p-fluorobenzylamine hydrochloride (2m)

1H NMR spectrum of 2,4-difluorobenzylamine hydrochloride (2n)

13C NMR spectrum of 2,4-difluorobenzylamine hydrochloride (2n)

1H NMR spectrum of 3,4-dichlorobenzylamine hydrochloride (2o)

13C NMR spectrum of 3,4-dichlorobenzylamine hydrochloride (2o)

1H NMR spectrum of p-(trifluoromethyl)benzylamine hydrochloride (2p)

13C NMR spectrum of p-(trifluoromethyl)benzylamine hydrochloride (2p)

1H NMR spectrum of p-aminobenzylamine hydrochloride (2q)

13C NMR spectrum of p-aminobenzylamine hydrochloride (2q)

1H NMR spectrum of p-(N,N-dimethylamino)benzylamine hydrochloride (2r)

13C NMR spectrum of p-(N,N-dimethylamino)benzylamine hydrochloride (2r)

1H NMR spectrum of p-(methylthio)benzylamine hydrochloride (2s)

13C NMR spectrum of p-(methylthio)benzylamine hydrochloride (2s)

1H NMR spectrum of p-phenyoxybenzylamine hydrochloride (2t)

13C NMR spectrum of p-phenyoxybenzylamine hydrochloride (2t)

1H NMR spectrum of 3,4-methylenedioxybenzylamine hydrochloride (2u)

13C NMR spectrum of 3,4-methylenedioxybenzylamine hydrochloride (2u)

1H NMR spectrum of 2-phenylethaneamine hydrochloride (2v)

13C NMR spectrum of 2-phenylethaneamine hydrochloride (2v)

1H NMR spectrum of p-phenylbenzylamine hydrochloride (2w)

13C NMR spectrum of p-phenylbenzylamine hydrochloride (2w)

1H NMR spectrum of 1-naphthalenemethylamine hydrochloride (2x)

13C NMR spectrum of 1-naphthalenemethylamine hydrochloride (2x)

1H NMR spectrum of 4-picolylamine hydrochloride (2y)

13C NMR spectrum of 4-picolylamine hydrochloride (2y)

1H NMR spectrum of 3-picolylamine hydrochloride (2z)

13C NMR spectrum of 3-picolylamine hydrochloride (2z)

1H NMR spectrum of 5-aminomethylindole (2aa)

13C NMR spectrum of 5-aminomethylindole (2aa)

1H NMR spectrum of furfurylamine hydrochloride (2bb)

13C NMR spectrum of furfurylamine hydrochloride (2bb)

1H NMR spectrum of 2-thiophenemethylamine hydrochloride (2cc)

13C NMR spectrum of 2-thiophenemethylamine hydrochloride (2cc)

1H NMR spectrum of 1-pentanamine hydrochloride (2dd)

13C NMR spectrum of 1-pentanamine hydrochloride (2dd)

1H NMR spectrum of 1-octanamine hydrochloride (2ee)

13C NMR spectrum of 1-octanamine hydrochloride (2ee)

1H NMR spectrum of 1-decanamine hydrochloride (2ff)

13C NMR spectrum of 1-decanamine hydrochloride (2ff)

1H NMR spectrum of 1-dodecanamine hydrochloride (2gg)

13C NMR spectrum of 1-dodecanamine hydrochloride (2gg)

1H NMR spectrum of 3-ethoxypropanamine hydrochloride (2hh)

13C NMR spectrum of 3-ethoxypropanamine hydrochloride (2hh)

1H NMR spectrum of neopentylamine hydrochloride (2ii)

13C NMR spectrum of neopentylamine hydrochloride (2ii)

1H NMR spectrum of cyclopropanemethylamine hydrochloride (2jj)

13C NMR spectrum of cyclopropanemethylamine hydrochloride (2jj)

1H NMR spectrum of cyclohexanemethylamine hydrochloride (2kk)

13C NMR spectrum of cyclohexanemethylamine hydrochloride (2kk)

1H NMR spectrum of 1-adamantanemethylamine hydrochloride (2ll)

13C NMR spectrum of 1-adamantanemethylamine hydrochloride (2ll)

1H NMR spectrum of m-xylylenediamine dihydrochloride (2mm)

13C NMR spectrum of m-xylylenediamine dihydrochloride (2mm)

1H NMR spectrum of p-xylylenediamine dihydrochloride (2nn)

13CNMR spectrum of p-xylylenediamine dihydrochloride (2nn)

1H NMR spectrum of 1,8-octanediamine dihydrochloride (2oo)

13C NMR spectrum of 1,8-octanediamine dihydrochloride (2oo)

1H NMR spectrum of 1,10-decanediamine dihydrochloride (2pp)

13C NMR spectrum of 1,10-decanediamine dihydrochloride (2pp)

5. References

[S1] 	Chandrashekhar, V. G. et al. Silica-supported Fe/Fe–O nanoparticles for the catalytic hydrogenation of nitriles to amines in the presence of aluminium additives. Nat. Catal. 5, 20–29 (2022). 10.1038/s41929-021-00722-x.

[S2]	Chen, F. et al. Stable and inert cobalt catalysts for highly selective and practical hydrogenation of C≡N and C=O bonds. J. Am. Chem. Soc. 138, 8781–8788 (2016). 10.1021/jacs.6b03439.

[S3]	Sanagawa, A. & Nagashima, H. Hydrosilane reduction of nitriles to primary amines by cobalt-isocyanide catalysts. Org. Lett. 21, 287–291 (2019). 10.1021/acs.orglett.8b03736.

[S4]	Gautam, N. et al. Bicyclic (alkyl)(amino)carbene (BICAAC) as a metal-free catalyst for reduction of nitriles to amines. Chem. Commum. 58, 3047–3050 (2022). 10.1039/D1CC06962D.

[S5]	Pandey, V. K., Tiwari, C. S. & Rit, A. Silver-catalyzed hydroboration of C–X (X = C, O, N) multiple bonds. Org. Lett. 23, 1681–1686 (2021). 10.1021/acs.orglett.1c00106.

[S6]	Neumann, J., Bornschein, C., Jiao, H. J., Junge, K. & Beller, M. Hydrogenation of aliphatic and aromatic nitriles using a defined ruthenium PNP pincer catalyst. Eur. J. Org. Chem. 2015, 5944–5948 (2015). 10.1002/ejoc.201501007.

[S7]	Elangovan, S. et al. Selective catalytic hydrogenations of nitriles, ketones, and aldehydes by well-defined manganese pincer complexes. J. Am. Chem. Soc. 138, 8809–8814 (2016). 10.1021/jacs.6b03709.

[S8]	Bisai, M. K., Gour, K., Das, T., Vanka, K. & Sen, S. S. Lithium compound catalyzed deoxygenative hydroboration of primary, secondary and tertiary amides. Dalton Trans. 50, 2354–2358 (2021). 10.1039/D1DT00364J.

[S9]	Yu, J. H. et al. Fabrication of ω-transaminase@metal-organic framework biocomposites for efficiently synthesizing benzylamines and pyridylmethylamines. Adv. Synth. Catal. 364, 380–390 (2022). 10.1002/adsc.202100997.

[S10]	Reeves, J. T. et al. A practical procedure for reduction of primary, secondary and tertiary amides to amines. Adv. Synth. Catal. 355, 47–52 (2013). 10.1002/adsc.201200835.

[S11]	Pandey, P. & Bera, J. K. Hydrosilylative reduction of primary amides to primary amines catalyzed by a terminal [Ni–OH] complex. Chem. Commun. 57, 9204–9207 (2021). 10.1039/D1CC03537A.

[S12]	Wang, Y. et al. Generalized chemoselective transfer hydrogenation/hydrodeuteration. Adv. Synth. Catal.  362, 4119–4129 (2020). 10.1002/adsc.202000759.

[S13]	Wübbolt, S. & Oestreich, M. Exhaustive chemoselective reduction of nitriles by catalytic hydrosilylation involving cooperative Si–H bond activation. Synlett 28, 2411–2414 (2017). 10.1055/s-0036-1588441.

[S14]	Audubert, C., Bouchard, A., Mathieu, G. & Lebel, H. Chemoselective synthesis of amines from ammonium hydroxide and hydroxylamine in continuous flow. J. Org. Chem. 83, 14203–14209 (2018). 10.1021/acs.joc.8b02387.

[S15]	Das, H. S. et al. Primary amides to amines or nitriles: a dual role by a single catalyst. Chem. Commun. 55, 11868–11871 (2019). 10.1039/C9CC05856G.

[S16]	Yuan, H. & Silverman, R. B. Substrates and inhibitors of gamma-aminobutyric acid aminotransferase containing bioisosteres of the carboxylic acid group: design, synthesis, and biological activity. Bioorg. Med. Chem. 14, 1331–1338 (2006). 10.1016/j.bmc.2005.09.067.

[S17]	Utsumi, T., Noda, K., Kawauchi, D., Ueda, H. & Tokuyama, H. Nitrile synthesis by aerobic oxidation of primary amines and in situ generated imines from aldehydes and ammonium salt with Grubbs catalyst. Adv. Synth. Catal. 362, 3583–3588 (2020). 10.1002/adsc.202000663.

[S18]	Tokmic, K., Jackson, B. J., Salazar, A., Woods, T. J. & Fout, A. R. Cobalt-catalyzed and Lewis acid-assisted nitrile hydrogenation to primary amines: a combined effort. J. Am. Chem. Soc. 139, 13554–13561 (2017). 10.1021/jacs.7b07368.

[S19]	Sheng, M. et al. Hydrotalcite-supported cobalt phosphide nanorods as a highly active and reusable heterogeneous catalyst for ammonia-free selective hydrogenation of nitriles to primary amines. ACS Sustainable Chem. Eng. 9, 11238–11246 (2021). 10.1021/acssuschemeng.1c03667.

[S20]	Yao, W. B. et al. A BEt3-base catalyst for amide reduction with silane. J. Org. Chem. 84, 6084–6093 (2019). 10.1021/acs.joc.9b00277.

[S21]	Fujita, S. et al. Ni2P nanoalloy as an air-stable and versatile hydrogenation catalyst in water: P-alloying strategy for designing smart catalysts. Chem. Eur. J. 27, 4439–4446 (2021). 10.1002/chem.202005037.

[S22]	Heilmann, M. & Tiefenbacher, K. A modular phosphorylated glycoluril-derived molecular tweezer for potent binding of aliphatic diamines. Chem. Eur. J. 25, 12900–12904 (2019). 10.1002/chem.201902556.