Supporting Information

Hierarchically Multifunctional Thermally Conductive Boron Nitride/Polyurethane Fibrous Membranes via Constructing Alternating Multi-Layer Orientation Structure

Fang Jiang 1, 2, 3, Yutao Li 1, Minghua Ye 1, Xiaolong Chen3, Yifeng Shen1, 3, Peng Ding*, 2 and Lei Yang*, 1, 3

1College of Textile Science and Engineering, Zhejiang Sci-Tech University, Hangzhou 310018, PR China

2Faculty of Science, Shanghai University, 99 Shangda Road, Shanghai 200444, PR China

3Shaoxing-keqiao Institute, Zhejiang Sci-Tech University, Shaoxing, 312000, PR China

* Corresponding Author, Email: yanglei@zstu.edu.cn (L. Yang); dingpeng@shu.edu.cn (P. Ding)

Tab. S1. BN loading in PBNF composites.

| FBN/PU single-layer (s-FBN/PU) fibrous membranes |  |
| --- | --- |
| FBN (g) | FBN loading in fibrous membranes (wt%) |
| 0 | 0 |
| 0.22 | 5 |
| 0.44 | 10 |
| 0.71 | 15 |
| 1 | 20 |
| FBN/PU multilayer (m-FBN/PU) fibrous membranes |  |
| FBN (g) | FBN loading in fibrous membranes (wt%) |
| 0.08 | 2 |
| 0.17 | 4 |
| 0.26 | 6 |
| 0.35 | 8 |
| 0.44 | 10 |

Fig. S1. TGA curve of a) m-FBN/PU fibrous membranes and b) s-FBN/PU fibrous membranes with different filler loading.

Fig. S2. Schematic illustration of the fabrication and structure of a) s-FBN/PU fibrous membranes and b) PU fibrous membranes.

Fig. S3. a) SEM image of FBN sheets; b) TEM image of FBN and insert is the corresponding FFT image; FTIR spectra of c) m-FBN/PU fibrous membranes and d) s-FBN/PU fibrous membranes with different FBN loading. e) HRTEM image of FBN.

Fig. S4. a) The FTIR spectra and b) XRD pattern of BN and FBN; XRD pattern of c) s-FBN/PU fibrous membranes and d) m-FBN/PU fibrous membranes.

Fig. S5. The SEM images of the surface of the PU fibrous membranes with different magnification.

Fig. S6. Visual diagram of water contact angle of a) m-FBN/PU fibrous membranes and b) s-FBN/PU fibrous membranes.

Fig. S7. a, c) Topography and b, d) their corresponding 3D images of the pure PU fibrous membranes and m-FBN/PU fibrous membranes.

Finite Element Analysis

The finite element simulation software (COMSOL) was applied to explore the effectiveness of the multilayer structure on the heat transfer processes of FBN/PU fibrous membranes.

Geometry and material parameters: The geometric dimension is simplified as cuboids with length, width and height of 10mm×10mm×0.257mm. For the multilayer membranes model, the 1, 3, and 5 layers are FBN/PU filler layer, and the 2 and 4 layers are PU matrix layer.

Tab. S2. The temperature field calculation parameters of FBN/PU fibrous membranes.

|  | m-FBN/PU fibrous membranes | s-FBN/PU fibrous membranes |
| --- | --- | --- |
| λ// (W·m-1·K-1) | 5.78 | 3.58 |
| ρ(g·cm-1) | 0.92 | 0.92 |
| Cp (J·g-1·K-1) | 1.86 | 1.80 |

Numerical simulation boundary conditions: The initial temperature of the model is set to 293.15 K (room temperature). Define the left and bottom boundary as a heat source and set to 373.15 K, while the other boundaries are conFig.d as heat flux heat dissipation conditions, and the heat transfer coefficient with air is set to 5 W·m-1·K-1. Thermal radiation is not taken into account. The computational mesh uses hexahedral scanning mesh, the number of meshes of m-FBN/PU fibrous membranes is 20880 while that of s-FBN/PU fibrous membranes is 5000. The calculation adopts transient analysis, the calculation time is set to 0.001 s, and the calculation time step is 0.00001 s.