Supplementary material

Hyperproduction of extracellular polymeric substance in Pseudomonas fluorescens for efficient Chromium (Ⅵ) absorption

Lijie Yang1, 5, Zhen Chen3, Ying Zhang2, Fuping Lu4, Yihan Liu4*, Mingfeng Cao1, 5, Ning He1,5*

1Department of Chemical and Biochemical Engineering, College of Chemistry and Chemical Engineering, Xiamen University, Xiamen 361005, P. R. China

2Shandong Institute of Commerce and Technology, Jinan 251000, P.R. China

3College of Life Science, Xinyang Normal University, Xinyang 464000, P. R. China

4Key Laboratory of Industrial Fermentation Microbiology, Ministry of Education, Tianjin Key Laboratory of Industrial Microbiology, The College of Biotechnology, Tianjin University of Science and Technology, Tianjin 300457, China

5The key Lab for Synthetic Biotechnology of Xiamen City, Xiamen University, Xiamen 361005, P. R. China

*Correspondence: Ning He, Yihan Liu

# E-mail address: hening@xmu.edu.cn, lyh@tust.edu.cn

# Tel.: +86-592-2183751

# Fax: +86-592-2184822

Figure S1 Effect of different concentration of glucose (a), urea (b) and yeast extract (c) on EPS production.

Figure S2 Effect of different concentration of phosphate (a), Mn2+ (b) and NaCl (c) on EPS production.

Figure S3 Optimization of culture conditions for EPS production. (a) Growth curves of P. fluorescens mutant T4-2; Effect of temperature (b), initial pH (c) and inoculums size (d) on EPS production.

Table S1. The models and equations used for the adsorption Cr (VI) of by EPS of P. fluorescens mutant T4-2

|  | Model | Equation | Model parameters |
| --- | --- | --- | --- |
| Adsorption isotherm | Langmuir | 1qe=1qm+1bqmCe | qe = equilibrium capacity of Cr (VI) adsorbed onto EPS (mg g−1), Ce = equilibrium concentration of Cr (VI) solution (mg L−1), qm = maximum adsorption capacity (mg g−1), and b = energy of adsorption (L mg−1); |
|  | Freundlich | logqe=logKF+1nlogCe | qe = equilibrium capacity of Cr (VI) adsorbed onto EPS (mg g−1), Ce = equilibrium concentration of Cr (VI) solution (mg L−1), KF = Freundlich constant (mg g-1), n = adsorption intensity of the EPS |
|  | Redlich-Peterson | qe=KCe1+αCeβ | K and α are the Redlich−Peterson isotherm constants and β is the exponent |
| Adsorption kinetics | Pseudo-first order | log(qe-qt)=logqe-k12.303t | qe = equilibrium adsorption capacity (mg g−1), qt = adsorption capacity (mg g−1) at any time t, k1 = first-order rate constant(h-1) |
|  | Pseudo-second order | tqt=1k2qe2+1qet | qe = equilibrium adsorption capacity (mg g−1), qt = adsorption capacity (mg g−1) at any time t, k2 = the second-order rate constant (mg g−1 h−1) |
|  | Webber-Morris | qt=kit0.5+c | qt = adsorption (mg g−1) at any time t, ki = intra-particle diffusion rate constant (mg g−1 h−0.5) |
| Adsorption thermodynamics | Vant Hoff’s equation | ∆G0=∆H0-T∆S0 ∆G0=-RTlnK0 lnK0=∆S0R-∆H0RT | ΔG0= Gibbs free energy change (kJ mol−1), R = the gas constant (J mol−1 K−1), T = temperature (K), k0 = the equilibrium constant, ΔH0 = enthalpy change (kJ mol−1), ΔS0 = entropy change (kJ mol−1 K−1) |
|  | Arrhenius equation | lnK=lnA-EaRT | Ea =the Arrhenius activation energy (kJ mol−1), A = the Arrhenius factor, R= the Arrhenius factor, K = the rate constant (k2) of the pseudo-second order kinetic mode |