Selection of solvents based on Hansen solubility parameters for calix[4]arene acetic acid derivatives as extractants of metal ions

Tatsuya Oshima · Tatsuya Ishibashi · Keisuke Ohto

T. Oshima (*) · T.Ishibashi

Department of Applied Chemistry, Faculty of Engineering, University of Miyazaki, 1-1 Gakuen Kibanadai-nishi, Miyazaki 889-2192, Japan

K. Ohto

Department of Chemistry and Applied Chemistry, Faculty of Science and Engineering, Saga University, 1-Honjo, Saga 840-8502, Japan

* Corresponding author at:

E-mail address: oshimat@cc.miyazaki-u.ac.jp

Tel: +81-985-58-7321	Fax: +81-985-58-7323

Supplementary Data

Table of Contents

Effect of the equilibrium pH on the distribution ratio of Pb(II): (Fig. S1)	2

Effect of the concentration of tOct[4]CH2COOH on the distribution ratio of Pb(II): (Fig. S2)	3

Hansen solubility parameters of solvents and solubility of tBu[4]CH2COOH in each solvent. (Table S1)	4

Hansen solubility parameters of solvents and solubility of tOct[4]CH2COOH in each solvent. (Table S2)	6

Fig. S1	Effect of the equilibrium pH on the distribution ratio of Pb(II): O/A = 0.2, pHeq 1.21-2.02 (in chloroform) or 1.90-3.82 (in 2-NON), [tOct[4]CH2COOH]=1.0×10-2 mol/L, [Pb(II)]init = 0.1×10-3 mol/L. The dashed lines are the theoretical line.

Fig. S2	Effect of the concentration of tOct[4]CH2COOH on the distribution ratio of Pb(II): O/A = 0.2, pHeq 1.43±0.01 (in chloroform) or 2.74±0.01 (in 2-NON), [tOct[4]CH2COOH]=0.1×10-3–10.0×10-3 mol/L, [Pb(II)]init = 0.1×10-3 mol/L. The solid line is the theoretical line.

Table S1. Hansen solubility parameters of solvents and solubility of tBu[4]CH2COOH in each solvent.

| Solvent | δD1 | δP1 | δH1 | Solubility | RED |
| --- | --- | --- | --- | --- | --- |
| Acetic Acid | 14.5 | 8 | 13.5 | insoluble | 1.82 |
| Acetone | 15.5 | 10.4 | 7 | soluble | 1.121* |
| Acetophenone | 18.8 | 9 | 4 | soluble | 1.137* |
| Anisole | 17.8 | 4.4 | 6.9 | insoluble | 0.635# |
| Benzyl Alcohol | 18.4 | 6.3 | 13.7 | soluble | 1.431* |
| γ-Butyrolactone (Gbl) | 18 | 16.6 | 7.4 | insoluble | 2.159 |
| Chloroform | 17.8 | 3.1 | 5.7 | soluble | 0.99 |
| Cycloheptanone | 17.2 | 10.6 | 4.8 | insoluble | 1.027 |
| Cyclohexane | 16.8 | 0 | 0.2 | insoluble | 2.284 |
| Diacetone Alcohol | 15.8 | 8.2 | 10.8 | insoluble | 1.009 |
| Dibenzyl Ether | 19.6 | 3.4 | 5.2 | insoluble | 1.398 |
| Diethyl Ketone | 15.8 | 7.6 | 4.7 | soluble | 0.956 |
| Diethylene Glycol | 16.6 | 12 | 19 | insoluble | 2.773 |
| Dipropylene Glycol | 16.5 | 10.6 | 17.7 | insoluble | 2.399 |
| Dodecane | 16 | 0 | 0 | insoluble | 2.379 |
| Ethanol | 15.8 | 8.8 | 19.4 | insoluble | 2.725 |
| Ethyl Acetate | 15.8 | 5.3 | 7.2 | soluble | 0.782 |
| Hexane | 14.9 | 0 | 0 | insoluble | 2.544 |
| Isopropyl Ether | 15.1 | 3.2 | 3.2 | insoluble | 1.634 |
| 2-Methyl Cyclohexanone | 17.6 | 7.8 | 4.7 | soluble | 0.694 |
| Methyl Ethyl Ketone (Mek) | 16 | 9 | 5.1 | soluble | 0.935 |
| Methyl Isoamyl Ketone | 16 | 5.7 | 4.1 | soluble | 1.028* |
| Methyl Isobutyl Ketone (Mibk) | 15.3 | 6.1 | 4.1 | insoluble | 1.216 |
| Octanoic Acid | 15.7 | 3.3 | 8.2 | insoluble | 1.099 |
| 1-Octanol | 16 | 5 | 11.2 | soluble | 1.077* |
| 1-Propanol | 16 | 6.8 | 17.4 | insoluble | 2.243 |
| 2-Propanol | 15.8 | 6.1 | 16.4 | insoluble | 2.066 |
| Propionic Acid | 14.7 | 5.3 | 12.4 | insoluble | 1.616 |
| Tetrahydrofuran (Thf) | 16.8 | 5.7 | 8 | soluble | 0.376 |
| Toluene | 18 | 1.4 | 2 | insoluble | 1.793 |
| 2,2,4-Trimethylpentane | 14.1 | 0 | 0 | insoluble | 2.714 |
| Water | 15.5 | 16 | 42.3 | insoluble | 7.994 |
| p-Xylene | 17.8 | 1 | 3.1 | insoluble | 1.686 |
| Dipropyl Ketone | 15.8 | 7.6 | 4.9 | insoluble | 0.926# |
| Diethylene Glycol Dibutyl Ether | 15.8 | 4.7 | 4.4 | insoluble | 1.116 |
| Isopropyl Benzene (Cumene) | 18.1 | 1.2 | 1.2 | insoluble | 1.958 |
| 1,2-Dimethoxybenzene | 19.2 | 4.4 | 9.4 | insoluble | 1.082 |
| 1,1,3,3-Tetramethoxypropane | 15 | 7.1 | 6.8 | insoluble | 1.052 |
| 1-Nonanol | 16 | 4.8 | 11 | insoluble | 1.064 |
| Hexanoic Acid | 16.3 | 4.2 | 11.5 | insoluble | 1.148 |
| Diphenyl Ether | 19.4 | 3.4 | 4 | insoluble | 1.465 |
| 1,8-Cineole (Eucalyptol) | 16.7 | 4.6 | 3.4 | insoluble | 1.121 |
| Cyclopentyl Methyl Ether (Cpme) | 16.7 | 4.3 | 4.3 | soluble | 0.996 |
| Nonylbenzene | 16.9 | 1.4 | 2.1 | insoluble | 1.762 |
| 2-Nonanone | 16.1 | 5.1 | 3.5 | insoluble | 1.153 |
| 1-Phenyl-1-Butanone | 18 | 5.6 | 3.6 | insoluble | 1 |
| p-Methylacetophenone | 18.8 | 6.9 | 4.4 | soluble | 0.978 |
| 3,4-Dimethoxyphenylacetone | 18.7 | 5.2 | 10 | insoluble | 0.894# |
| Valerophenone | 17.9 | 5.3 | 3.5 | insoluble | 1.03 |
| 2-Methyl Valeric Acid | 16.1 | 5.3 | 11.1 | insoluble | 1.01 |

1 HSPs (δD, δP, δH) [M Pa1/2] values were introduced from HSPiP software ver.5. [22]

* wrong out (soluble but RED > 1)

# wrong in (insoluble but RED < 1)

Table S2. Hansen solubility parameters of solvents and solubility of tOct[4]CH2COOH in each solvent.

| Solvent | δD1 | δP1 | δH1 | Score | RED |
| --- | --- | --- | --- | --- | --- |
| Acetic Acid | 14.5 | 8 | 13.5 | insoluble | 2.769 |
| Acetone | 15.5 | 10.4 | 7 | insoluble | 1.789 |
| Acetophenone | 18.8 | 9 | 4 | soluble | 1.336* |
| Anisole | 17.8 | 4.4 | 6.9 | soluble | 0.674 |
| Benzyl Alcohol | 18.4 | 6.3 | 13.7 | insoluble | 2.415 |
| γ-Butyrolactone (Gbl) | 18 | 16.6 | 7.4 | insoluble | 3.092 |
| Chloroform | 17.8 | 3.1 | 5.7 | soluble | 0.575 |
| Cycloheptanone | 17.2 | 10.6 | 4.8 | insoluble | 1.482 |
| Cyclohexane | 16.8 | 0 | 0.2 | insoluble | 1.599 |
| Diacetone Alcohol | 15.8 | 8.2 | 10.8 | insoluble | 1.949 |
| Dibenzyl Ether | 19.6 | 3.4 | 5.2 | insoluble | 1.237 |
| Diethyl Ketone | 15.8 | 7.6 | 4.7 | insoluble | 1.026 |
| Diethylene Glycol | 16.6 | 12 | 19 | insoluble | 4.081 |
| Dipropylene Glycol | 16.5 | 10.6 | 17.7 | insoluble | 3.643 |
| Dodecane | 16 | 0 | 0 | insoluble | 1.732 |
| Ethanol | 15.8 | 8.8 | 19.4 | insoluble | 3.939 |
| Ethyl Acetate | 15.8 | 5.3 | 7.2 | insoluble | 1.005 |
| Hexane | 14.9 | 0 | 0 | insoluble | 1.996 |
| Isopropyl Ether | 15.1 | 3.2 | 3.2 | insoluble | 1.176 |
| 2-Methyl Cyclohexanone | 17.6 | 7.8 | 4.7 | soluble | 0.802 |
| Methyl Ethyl Ketone (Mek) | 16 | 9 | 5.1 | insoluble | 1.255 |
| Methyl Isoamyl Ketone | 16 | 5.7 | 4.1 | soluble | 0.676 |
| Methyl Isobutyl Ketone (Mibk) | 15.3 | 6.1 | 4.1 | soluble | 1.037* |
| Octanoic Acid | 15.7 | 3.3 | 8.2 | insoluble | 1.259 |
| 1-Octanol | 16 | 5 | 11.2 | insoluble | 1.796 |
| 1-Propanol | 16 | 6.8 | 17.4 | insoluble | 3.335 |
| 2-Propanol | 15.8 | 6.1 | 16.4 | insoluble | 3.09 |
| Propionic Acid | 14.7 | 5.3 | 12.4 | insoluble | 2.361 |
| Tetrahydrofuran (Thf) | 16.8 | 5.7 | 8 | soluble | 0.946 |
| Toluene | 18 | 1.4 | 2 | soluble | 1.095* |
| 2,2,4-Trimethylpentane | 14.1 | 0 | 0 | insoluble | 2.254 |
| Water | 15.5 | 16 | 42.3 | insoluble | 9.911 |
| p-Xylene | 17.8 | 1 | 3.1 | insoluble | 1.021 |
| Dipropyl Ketone | 15.8 | 7.6 | 4.9 | insoluble | 1.03 |
| Diethylene Glycol Dibutyl Ether | 15.8 | 4.7 | 4.4 | soluble | 0.72 |
| Isopropyl Benzene (Cumene) | 18.1 | 1.2 | 1.2 | insoluble | 1.269 |
| 1,2-Dimethoxybenzene | 19.2 | 4.4 | 9.4 | insoluble | 1.577 |
| 1,1,3,3-Tetramethoxypropane | 15 | 7.1 | 6.8 | insoluble | 1.4 |
| 1-Nonanol | 16 | 4.8 | 11 | insoluble | 1.748 |
| Hexanoic Acid | 16.3 | 4.2 | 11.5 | insoluble | 1.825 |
| Diphenyl Ether | 19.4 | 3.4 | 4 | insoluble | 1.133 |
| 1,8-Cineole (Eucalyptol) | 16.7 | 4.6 | 3.4 | soluble | 0.38 |
| Cyclopentyl Methyl Ether (Cpme) | 16.7 | 4.3 | 4.3 | soluble | 0.289 |
| Nonylbenzene | 16.9 | 1.4 | 2.1 | insoluble | 1.026 |
| 2-Nonanone | 16.1 | 5.1 | 3.5 | soluble | 0.628 |
| 1-Phenyl-1-Butanone | 18 | 5.6 | 3.6 | insoluble | 0.494# |
| p-Methylacetophenone | 18.8 | 6.9 | 4.4 | soluble | 0.957 |
| 3,4-Dimethoxyphenylacetone | 18.7 | 5.2 | 10 | insoluble | 1.57 |
| Valerophenone | 17.9 | 5.3 | 3.5 | insoluble | 0.437# |
| 2-Methyl Valeric Acid | 16.1 | 5.3 | 11.1 | insoluble | 1.761 |

1 HSPs (δD, δP, δH) [M Pa1/2] values were introduced from HSPiP software ver.5. [22]

* wrong out (soluble but RED > 1)

# wrong in (insoluble but RED < 1)