Supporting Information

Direct OC-CHO coupling towards highly C2+ products selective electroreduction over stable Cu0/Cu2+ interface

Xin Yu Zhang,1† Zhen Xin Lou,1† Jiacheng Chen,2 Yuanwei Liu,1 Xuefeng Wu,1 Jia Yue Zhao,1 Hai Yang Yuan,1* Minghui Zhu,2 Sheng Dai,3 Hai Feng Wang,4 Chenghua Sun,5 Peng Fei Liu1* & Hua Gui Yang1*

1 Key Laboratory for Ultrafine Materials of Ministry of Education, Shanghai Engineering Research Center of Hierarchical Nanomaterials, School of Materials Science and Engineering, East China University of Science and Technology, 130 Meilong Road, Shanghai, 200237 (China)

2 State Key Laboratory of Chemical Engineering, School of Chemical Engineering, East China University of Science and Technology, 130 Meilong Road, Shanghai, 200237 (China)

3 Key Laboratory for Advanced Materials and Feringa Nobel Prize Scientist Joint Research Center, Institute of Fine Chemicals, School of Chemistry and Molecular Engineering, East China University of Science and Technology, 130 Meilong Road, Shanghai, 200237 (China)

4 Key Laboratory for Advanced Materials, Centre for Computational Chemistry and Research Institute of Industrial Catalysis, School of Chemistry and Molecular Engineering, East China University of Science and Technology, 130 Meilong Road, Shanghai, 200237 (China)

5 Department of Chemistry and Biotechnology, and Center for Translational Atomaterials, Swinburne University of Technology, Hawthorn, VIC, 3122 (Australia)

† These authors contributed equally to this work.

* Emails: hgyang@ecust.edu.cn; pfliu@ecust.edu.cn; hyyuan@ecust.edu.cn

Supplementary Fig. 1 a Cu0/Cu2+ structure constructed by Cu loaded on Cu2P2O7; b Cu0/Cu1+ structure constructed by Cu loaded on Cu2O.

Supplementary Fig. 2 Schematic illustration of the sol-gel preparation process, showing that the final Cu3(PO4)2 (~1.13 g) and Cu2P2O7 (~0.91 g) products were obtained.

Supplementary Fig. 3 XRD pattern of CuO control sample, which indicates the crystalline phase of CuO.

Supplementary Fig. 4 a TEM image and b HRTEM image of the Cu3(PO4)2 sample. c HAADF-STEM image of Cu3(PO4)2 and d-f cooresponding elemental maps of d Cu, e P, and f O elements, respectively.

Supplementary Fig. 5 a Low-magnificaiton TEM image and b HRTEM image of the Cu2P2O7 sample. c HAADF-STEM image of Cu2P2O7 and d-f cooresponding elemental maps of d Cu, e P, and f O elements, respectively.

Supplementary Fig. 6 a TEM image and b HRTEM image of the CuO sample.

Supplementary Fig. 7 a HAADF-STEM image of the Cu3(PO4)2 sample and b TEM image of the Cu2P2O7 sample after 0.5 hour’s CO2RR at the applied potential of -1.40 V vs. RHE.

Supplementary Fig. 8 False-color HRTEM images of the a Cu3(PO4)2 and b Cu2P2O7 sample after CO2RR at the potential of -1.40 V vs. RHE.

Supplementary Fig. 9 a TEM image and b HR-TEM image of the CuO control sample after 0.5 hour’s CO2RR at the applied potential of -1.40 V vs. RHE, showing that the pristine CuO phase has been reduced to metallic Cu during the test.

Supplementary Fig. 10 XPS spectra of Cu 2p region of Cu2P2O7 and CuO control sample collected before and after CO2RR at -1.40 V vs. RHE for 1 h, showing that the Cu species of Cu2P2O7 exhibited the main component of Cu2+, while Cu species of CuO were largely reduced to metallic Cu0 states after CO2RR.

Supplementary Fig. 11 a, b XPS spectra of Cu2P2O7 before and after 1 hour’s CO2RR at the applied potential of -1.40 V vs. RHE in a P 2p and b O 1s regions, indicating the phosphate group persisted during the test. Notes: Cu-O might result from the slight oxidation in the air.

Supplementary Fig. 12 XPS spectra of CuO control sample before and after 1 hour’s CO2RR at the applied potential of -1.40 V vs. RHE in O 1s region.

Supplementary Fig. 13 FT-IR spectra of Cu2P2O7 before and after 1 hour’s CO2RR at the applied potential of -1.40 V vs. RHE.

Supplementary Fig. 14 a, b Raman spectra of a Cu2P2O7 and b CuO control sample before and after 1 hour’s CO2RR at the applied potential of -1.40 V vs. RHE.

Supplementary Fig. 15 a, b Operando Raman spectra of Cu2P2O7 during CO2RR at a -1.40 V vs. RHE and b -1.80 V vs. RHE in CO2-saturated 0.1 M KHCO3.

Supplementary Fig. 16 Faradaic efficiencies of gas products of a Cu3(PO4)2/GC, b Cu2P2O7/GC and c CuO/GC at different applied potentials in CO2-saturated 0.1 M KHCO3, suggesting the superior C2H4 selectivity for CuPO.

Supplementary Fig. 17 Potential dependence on time during CO2RR at -100~-450 mA cm-2 in 2.0 M KOH aqueous electrolyte on the Cu3(PO4)2/Cu/PTFE.

Supplementary Fig. 18 Digital photograph of the homemade cell attached to the PerkinElmer spectrum 100 spectrometer for in situ SEIRAS measurement. The CO2 gas flow rate through the gas chamber was controlled as 10 sccm by a gas flow controller.

Supplementary Table 1 Cu0, Cu1+, and Cu2+ ratios and for the fitting of the linear combination of XANES spectra.

| Cu3(PO4)2 Cu oxidation state | Time (-1.45 V vs. RHE) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 6 min | 12 min | 18 min | 24 min | 30 min | post |
| Cu0 | 0.04 | 0.06 | 0.16 | 0.23 | 0.28 | 0.08 |
| Cu1+ | 0.01 | 0.06 | 0.12 | 0.14 | 0.24 | 0.41 |
| Cu2+ | 0.95 | 0.88 | 0.72 | 0.63 | 0.49 | 0.51 |
| CuO Cu oxidation state | Time (-1.45 V vs. RHE) |  |  |  |  |  |
|  | 6 min | 12 min | 18 min | 24 min | 30 min | post |
| Cu0 | 0.04 | 0.18 | 0.62 | 0.68 | 0.73 | 0.69 |
| Cu1+ | 0.00 | 0.20 | 0.13 | 0.13 | 0.13 | 0.17 |
| Cu2+ | 0.96 | 0.63 | 0.25 | 0.19 | 0.13 | 0.13 |

Supplementary Table 2 Faradaic efficiencies of gas products for CuPO/GC in 0.1 M KHCO3.

| Cu3(PO4)2/GC Faradaic efficiencies (%) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Potential (V vs. RHE) | Current density (mA cm2) | H2 | CO | CH4 | C2H4 | Total all |
| -1.20 | -18.1 | 42.9 | 18.7 | 2.0 | 37.9 | 101.6 |
|  | -18.6 | 42.4 | 16.9 | 2.0 | 37.0 | 98.2 |
|  | -18.6 | 42.4 | 15.4 | 2.1 | 38.2 | 98.2 |
| -1.25 | -19.1 | 29.3 | 8.7 | 2.4 | 54.2 | 95.1 |
|  | -19.3 | 24.7 | 9.5 | 1.6 | 65.4 | 101.2 |
|  | -19.6 | 24.0 | 10.0 | 1.5 | 65.6 | 101.1 |
| -1.30 | -23.7 | 22.9 | 8.1 | 1.2 | 58.0 | 90.1 |
|  | -23.2 | 22.8 | 8.0 | 1.3 | 67.3 | 99.4 |
|  | -23.5 | 20.0 | 7.1 | 1.3 | 68.4 | 96.7 |
| -1.35 | -27.3 | 20.9 | 6.7 | 1.3 | 63.8 | 92.7 |
|  | -27.1 | 19.1 | 6.5 | 1.1 | 68.9 | 95.6 |
|  | -27.1 | 19.8 | 6.4 | 1.1 | 69.7 | 97.0 |
| -1.40 | -29.7 | 18.6 | 5.4 | 2.2 | 63.2 | 89.5 |
|  | -29.6 | 13.3 | 5.3 | 2.0 | 72.4 | 92.7 |
|  | -29.7 | 13.0 | 4.9 | 2.0 | 71.3 | 91.5 |
| -1.45 | -33.0 | 20.1 | 4.6 | 1.8 | 63.9 | 90.4 |
|  | -33.0 | 19.8 | 4.6 | 1.8 | 71.7 | 97.9 |
|  | -33.1 | 23.0 | 4.2 | 1.4 | 73.4 | 102.0 |
| -1.50 | -36.7 | 24.4 | 3.7 | 1.9 | 63.0 | 93.1 |
|  | -36.6 | 22.1 | 3.6 | 2.1 | 69.6 | 97.3 |
|  | -36.7 | 24.0 | 3.4 | 1.6 | 70.0 | 99.0 |
| Cu2P2O7/GC Faradaic efficiencies (%) |  |  |  |  |  |  |
| Potential (V vs. RHE) | Current density (mA cm2) | H2 | CO | CH4 | C2H4 | Total all |
| -1.20 | -14.7 | 19.5 | 17.8 | 6.3 | 46.8 | 90.4 |
|  | -15.1 | 12.4 | 3.7 | 8.2 | 57.0 | 81.7 |
|  | -15.4 | 11.6 | 3.7 | 8.0 | 62.9 | 86.8 |
| -1.30 | -20.1 | 14.5 | 13.1 | 5.7 | 48.8 | 82.6 |
|  | -20.3 | 15.0 | 14.0 | 14.6 | 51.0 | 94.7 |
|  | -20.7 | 12.7 | 3.4 | 4.7 | 66.8 | 87.6 |
| -1.40 | -26.3 | 15.8 | 10.4 | 6.7 | 55.3 | 88.4 |
|  | -27.9 | 14.2 | 3.1 | 3.3 | 66.9 | 87.5 |
|  | -28.0 | 15.7 | 4.0 | 3.6 | 69.7 | 92.9 |
| -1.50 | -33.0 | 17.4 | 7.6 | 10.1 | 57.9 | 92.9 |
|  | -33.9 | 21.5 | 2.9 | 1.2 | 63.4 | 89.0 |
|  | -34.3 | 23.3 | 1.0 | 1.2 | 66.5 | 92.1 |
| Supplementary Table 3 Faradaic efficiencies of gas products for CuO/GC in 0.1 M KHCO3. |  |  |  |  |  |  |
| Potential (V vs. RHE) | Current density (mA cm2) | H2 | CO | CH4 | C2H4 | Total all |
| -1.20 | -5.0 | 75.1 | 5.4 | 6.2 | 9.3 | 92.5 |
|  | -5.1 | 74.0 | 6.8 | 6.0 | 7.7 | 94.6 |
|  | -5.4 | 88.7 | 7.2 | 5.7 | 6.0 | 107.6 |
| -1.25 | -6.9 | 78.8 | 6.7 | 6.7 | 5.3 | 97.5 |
|  | -6.9 | 67.2 | 7.8 | 6.7 | 4.3 | 85.9 |
|  | -7.2 | 75.2 | 8.0 | 6.4 | 5.1 | 94.7 |
| -1.30 | -8.6 | 74.8 | 6.3 | 9.1 | 6.0 | 96.2 |
|  | -8.4 | 70.1 | 7.4 | 7.4 | 5.0 | 89.8 |
|  | -8.3 | 81.1 | 8.9 | 7.5 | 4.8 | 102.3 |
| -1.35 | -10.0 | 50.1 | 2.7 | 12.4 | 7.5 | 72.7 |
|  | -10.1 | 62.4 | 3.8 | 12.3 | 6.4 | 85.0 |
|  | -10.0 | 76.2 | 5.1 | 10.9 | 6.1 | 98.1 |
| -1.40 | -10.1 | 65.9 | 4.6 | 19.9 | 7.1 | 97.5 |
|  | -9.7 | 55.2 | 6.4 | 19.2 | 5.3 | 86.1 |
|  | -9.6 | 52.4 | 8.1 | 17.9 | 4.4 | 82.7 |
| -1.45 | -14.0 | 69.9 | 3.1 | 17.8 | 4.0 | 94.7 |
|  | -13.9 | 74.9 | 4.5 | 13.5 | 3.7 | 96.5 |
|  | -13.7 | 71.7 | 5.1 | 14.7 | 2.5 | 94.1 |
| -1.50 | -17.6 | 71.4 | 2.2 | 22.1 | 4.5 | 100.3 |
|  | -17.0 | 69.0 | 3.0 | 16.5 | 3.3 | 91.7 |
|  | -16.7 | 84.6 | 4.4 | 14.9 | 3.2 | 107.1 |

Supplementary Table 4 Maximum FEC2+, jC2+ and the corresponding potential of CuPO, and some recently reported outstanding CO2-to-C2+ electrocatalysts.

| Catalyst | Electrolyte | FEC2+ (%) | jC2+ (mA cm2) | Reference |
| --- | --- | --- | --- | --- |
| CuPO/Cu/PTFE | 2.0 M KOH | 90.9 | -318.2 | This work |
| Cu-Pd1 | 0.5 M K2SO4 (pH=2) | 89 | -445 | Nat. Catal. 5, 564−570 (2022) |
| Cu(OH)2/Cu foil2 | 1 M KOH | 87 | -217 | Angew. Chem. Int. Ed. 60, 4879−4885 (2021) |
| F-Cu3 | 0.75 M KOH | 85.8 | -1372.8 | Nat. Catal. 3, 478−487 (2020) |
| reconstructed Cu4 | 3 M KOH | ~84 | -336 | Adv. Mater. 30, 1804867 (2018) |
| Cu/GDL5 | 3 M KCl | 82.7 | -97.3 | J. Am. Chem. Soc. 143, 3245−3255 (2021) |
|  | 2 M KCl | 80.4 | -120.6 |  |
| dCu2O/Ag2.3%6 | 1 M KOH | 82.1 | -656.8 | Nat. Commun. 13, 3754 (2022) |
| CuPb-0.7/C7 | 1 M KOH | 81.6 | -326.4 | ACS Nano 15, 1039–1047 (2021) |
| Cu_I8 | 0.1 M KHCO3 | ~80 | ~-31.2 | Angew. Chem. Int. Ed. 58, 17047−17053 (2019) |
| B-Cu-Zn9 | 1 M KOH | 79 | -158 | Angew. Chem. Int. Ed. 60, 9135−9141 (2021) |
| Cu(B)-210 | 0.1 M KHCO3 | 79 | -55 | Nat. Chem. 10, 974−980 (2018) |
| Cu-FEP11 | 1 M KOH | ~77 | ~-600 | Adv. Energy Mater. 12, 2103663 (2022) |
| monodispersed Cu2O NPs12 | 1 M KHCO3 | 75.5 | -226.5 | Joule 4, 1−17 (2020) |
|  |  | 68.4 | -342 |  |
| multi-hollow Cu2O13 | 2 M KOH | 75.2 | -267 | J. Am. Chem. Soc. 142, 6400–6408 (2020) |
| OD-Cu14 | 1 M KHCO3 | 74.9 | -224.7 | J. Am. Chem. Soc. 144, 259−269 (2022) |
| N-Cu15 | 1M KOH | 73.7 | -810.7 | J. Am. Chem. Soc. 144, 14936–14944 (2022) |
| Cu-CuI16 | 1 M KOH | 71 | -591 | Angew. Chem. Int. Ed. 60, 14329−14333 (2021) |
| Cu-D17 | 1 M KOH | 64 | -255 | J. Am. Chem. Soc. 143, 8011−8021 (2021) |

Supplementary Note 1. Data extraction.

In the preparation phase of extracting materials from the Materials Project (MP) database, we obtained all materials containing Cu2+ used the pymatgen package with Python code.18 Here, in the potential candidates, one metal element Cu and the non-metal elements (B, C, N, O, F, Si, P, S, Cl, Br, I, Se) are considered. A total of 83 candidates were obtained for the further high-throughput screening.

Supplementary Note 2. Materials.

Copper nitrate trihydrate (Cu(NO3)2·3H2O) was purchased from Aladdin, and Ammonium dihydrogen phosphate (NH4H2PO4) was obtained from Sinopharm Chemical Reagent Co., Ltd. Citric acid monohydrate (C6H10O8) was purchased from Shanghai Lingfeng Chemical Reagent Co., Ltd. Ammonium fluoride (NH4F), carbon paper (TGP-H-060) and Nafion 117 proton exchange membrane were bought from Alfa Aesar. Potassium hydroxide (KOH), Potassium bicarbonate (KHCO3) and iso-propyl alcohol (AR, ≥99.0%) were obtained from Shanghai Chemical Reagent Co., Ltd. Deuterium oxide (D2O) was bought from J&K Scientific Ltd. Dimethyl sulfoxide (DMSO, C2H6OS), Nafion (5 wt% in a mixture of lower aliphatic alcohols and water) was obtained from Sigma-Aldrich. Carbon dioxide (CO2, 99.9999%) was bought from Shanghai Jiajie Special Gas Co., Ltd. All reagents were commercially available as analytical grade. All water used was purified with a Millipore system (typically 18.2 MΩ cm resistivity).

References

- Xie, Y. et al. High carbon utilization in CO2 reduction to multi-carbon products in acidic media. Nat. Catal. 5, 564−570 (2022).

- Zhong, D. et al. Coupling of Cu(100) and (110) facets promotes carbon dioxide conversion to hydrocarbons and alcohols. Angew. Chem. Int. Ed. 60, 4879−4885 (2021).

- Ma, W. et al. Electrocatalytic reduction of CO2 to ethylene and ethanol through hydrogen-assisted C–C coupling over fluorine-modified copper. Nat. Catal. 3, 478−487 (2020).

- Kibria, M. G. et al. A surface reconstruction route to high productivity and selectivity in CO2 electroreduction toward C2+ hydrocarbons. Adv. Mater. 30, 1804867 (2018).

- Zhang, X. et al. Selective and high current CO2 electro-reduction to multicarbon products in near-neutral KCl electrolytes. J. Am. Chem. Soc. 143, 3245−3255 (2018).

- Wang, P. et al. Boosting electrocatalytic CO2–to–ethanol production via asymmetric C–C coupling. Nat. Commun. 13, 3754 (2022).

- Wang, P. et al. Synergized Cu/Pb core/shell electrocatalyst for high-efficiency CO2 reduction to C2+ liquids. ACS Nano 15, 1039−1047 (2020).

- Gao, D. et al. Selective CO2 electroreduction to ethylene and multicarbon alcohols via electrolyte-driven nanostructuring. Angew. Chem. Int. Ed. 58, 17047−17053 (2019).

- Song, Y. et al. B-Cu-Zn Gas Diffusion Electrodes for CO2 Electroreduction to C2+ products at high current densities. Angew. Chem. Int. Ed. 60, 9135−9141 (2021).

- Zhou, Y. et al. Dopant-induced electron localization drives CO2 reduction to C2 hydrocarbons. Nat. Chem. 10, 974−980 (2018).

- Pham, T. H. M. et al. Enhanced electrocatalytic CO2 reduction to C2+ products by adjusting the local reaction environment with polymer binders. Adv. Energy Mater. 12, 2103663 (2022).

- Miao, R. K. et al. Electroosmotic flow steers neutral products and enables concentrated ethanol electroproduction from CO2. Joule 5, 2742−2753 (2021).

- Wu, Z.-Z. et al. Identification of Cu(100)/Cu(111) interfaces as superior active sites for CO dimerization during CO2 electroreduction. J. Am. Chem. Soc. 144, 259−269 (2022).

- Chen, Z. et al. Grain-boundary-rich copper for efficient solar-driven electrochemical CO2 reduction to ethylene and ethanol. J. Am. Chem. Soc. 142, 6878−6883 (2020).

- Zheng, M. et al. Electrocatalytic CO2-to-C2+ with ampere-level current on heteroatom-engineered copper via tuning *CO intermediate coverage. J. Am. Chem. Soc. 144, 14936−14944 (2022).

- Li, H. et al. High-rate CO2 electroreduction to C2+ products over a copper-copper iodide catalyst. Angew. Chem. Int. Ed. 60, 14329−14333 (2021).

- Niu, Z.-Z. et al. Hierarchical copper with inherent hydrophobicity mitigates electrode flooding for high-rate CO2 electroreduction to multicarbon products. J. Am. Chem. Soc. 143, 8011−8021 (2021).

- Jain, A. et al. Commentary: the materials project: a materials genome approach to accelerating materials innovation. APL Mater. 1, 011002 (2013).