Crosslinking modification of polyamide composite membranes toward high performance for DMAc/H2O dehydration

Wenzhong Ma a, b*, Ziang Wei a , Jing Zhong b*, Chao Jiang b, Xiangyuan Songa, Guorui Yuana, Zaiqi Cheng a, Binghao Ma a, Hideto Matsuyama c

a Jiangsu Key Laboratory of Environmentally Friendly Polymeric Materials, National Experimental Demonstration Center for Materials Science and Engineering, School of Materials Science and Engineering, Changzhou 213164, Jiangsu, P. R. China

b Jiangsu Key Laboratory of Advanced Catalytic Materials and Technology, School   of  Petrochemical  Engineering,  Changzhou  University, Changzhou          213164,           China

c Research Center for Membrane and Film Technology, Department of Chemical Science and Engineering, Kobe University, 1-1 Rokkodai, Nada-ku, Kobe 657-8501, Japan

Wenzhong Ma, Email: wenzhong-ma@cczu.edu.cn

Jing Zhong, Email: zjwyz@cczu.edu.cn

Herein, the effects of the interfacial polymerization conditions on the pervaporation performance of the TEPA-PA TFC membrane (including the contact time and concentrations of the organic/water phases) were systematically described. The pervaporation separation of a 90 wt% DMAc/H2O system through the TEPA-PA TFC membrane at 30 °C was investigated.

The effect of different organic/water phase contact times on the pervaporation performance of the TEPA-PA membranes was investigated, as shown in Fig. S1a. In this case, the TEPA concentration in the water phase and the TMC concentration in the organic phase were set at 2 wt% and 0.15 wt%, respectively. The organic/water phase contact time ranged from 10 to 120 s. When the contact time was 30 s, the permeate flux and the water content on the permeate side were 0.1 L m–2·h–1 and 81.3 wt%, respectively. With increasing contact time, the permeate flux eventually decreased, and the water content on the permeate side increased gradually. When the contact time was 90 s, the trend for permeate flux and water content on the permeate side was stable. The permeate flux achieved a value of 0.073 L m–2·h–1, and the water content on the permeate side was 96.3 wt%. This was mainly due to an increase in the contact time, i.e., an increase in the reaction time that allowed for a denser separation layer.

The pervaporation performance of the TEPA-PA TFC membranes synthesized from different aqueous-phase concentrations (from 0.5 to~2.5 wt%) and organic phase concentrations (from 0.05 to~0.2 wt%) was investigated, as shown in Fig. 7b and c, respectively. When synthesizing these TEPA-PA TFC membranes, the TMC concentration in the organic phase solutions was set to 0.15 wt%, while the organic/water phase contact time was defined to be 90 s. When the TEPA concentration was 0.5 wt%, the permeate flux, and the permeate-side water content were 0.098 m-2 h-1 bar-1 and 39.6 wt%, respectively. At smaller TEPA concentrations, the TEPA-PA TFC membrane exhibited a higher permeate flux and a smaller water content on the permeate side. With increasing TEPA concentration, the permeate flux decreased, and the water content on the permeate side increased. This may be attributed to the denser PA layer that was formed at higher TEPA concentrations. The TEPA-PA TFC membrane was derived from 2 wt% TEPA that reacted for 90 s with different TMC-content organic-phase solutions (Fig. S1c). For a TMC concentration of 0.15 wt%, the trend of the permeate flux and the permeate-side water-content values stabilized at 0.066 L m–2·h–1 and 96.6 wt%, respectively. As the concentration of TMC increased, the trend in the pervaporation performance was similar to that of the TEPA-content effect.

Fig. S1. Effects of different interfacial polymerization conditions (a–c) on the pervaporation performance of the TEPA-PA TFC membrane due to: (a) organic/water phase contact time; (b) TEPA concentration in the aqueous phase; (c) TMC concentration in the organic phase;