Supplementary Material

Behavior and mechanisms of ciprofloxacin adsorption on aged Polylactic Acid and Polyethylene microplastics

Table Captions

Table S1 Physicochemical properties of microplastics (MPs) used in this study.

Table S2 Internal diffusion parameters for the adsorption of Ciprofloxacin (CIP) onto microplastics (MPs).

Table S3 Thermodynamic parameters for the adsorption of Ciprofloxacin (CIP) onto microplastics (MPs).

Table S4 Significance analysis of the difference of the influence factors at p 0.05 level.

Table S1 Physicochemical properties of microplastics (MPs) used in this study.

| MPs | surface area m2 /g | Total hole volume cm³/g | Contact angle ° |
| --- | --- | --- | --- |
| Original PLA | 1.7915 | 0.021023 | 71.22 |
| Aged PLA | 4.2525 | 0.032908 | 69.88 |
| Original PE | 0.6978 | 0.001273 | 87.5 |
| Aged PE | 1.0016 | 0.001152 | 83.97 |

Table S2 parameters of Webber-Morris model for CIP adsorption on Microplastics.

| MPs | Stage I |  |  | Stage II |  |  | Stage III |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Kip1a | C1 | R2 | Kip2a | C2 | R2 | Kip3a | C3 | R2 |
| Original PLA | 0.153 | 0.217 | 0.93 | 0.005 | 0.359 | 0.812 | 0.003 | 0.382 | 0.491 |
| Aging PLA | 0.046 | 0.292 | 0.65 | 0.007 | 0.415 | 0.600 | 0.004 | 0.432 | 0.85 |
| Original PE | 0.055 | 0.037 | 0.86 | 0.001 | 0.271 | 0.114 | - | - | - |
| Original PE | 0.021 | 0.034 | 0.85 | -0.002 | 0.167 | 0.544 | - | - | - |

a (mg/ (g-min1/2 )).

Table S3 Thermodynamic parameters for the adsorption of norfloxacin (NOR) onto microplastics (MPs).

| MPs |  | Temperature/K | LnKc | ΔG/ kJ-mol- 1 | ΔH/ kJ-mol- 1 | ΔS/kJ-(mol -K)-1 |
| --- | --- | --- | --- | --- | --- | --- |
| r | Original PLA | 288 | -2.52 | 6.03 | 18.24 | 0.042 |
|  |  | 298 | -2.38 | 5.90 |  |  |
|  |  | 308 | -2.02 | 5.18 |  |  |
|  | Aging PLA | 288 | -1.81 | 4.33 | 10.15 | 0.020 |
|  |  | 298 | -1.73 | 4.28 |  |  |
|  |  | 308 | -1.53 | 3.93 |  |  |
|  | Original PE | 288 | -2.80 | 6.69 | 27.02 | 0.069 |
|  |  | 298 | -2.74 | 6.78 |  |  |
|  |  | 308 | -2.06 | 5.27 |  |  |
|  | Aging PE | 288 | -2.20 | 5.26 | 8.74 | 0.012 |
|  |  | 298 | -2.12 | 5.26 |  |  |
|  |  | 308 | -1.96 | 5.02 |  |  |

Table S4 Significance analysis of the difference of the influence factors at p 0.05 level.

| MP type Influence factors |  | PLA | Aged PLA | PE | Aged PE |
| --- | --- | --- | --- | --- | --- |
| pH | 3 | c | b | b | b |
|  | 5 | ab | a | ab | ab |
|  | 7 | ab | a | a | ab |
|  | 9 | a | a | a | a |
|  | 11 | bc | a | ab | ab |
| NaCl (%) | 0 | a | a | a | a |
|  | 0.5 | ab | b | ab | b |
|  | 1 | b | bc | b | b |
|  | 2 | b | cd | b | b |
|  | 3.5 | b | d | b | b |
| fulvic acid concentration (mg/L) | 0 | a | a | a | a |
|  | 5 | bc | b | b | b |
|  | 10 | bc | b | c | c |
|  | 15 | c | b | c | c |
|  | 20 | b | a | b | ab |
| NOR concentration (mg/L) | 0 | a | a | a | a |
|  | 1 | b | b | b | b |
|  | 2 | b | ab | b | b |
|  | 3 | ab | ab | b | b |
|  | 4 | ab | ab | ab | ab |
|  | 5 | ab | ab | b | b |