# Supplementary Material - Thermal Fractional Diffusion: Experimental Evidence from the Discrepancies in the Amplitude and Phase in Photothermal Technique

A. Somera,∗, A. Novatskia, Gerson Kniphoff da Cruza, Claudia Bonardi Kniphoff da Cruza, Francisco Carlos Serbenaa, Ervin Kaminski Lenzia

aDepartamento de Física, Universidade Estadual de Ponta Grossa, Av. Gen. Carlos Cavalcanti 4748, Ponta Grossa 84030-900, PR, Brazil

## Results of the fit of experimental data

The best fits by using the classical model for simultaneous (orange) and individual (blue) are shown in figure. The obtained parameters from NonLinearModelfit for the fit shown in figure S1 are presented in Table S1. The A Fit represents the induvial fit for the amplitude of the PA signal, represented by the solid blue line. The ∅ Fit represents the induvial fit for the phase of the PA signal, represented by the solid blue line. The Classic is the result of the solid orange line, which represents the simultaneous fit of amplitude and phase of the PA signal with the classical model. The comparison between the results of the best simultaneous fit with GCEII (orange) and the Classical result (blue) is shown in Figure S2, and for GCEIII, it is shown in Figure S3. Table S1 provides the fitted parameters. The green lines are the TD and TE contributions for the fractional models.

Table S1 – Parameters obtained from the fit of one set of measurements of each sample for the results presented in Figures S1 and S2. The Classical, GCEII and GCEIII results are obtained from Simultaneous Fit of Amplitude and Phase.

| Sample | Fit | C1 (a. u.) | C2 (10-3 m.s1/2) | αs (10-6 m²/s) | fc2 (Hz) | δc3 | τ (10-5 s) | γ | R² |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A285 | A Fit | 325 | 1.86 | 4.467 | 8.3 | 1.5 | - | - | 0.9998 |
|  | ∅ Fit | 1400 | 1.83 | 3.432 | 35 | 0.75 | - | - | 0.9999 |
|  | Classical | 232 | 2.08 | 4.084 | 20 | 0.86 | - | - | 0.9997 |
|  | GCEII | 255 | 4.34 | 4.107 | 33 | - | 2.82 | 0.924 | 0.9999 |
|  | GCEIII | 250 | 3.05 | 5.005 | 20 | - | 4.09 | 0.999 | 0.9999 |
| A400 | A Fit | 298 | 2.15 | 6.363 | 13 | 2.2 | - | - | 0.9998 |
|  | ∅ Fit | 939 | 1.27 | 4.750 | 30 | 1.20 | - | - | 0.9985 |
|  | Classic | 302 | 2.11 | 6.340 | 14 | 1.36 | - | - | 0.9996 |
|  | GCEII | 459 | 1.67 | 4.189 | 19 | - | 5.00 | 0.998 | 0.9994 |
|  | GCEIII | 401 | 1.92 | 5.250 | 17 | - | 4.98 | 0.999 | 0.9994 |
| A480 | A Fit | 206 | 3.21 | 5.983 | 9.0 | 2.00 | - | - | 0.9998 |
|  | ∅ Fit | 511 | 2.13 | 5.267 | 9.7 | 1.71 | - | - | 0.9998 |
|  | Classic | 220 | 3.16 | 5.644 | 10 | 1.44 | - | - | 0.9998 |
|  | GCEII | 385 | 1.17 | 4.035 | 13 | - | 6.82 | 0.997 | 0.9998 |
|  | GCEIII | 354 | 1.97 | 4.233 | 11 | - | 6.78 | 0.962 | 0.9998 |
| A600 | A Fit | 150 | 4.59 | 7.293 | 8.3 | 2.23 | - | - | 0.9999 |
|  | ∅ Fit | 919 | 2.97 | 6.297 | 6.2 | 1.09 | - | - | 0.9998 |
|  | Classic | 167 | 4.50 | 6.615 | 8.5 | 0.77 | - | - | 0.9996 |
|  | GCEII | 342 | 2.16 | 4.633 | 15 | - | 4.23 | 0.997 | 0.9996 |
|  | GCEIII | 394 | 1.86 | 4.299 | 15 | - | 4.04 | 0.934 | 0.9996 |

Figure S1 – Experimental data and the curves obtained from the fitted parameters with the classical model of one set of measurements for each sample.

Figure S2 – Experimental data and the curves obtained from the fitted parameters with the fractional GCEII model of one set of measurements for each sample.

Figure S3 – Experimental data and the curves obtained from the fitted parameters with the fractional GCEIII model of one set of measurements for each sample.