Supplementary Information for Permittivity Boosting by Induced Strain from Local Doping in Titanates from First Principles

Alex Kutana, Yuho Shimano, Ryoji Asahi

The parent compound for substituted perovskites is a paraelectric calcium titanate CaTiO3 (mineral perovskite) that crystallizes into an orthorhombic Pnma (62) phase at low temperatures;1 the observed high temperature phases include tetragonal I4/mcm (140), and a cubic Pm3m (221) phase for T>1580 K.2,3 The breaking of the ideal cubic Pm3m symmetry occurs by a−a−c+ tilting of the TiO6 octahedra. Our calculated average ionic dielectric constant for this material at PBEsol lattice constant is 124, in the range of previously reported theoretical values4 ~93-268, which varied depending on whether a theoretical (LDA) or experimental value of the lattice constant was used. The Ruddlesden-Popper phases5,6 Sr2TiO4 and Sr3Ti2O7 have the I4/mmm (139) symmetry, and TiO2 rutile has the P42/mnm (136) symmetry.

Figure S1. Ionic part of the dielectric constant, εion, as a function of max(dTi-O), the maximum length of the Ti-O bond in co-doped TiO2 rutile. The vertical line at max(dTi–O)=2.036 Å is drawn to guide the eye.

Figure S2. εion of TiO2 rutile as a function of uniaxial and uniform strain.

Figure S3. εion of SiO2, SnO2 rutile structures as a function of uniaxial and uniform strain.

Table S1. Phonon modes of Pnma CaTiO3 contributing to dielectric constant.

|  | ν (THz) | εpartial | mode # |
| --- | --- | --- | --- |
| εxx |  |  |  |
|  | 3.828 | 109.1 | 6 |
|  | 5.026 | 19.9 | 12 |
|  | 6.379 | 2.5 | 21 |
| εyy |  |  |  |
|  | 4.021 | 96 | 7 |
|  | 5.222 | 24.1 | 14 |
|  | 9.172 | 2.6 | 31 |
|  | 15.56 | 2.2 | 53 |
| εzz |  |  |  |
|  | 3.599 | 22.4 | 5 |
|  | 4.432 | 55.0 | 9 |
|  | 5.668 | 26.3 | 16 |
|  | 15.90 | 2.5 | 55 |

Table S2. Ionic part of the dielectric tensor in substituted and co-doped titanates shown in Fig. 2.

| compound | εxx | εyy | εzz |
| --- | --- | --- | --- |
| CaTiO3 | 136.0 | 126.9 | 108.2 |
| Ba2Sr2Ti4O12 | 697.0 | 407.2 | 9015.2 |
| Ba2Ca2Ti4O12 (α) | 92.8 | 53.4 | 1228.7 |
| Ba2Ca2Ti4O12 (β) | 105.1 | 432.5 | 564.2 |
| BaCa3Ti4O12 | 175.4 | 186.3 | 252.4 |
| Ti6InNbO16 | 213.4 | 106.6 | 2767.9 |
| Ti2O4 | 125.8 | 125.8 | 169.0 |

Table S3. Born effective charges Z*κ,zz in BaxSryCa1−x−yTiO3. O1 atoms are part of Ti-O chains aligned with the z axis, O2 atoms are part of other Ti-O chains. For symmetry inequivalent atoms in substituted structures, maximum value is taken.

|  | Ca | Sr | Ba | Ti | O1 | O2 |
| --- | --- | --- | --- | --- | --- | --- |
| CaTiO3 | 2.38 | – | – | 7.32 | -5.76 | -1.97 |
| Ba2Sr2Ti4O12 | – | 2.54 | 2.7 | 7.69 | -6.35 | -2.09 |
| Ba2Ca2Ti4O12 (α) | 2.51 | – | 2.62 | 7.30 | -6.12 | -2.06 |
| Ba2Ca2Ti4O12 (β) | 2.51 | – | 2.61 | 7.57 | -6.16 | -2.11 |
| BaCa3Ti4O12 | 2.46 | – | 2.66 | 7.41 | -6.14 | -2.07 |
| BaTiO3 | – | – | 2.72 | 7.74 | -6.16 | -2.15 |

Table S4. U values used for Hubbard correction applied to d electrons.

| el | O | Mg | Al | Ca | Sc | Ti | V | Cr | Ga | Sr | Y | Zr | Nb | Mo | In | Ba |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| U (eV) | 0 | 0 | 0 | 0 | 0 | 0 | 3 | 3 | 0 | 0 | 3 | 3 | 3 | 3 | 0 | 0 |

| el | La | Hf | Ta | W | Pb |
| --- | --- | --- | --- | --- | --- |
| U (eV) | 3 | 3 | 3 | 3 | 0 |

The atomic structures and calculated properties are provided in json format.

References

(1)	Kay, H. F.; Bailey, P. C. Structure and Properties of CaTiO3. Acta Crystallogr. 1957, 10 (3), 219–226. https://doi.org/10.1107/S0365110X57000675.

(2)	Kennedy, B. J.; Howard, C. J.; Chakoumakos, B. C. Phase Transitions in Perovskite at Elevated Temperatures - a Powder Neutron Diffraction Study. J. Phys. Condens. Matter 1999, 11 (6), 1479–1488. https://doi.org/10.1088/0953-8984/11/6/012.

(3)	Yashima, M.; Ali, R. Structural Phase Transition and Octahedral Tilting in the Calcium Titanate Perovskite CaTiO3. Solid State Ion. 2009, 180 (2), 120–126. https://doi.org/10.1016/j.ssi.2008.11.019.

(4)	Cockayne, E.; Burton, B. P. Phonons and Static Dielectric Constant in CaTiO3 from First Principles. Phys Rev B 2000, 62 (6), 3735–3743. https://doi.org/10.1103/PhysRevB.62.3735.

(5)	Ruddlesden, S. N.; Popper, P. New Compounds of the K$\sb 2$NIF$\sb 4$ Type. Acta Crystallogr. 1957, 10 (8), 538–539. https://doi.org/10.1107/S0365110X57001929.

(6)	Ruddlesden, S. N.; Popper, P. The Compound Sr$\sb 3$Ti$\sb 2$O$\sb 7$ and Its Structure. Acta Crystallogr. 1958, 11 (1), 54–55. https://doi.org/10.1107/S0365110X58000128.