S1. Characterization of MChi

The MChi was examined by FTIR, SEM/EDAX, TEM, XRD, VSM, BET, and TGA techniques. Fourier transform infrared (FTIR, Nicolet IS50 Thermo Fisher Scientific) spectroscopy was used to examine the functional groups of the MChi in the 4000 to 400 cm−1 region. A scanning electron microscopy (SEM) equipped with energy dispersive X-ray analysis (EDAX) (JEOL, JSM6510LV, Japan) was used to detect the surface morphology and elemental composition of the MChi. Transmission Electron Microscope (TEM, JEOL, 2100) was used to scrutinize the particle shape of the MChi nanocomposite. The specific surface area and pore structure of the adsorbent were obtained by N2 ad-/de-sorption test (Micromeritics ASAP, 2020). X-ray diffraction (XRD) analysis of the composite was executed using an X-ray diffractometer (MiniFlex™ II benchtop XRD system, Rigaku Corporation, Tokyo, Japan) in the 2θ range of 10-80° at 40 kV and a current of 30 mA. Thermogravimetric analysis of the MChi was executed using the thermogravimetric analyzer (TGA, Perkin Elmer, 8000). The sample was heated at 30 °C min-1 from 30 to 800 °C under the N2 flow. Magnetic properties were estimated using a vibrating sample magnetometer (VSM, Lakeshore, 7410) at room temperature with a maximum magnetic field of 20 kOe.

The point of zero charge (pHPC) of the MChi was determined using the procedure given in the literature (Mashkoor and Nasar, 2020c). In brief, the initial pH (pHo) of the 0.1 M solution of KNO3 (30 ml) was adjusted to a pH range of 3 to 12 using 0.1 M HCl or NaOH solution. After adding 0.025g of MChi to each solution, the flasks were firmly covered and kept in a dark place for 48 h at room temperature. The final pH (pHf) of the solutions was recorded. Finally, the pHPC was obtained from the intersection point on the pHo-axis of the ∆pH (= pHo-pHf) vs. pHo plot.