Extraction and surface modification of cellulose fibers and its reinforcement in starch-based film for packaging composites

Halimatun Saadiah Hafida,*, Farah Nadia Omarb,*, Ezyana Kamal Bahrinc,d,Minato Wakisakae

aInstitute of Plantation Studies, Universiti Putra Malaysia, 43400 UPM Serdang, Selangor, Malaysia

bPreparatory Center for Science and Technology (PPST), Universiti Malaysia Sabah, Jalan UMS, 88400 Kota Kinabalu, Sabah, Malaysia

cInstitute of Plantation Studies, Universiti Putra Malaysia, 43400, UPM Serdang, Selangor, Malaysia

dCentre of Foundation Studies for Agricultural Science, Universiti Putra Malaysia, 43400, UPM Serdang, Selangor, Malaysia

eGraduate School of Life Science and Systems Engineering, Kyushu Institute of Technology, 2-4 Hibikino, Wakamatsu-ku, Kitakyushu, 808-0196, Japan

Corresponding authors:

farahnadiaomar@ums.edu.my

halimatun@upm.edu.my

SUPPORTING INFORMATION

List of Tables

Table S1 Level of independent variables used in Box-Behnken design

Table S1. Level of independent variables used in Box-Behnken design

| Variables | Coded level |  |  |
| --- | --- | --- | --- |
|  | Low (-1) | Center (0) | High (1) |
| Temperature (C) | 60 | 75 | 90 |
| Ultrasonic power (%) | 60 | 70 | 80 |
| Time (hour) | 1.0 | 1.5 | 2.0 |